## Slide 1
MONOLITHIC PIXEL DETECTORS
Walter Snoeys
  Acknowledgements
  Collegues in ESE group and Alice Pixel, LHCb RICH, NA57, WA97, RD19, TOTEM and LePIX Collaborations
  S. Parker, C. Kenney, C.H. Aw, G. Rosseel, J. Plummer
  E. Heijne, M. Campbell, E. Cantatore, …
  K. Kloukinas, W. Bialas, B. Van Koningsveld, A. Marchioro…
  A. Potenza, M. Caselle, C. Mansuy, P. Giubilato, S. Mattiazzo, D. Pantano, A. Rivetti, Y. Ikemoto, L. Silvestrin, D. Bisello, M. Battaglia
  P. Chalmet, H. Mugnier, J. Rousset
  T. Kugathashan, C. Tobon, C. Cavicchioli, L. Musa
  A. Dorokhov, C. Hu, C. Colledani, M. Winter
  I. Peric

## Slide 2
MONOLITHIC DETECTORS : definition
Integrate the readout circuitry – or at least the front end – together with the detector in one piece of silicon
The charge generated by ionizing particle is collected on a designated collection electrode
Readout circuit
Collection electrode
Sensitive layer
High energy particle

## Slide 3
Motivation:
  Easier integration, lower cost, possibly better power-performance ratio
  Promising not only for pixel detectors, but also for full trackers
  Potential of strong impact on power consumption and hence on material in high energy physics experiments
Difference between high energy physics and traditional imaging:
  single particle hits instead of continuously collected signal
Now in two experiments:
  DEPFET pixels in Belle-II
  MAPS in STAR experiment
both relatively slow (row by row) readout, not always applicable
Not yet in LHC, considered for upgrades (eg Alice) and for CLIC/ILC
MONOLITHIC DETECTORS

## Slide 4
DEPFET (MPI MUNICH)
An example in special technology
  An annular PFET on top of a fully depleted substrate (back side junction).
  A potential well under the gate area collects the charge generated in the substrate.
  The potential of this potential well changes with collected charge and modulates the PFET source-drain current.
  Charge collection continues even if DEPFET is switched off.
  Clear gate allows reset of the potential well.
  The readout can occur via the source (voltage out), or via the drain (current out)
  Very small collection electrode capacitance, allows high S/N operation.
  Need steering and rest of readout off chip or on another chip.
500pA/e-

## Slide 5
  Cfr M. Winter’s presentation
  Commercial CMOS technologies
  Very few transistors per cell
  Pixel size : 20 x 20 micron or lower
  Charge collection by diffusion, more sensitive to bulk damage (see next slides)
  Serial readout, slower readout
  Time tagging can be envisaged but would like to have faster signal collection, and will need extra power.
Monolithic Active Pixel Sensors (MAPS)
RESET
COLUMN BUS
ROW SELECT
Example: three transistor cell
cfr. M. Winter et al

## Slide 6
Main challenges in high energy physics:
          radiation tolerance and power consumption
Key parameters:
    Charge collection mechanism: drift vs diffusion
        Collected charge over input capacitance ratio & architecture
            Technology
MONOLITHIC DETECTORS

## Slide 7
Collection by diffusion – ex.: standard MAPS*
MAPS: Monolithic Active Pixel Sensors
Need collection by drift for radiation tolerance beyond a few 1013neq/cm2 !
(A. Dorokhov et al., IPHC, France)

## Slide 8
Drift vs diffusion – influence on cluster size
Measurement on LePIX prototypes (50x50 micron pixels !)
0 Volts bias
Diffusion: at zero bias, incident protons generate on average clusters of more than 30 50x50 micron pixels.
Drift: for significant reverse bias (60V) cluster reduced to a few pixels only
60 Volts bias

## Slide 9
Services: cables, power suppliers, cooling etc… represent signficant effort and fraction of the total budget
Subject to severe spatial constraints, limit for future upgrades
Power often consumed at CMOS voltages, so kWs mean kAs
                Even if power for detector is low, voltage drop in the cables has to be minimized: example analog supply one TOTEM Roman Pot:
                ~ 6A @ 2.5 V
                ~100m 2x16mm2 cable: 0.1 ohm or 0.6 V drop one way
                26kg of Copper for ~ 15 W
Low power is key to low mass
W. Snoeys – Legnaro, April 2013

## Slide 10
The CMS tracker before dressing…

## Slide 11
… and after
11
33 kW in the detector and… 62 kW in the cables !

## Slide 12
12

## Slide 13
… and after
13

## Slide 14: Tracker power and material budget
ATLAS
CMS
W. Snoeys – Legnaro, April 2013

## Slide 15
Low power is key for low mass
Now ~ 20mW/cm2 for silicon trackers and > 200 mW/cm2 for pixels
Cannot increase this by much, but upgrades consider more luminosity & functionality (trigger…), so more for less or equal power.
  Lower analog power: see next slides
  Lower digital power: look for new architectures (example next slide)
  Lower power for data transmission: may well be ultimate limit
  Lower detector power after radiation damage cannot exploit 300 microns thick depletion : after heavy fluence (except 3D detectors).
Would like to improve assembly/integration, need to profit from industry’s automation
What next ?
W. Snoeys – Legnaro, April 2013

## Slide 16: Architecture example: reduce number of signals Orthopix n-maps orthogonal static sparsification
Encoding
Purity
(x1,y1)
(x2,y2)
…
(xp,yp)
(xp+1,yp+1)
(xr,yr)
…
(xn,yn)
Decoding
X
X
X
X
X
O
Minimize ambiguity introducing orthogonal projections
For 4 projections reduction from N2 to 4N

## Slide 17: Analog Power Consumption: Noise sources in a FET
EQUIVALENT WITH :
WHERE:
In weak inversion (WI): gm ~ I
dveq2 = (KF /(WLCox2fα)+ 2kTn/gm)df
In strong inversion (SI) gm ~ √I
dveq2 = (KF /(WLCox2fα)+ 4kTγ/gm)df
dieq2
dieq2 = gm2dveq2
Transconductance gm related to power consumption
W. Snoeys – Legnaro, April 2013

## Slide 18: Noise sources in a FET (2)
NMOS
PMOS
Note : Radiation tolerance (0.25 mm CMOS) !
Deeper submicron generally even more rad tolerant
W. Snoeys – Legnaro, April 2013

## Slide 19
Analog power is very strongly dependent on Q/C
Want SMALL electrode for low C
m = 2 for weak inversion up to 4 for strong inversion
or
For constant S/N:
Signal-to-noise, charge over input capacitance ratio and
analog power consumption for MOS input transistor
W. Snoeys – Legnaro, April 2013

## Slide 20
HIGH Q/C FOR LOW POWER
+
+
+
+
-
-
-
-
+
+
+
+
-
-
-
-
+
+
+
-
-
-
-
+
n+
p=
V=
300 mm
30 mm
3 mm
Collection depth
doubling Q/C allows
(at least) 4x power reduction for same S/N
Transistor noise ≈ 0.16 mV at 40 MHz BW for 1 uA
(1uA/100x100 um pixel = 10 mW/sq cm)
Q/C = 50mV (0.25fC/5fF=50mV) can be achieved
(e.g. for 20 um collection depth and 5fF)
but need collection by drift
Much better than that would almost be a ‘digital’ signal
Monolithic
W. Snoeys – Legnaro, April 2013

## Slide 21: What is a ‘digital signal’ ? The Boltzmann tyranny
Ion
Ioff
Exp( )
nkT/q
Vgs
Weak
inversion
Strong
inversion
Weak inversion slope ~ 60 mV/decade, Ion/Ioff=104 => 250 mV
Need this on a single pixel !!
W. Snoeys – Legnaro, April 2013

## Slide 22: Standard charge sensitive pulse processing front end (no integration over a fixed time)
ENC: total integrated noise at the output of the pulse shaper with respect to the output signal which would be produced by an input signal of 1 electron. The units normally used are rms electrons.
RESET: switch or high valve resistive element
RESET
Pulse
Processing
H(s)
OTA
Charge Sensitive
Amplifier
Shaper
W. Snoeys – Legnaro, April 2013

## Slide 23
Ref.: Z.Y. Chang and W.M.C. Sansen : ISBN 0-7923-9096-2, Kluwer Academic Publishers, 1991
thermal
1/fnoise
shot noise
ANALOG POWER
‘standard’ front end noise equations
Transconductance gm related to power consumption
W. Snoeys – Legnaro, April 2013

## Slide 24
Ref.: Z.Y. Chang and W.M.C. Sansen : ISBN 0-7923-9096-2, Kluwer Academic Publishers, 1991
Ref. 2 : V. Radeka “Low-noise techniques in detectors” Ann. Rev. Nucl. Sci. 1988, 38, 217-77
Ref. 3 : E. Nygard et al. NIM A 301 (1991) 506-516
Influence of shaper order n
W. Snoeys – Legnaro, April 2013

## Slide 25
Note: for longer integration times
rolling shutter architectures, etc…
Noise often leakage current dominated (shot noise), but significant progress (4T cells, leakage reduction…)
Impressive noise numbers (ENCs of a few electrons down to even subelectron ENC using multiple sampling of reset and signal level.
For high energy physics longer integration not always applicable, also investigating different architectures for lower power
W. Snoeys – Legnaro, April 2013

## Slide 26
Collection electrode
High energy particle
Collection electrode
High energy particle
A uniform depletion layer for uniform response: larger pixels more difficult
Optimal geometry and segmentation of the read-out electrode (minimum C)
Effective charge resetting scheme robust over a large range of leakage currents
Pattern density rules in very deep submicron technologies very restrictive.
Insulation of the low-voltage transistors from the high voltage substrate.
Sensor needs to be designed in close contact with the foundry!
High Q/C yields DEVICE DESIGN challenge
uniform depletion layer with a small collection electrode
W. Snoeys – Legnaro, April 2013

## Slide 27
Additional N-diffusion will collect and cause loss of signal charge
 Need wells to shield circuitry and guide charge to the collection electrode for full efficiency
DEVICE DESIGN challenge
Collect only on collection electrode, not elsewhere
Nwell collection electrode
Psubstrate
Wells with junction on the front
Uniform depletion with small Nwell and large Pwell difficult
Large fields or important diffusion component (MAPS)
Wells with junction on the back. Need full depletion
Psubstrate
Pwell
Collection Electr
Nwell with circuitry
Back side N diffusion
Psubstrate
Pwell
With circuitry
Nwell collection electrode
W. Snoeys – Legnaro, April 2013

## Slide 28: No shielding well
G. Vanstraelen (NIMA305, pp. 541-548, 1991)
V. Re et al., superB development: Nwell containing PMOS transistors not shielded
Nwell much deeper than rest of circuit to limit inefficiency
Nwell collection electrode
Psubstrate
W. Snoeys – Legnaro, April 2013

## Slide 29: Nwell collection electrode surrounded by Pwell containing circuitry
Uniform depletion with small Nwell and large Pwell difficult
Large fields or important diffusion component (cfr MAPs)
  MAPS (NMOS only) or Quadruple well technologies: INMAPS for full CMOS in-pixel
Cfr: Alice ITS upgrade, see also M. Winter’s presentation, also here positive influence of reverse substrate bias
Psubstrate
Pwell
With circuitry
Nwell collection electrode
Deep Pwell
Pwell
P-substrate
Nwell
Nwell Collection Electrode
Pwell
Nwell
P-epitaxial layer
W. Snoeys – Legnaro, April 2013

## Slide 30
P-type collection electrode covers 1/10 of the width.
Full depletion required (otherwise short between the collection electrodes)
At zero well bias and full depletion punchthrough between Nwell and N-diffusion on the back
USE OF A WELL with BACK SIDE JUNCTION
Example of device design and simulation
W. Snoeys – Legnaro, April 2013

## Slide 31
A few volts on the well (with 65 V on the back) diverts all flow lines to the collection electrode because a potential barrier is formed underneath the well.
The back side to Nwell current drops by orders of magnitude as the punchthrough is eliminated.
USE OF A WELL with BACK SIDE JUNCTION
Example of device design and simulation
W. Snoeys – Legnaro, April 2013

## Slide 32
Increasing the well bias increases the potential barrier and moves the potential valley deeper into the substrate
USE OF A WELL with BACK SIDE JUNCTION
Example of device design and simulation
W. Snoeys – Legnaro, April 2013

## Slide 33
Increasing the well bias increases the potential barrier and moves the potential valley deeper into the substrate
USE OF A WELL with BACK SIDE JUNCTION
Example of device design and simulation
W. Snoeys – Legnaro, April 2013

## Slide 34
Operational limits
USE OF A WELL with BACK SIDE JUNCTION
Example of device design and simulation
W. Snoeys – Legnaro, April 2013

## Slide 35
WELL & BACK SIDE JUNCTION (34x125 μm pixel)
Need full depletion, works well
but double-sided process difficult
C=26fF P-type 1E12 cm3
Psubstrate
Nwell with circuitry
Back side N diffusion

## Slide 36
NMOS in Pwell
Would like small collection electrode for minimum capacitance (C)
In-pixel circuitry placed in the Nwell collection electrode prevents loss of signal charge, but:
    Higher input capacitance, unless in-pixel circuit very simple
      special architectures (see P. Giubilato & Y. Ono, pixel 2012, Japan)
      ‘rolling shutter’ or frame readout as in MAPS
      hybridization and use it as smart detector (see next slide & presentation) in hybrid configuration
    Risk of coupling circuit signals into input
ALTERNATIVE: ALL CIRCUITRY IN COLLECTION ELECTRODE
CIRCUIT DESIGN challenge: minimize in-pixel circuit for low C
Nwell collection electrode
Pwell
PMOS in Nwell
P-substrate
W. Snoeys – Legnaro, April 2013

## Slide 37
HEIDELBERG SLIDE 1
I. Peric et al.
Radiation tolerance !

## Slide 38: LePIX: 90 nm CMOS on high resistivity
Try to maximize Q/C: small collection electrode, and high resistivity substrate of several 100 Ωcm, 40 microns depletion for ~40 V, 90nm CMOS
-V
P+
P+
Biasing diode
Readout
P- substrate.
Edge of depletion layer
N+
P+
N well
Collection electrode
D
One cell
Minimize size
P- substrate
Edge of depletion layer
-V
D
Guard ring structure
Pixel cells with Nwell diffusion
Substrate contact
Peripheral readout circuit embedded in Nwell and also surrounded by the guard ring
W. Snoeys – Legnaro, April 2013

## Slide 39
LePIX: 300 GeV pions at SPS
W. Snoeys – Legnaro, April 2013
LePIX: 90 nm CMOS on high resistivity
(cfr P. Giubilato et al, Pixel 2012, Japan)
Counts [-]
Cluster peak [ADC counts]

## Slide 40
W. Snoeys – Legnaro, April 2013
Low bias (20V)
π
p
p Landau tail
Cluster multiplicity [pxls]
p
Cluster mass [ADC counts]
π
p
High bias (60V)
p Landau tail
π
LePIX: 90 nm CMOS on high resistivity
Influence of back bias
LePIX with 300 MeV pions and protons at PSI cyclotron

## Slide 41
W. Snoeys – Legnaro, April 2013
LePIX: 90 nm CMOS on high resistivity
(cfr P. Giubilato et al, Pixel 2012, Japan)
LePIX with 55Fe source at room temperature
Calibration peak (5.9 keV)
m: 5.90 keV (269 ADC)
σ: 136 eV (6.2 ADC)
Small peak (6.49 keV)
m: 6.45 keV (294 ADC)
σ: 143 eV (6.5 ADC)
Counts [-]
ADC counts [-]

## Slide 42: Silicon on Insulator (SOI)
Y. Arai et al
Very impressive technology development … offers good Q/C
BOX causes reduced radiation tolerance, double BOX likely to improve this.
W. Snoeys – Legnaro, April 2013

## Slide 43
CHARGE COUPLED DEVICES (CCD)
  Signal charge is collected in potential well under a gate and then transferred from one location to the next => serial readout needing large drive currents for large area devices
  Increase speed ColumnParallelCCD (CPCCD) Readout per column in parallel
  Interesting development (figure above LCFI collaboration): In Situ Storage Sensor: store hits and read out during quiet periods, need special technology (combination of CCD and CMOS)
W. Snoeys – Legnaro, April 2013

## Slide 44
Silicon Avalanche Photo Diodes
  Large and fast signals, radiation tolerance to be investigated further
  TOTEM experiment is looking at avalanche photodiodes as one of the possibilities to try to reach 10 picoseconds in its Roman Pots
  One nice development by Sebastian White et al.(separate APD matrix)
  Single photon avalanche diodes (SPAD)
  E. Charbon et al ISSCC 2011
W. Snoeys – Legnaro, April 2013

## Slide 45
just a few remarks: PROCESSING
CMOS standard processing now on 200 or 300 mm diameter wafers
Processing very high resistivity silicon has some particularities:
High resistivity (detector grade) to be found at larger diameter
Float-zone silicon has many less impurities/defects than Czochralski. These defects pin down dislocations, rendering the material more robust. Float-zone material is MUCH MORE FRAGILE
Several process steps can introduce impurities increasing detector leakage
  Work at higher leakage current (often quickly dominated by radiation induced leakage anyway)
  Try to make certain steps cleaner
  Use gettering techniques, which during processing render defects more mobile and provide traps for these where they are no longer harmful.
More technologies interesting for particle detectors become available
also with high resistivity epitaxial layers
3D assembly might provide ‘holy grail’ of monolithic
significant progress recently(eg SOI development, quadruple well technology)
W. Snoeys – Legnaro, April 2013

## Slide 46
MONOLITHIC DETECTORS
Clearly have transformed the world of photography and imaging in general
Very significant progress even recently, eg subelectron noise by multiple correlated sampling (eg. S. Kawahito, pixel2012).
Presented noise performance, the possibility to simulate and design the device, different approaches for the device, the influence of reverse bias on radiation tolerance and cluster size
In High Energy Physics:
  Already adopted for two experiments (Belle-II and STAR)
  Main option for ITS upgrade in Alice using quadruple well technology, less stringent requirements for radiation tolerance and speed, but high occupancy numbers
  A possible option in CMS, in Atlas HV CMOS also considered for use as a smart sensor
W. Snoeys – Legnaro, April 2013

## Slide 47
MONOLITHIC DETECTORS for HEP
More processes interesting for high energy physics become available
Power consumption: Approaching digital signal from particle hit => ultimately eliminate analog power
  Need sufficient and uniform depletion/collection depth and small collection electrode for sufficient Q/C
  Need appropriate architecture to match or improve present day power consumption (Pixels ~200 mW/cm2,trackers ~20 mW/cm2). Clock distribution to every pixel will eat significant fraction of the total power budget
  Need to reduce power to transmit the data off-chip, may well be ultimate limit.
Radiation tolerance very challenging for inner layers but promising results with HV CMOS
Not ready at the time of LHC detector construction, but might get there for some of the upgrades.
W. Snoeys – Legnaro, April 2013

## Slide 48: Thank You !
W. Snoeys – Legnaro, April 2013