## Slide 1: Radiation effects on position sensitive semiconductor detectors
Gregor Kramberger
Jožef Stefan Institute
Ljubljana, Slovenia

## Slide 2
Silicon detectors are essentially “solid state ionization cells”:
Important numbers
  signal of mip in 300 mm ~ 23000 e
  Saturated velocity of: electrons ~110 mm/ns , ~80 mm/ns (drift time >= 4ns)
  Neff of orders 1012 cm-3 -> in 300 mm 1012 cm-3 corresponds to 70 V
  Required S/N>8 (more conservative 10)
Purpose of the lecture is to understand the concepts rather than list numerous results.
In spite of 2h it is not possible to cover everything and I apology if some topics were left uncovered --- that does not mean they are not important!
Based on my personal experience too much equations and numbers confuse listeners and make them fall asleep. Avoiding them makes the lectures less “scientific”, but maybe more enjoyable. However it is not possible to be completely without …
It is impossible to start without any background. So the important numbers from yesterday…

## Slide 3: Outline
Motivation and basics
  LHC …. HL-LHC, but also other fields
  What are the challenges?
Radiation damage
  Fluence, dose, NIEL
  Macroscopic effects on detector performance
  Influence of radiation to signal and noise
Radiation damage effects in silicon (material studies/engineering)
  Leakage current
  Effective doping concentration and electric field for different silicon materials: FZ, MCZ, DOFZ
  Trapping of the charge
Radiation effects in segmented detectors
  p-in-n, n-in-n and n-in-p sensors
  3D sensors and thin devices
Operation at very high fluences – recent highlights
  Active bulk
  Charge multiplication
Conclusions
Microscopic damage in semiconductor detectors M.Bruzzi
Basics on Silicon Sensors and Detector Systems P. Giubilato
Some overlap with other lectures
At all points shown how to get more radiation hard detectors
Notes: Je commence ma présentation avec la table des matières:
La première chose que je vais vous présenter est pourquoi nous avons besoin de nouveaux détecteurs: Qu’elle est la motivation de développer de nouveaux détecteurs résistantes au rayonnement intense?
En suite je vais présenter la collaboration CERN-RD50 qui travaille sur ce sujet.
En suite je vais vous donnez une brève revue au sujet des dommages du rayonnement dans les détecteurs au silicium
  Je vais commencer par les défauts microscopiques dans le cristal de silicium qui sont produit pendant l'irradiation. La production, la formation et les techniques de mesure des défauts microscopiques. Leur influence sur l'opération des détecteurs
  Je vais parler des dommages macroscopiques qui (comme je le disais auparavant) sont provoqué par les dommages microscopiques: les dommages macroscopiques sont: (1) changement de la concentration effective de dopants (changement de la tension de désertion) (2) augmentation du courrant inverse (Ce qui provoque une augmentation du bruit) (3) perte des charges collectées
En suite je vais parler de approches de RD50 pour développer des détecteurs résistant aux rayonnements: comme le « material and device engineering »cela veut dire :
  on change la concentration des impuretés dans le cristal (par exemple en augmente la concentration en oxygène)
  on change la conception du détecteur (par exemple on construit des détecteurs 3D)
À la fin je vais donner un récapitulatif et la conclusion.

## Slide 4: First considerations about radiation hardness for HEP - SSC
(Detectors and Experiments for the Superconducting Super Collider, pg. 491, Snowmass 1984
1984 considerations for SSC
Now 105 upra
“Silicon strip detectors (near the beam pipe) appear to be limited to…≤ 1032....the 1032 limit could be optimistic.” (PSSC Summary Report pg. 130, 1984)
(Detectors and Experiments for the Superconducting Super Collider, pg. 491, Snowmass 1984
T. Kondo et al, Radiation Damage Test of Silicon Microstrip Detectors, pg. 612, Snowmass 1984

## Slide 5: And we are we know now …
LEP HERA , Tevatron LHC HL-LHC
e+e- 1.5∙1031 cm-2 s-1
pp 1035 cm-2 s-1 ?
high collision rates -> more particles hitting the detectors -> larger damage
(at LHC ~20 collisions every 50 ns at present)
pp 1.4∙1032 cm-2 s-1
pp ~1034 cm-2 s-1
90’
2020
ep 7∙1031 cm-2 s-1
But we are not alone …
medicine – smaller damage
space – smaller damage
fusion reactors – larger damage
Amount of particles that hit the detectors is called fluence:

## Slide 6: The challenge: HL-LHC - visually
SLHC luminosity ~200-400 interactions/bx
LHC luminosity

## Slide 7
Motivation for R&D on Radiation Tolerant Detectors HL-LHC
LHC upgrade LHC (2009) L = 1034cm-2s-1 f(r=4cm) ~ 3·1015cm-2
HL-LHC (>2020) L = 1035cm-2s-1 f(r=4cm) ~ 1.6·1016cm-2
LHC (Replacement of components) e.g. - LHCb Velo detectors - ATLAS IBL
3000 fb-1
10 years
500 fb-1
 5
HL-LHC compared to LHC:
Higher radiation levels  Higher radiation tolerance needed!
Higher multiplicity  Higher granularity needed!
Power Consumption ? Cooling ? Connectivity Low mass ? Costs ?
 Need for new detectors & detector technologies

0
1
0
2
0
3
0
4
0
5
0
6
0
r
[
c
m
]
1
0
1
3
5
1
0
1
4
5
1
0
1
5
5
1
0
1
6
F
e
q
[
c
m
-
2
]
t
o
t
a
l
f
l
u
e
n
c
e
F
e
q
t
o
t
a
l
f
l
u
e
n
c
e
F
e
q
n
e
u
t
r
o
n
s
F
e
q
p
i
o
n
s
F
e
q
o
t
h
e
r
c
h
a
r
g
e
d
HL
-
L
H
C
(
5
y
e
a
r
s
,
2
5
0
0
f
b
-
1
)
h
a
d
r
o
n
s
F
e
q
A
T
L
A
S
S
C
T
-
b
a
r
r
e
l
A
T
L
A
S
P
i
x
e
l
P
i
x
e
l
M
i
n
i
s
t
r
i
p
M
a
c
r
o
p
i
x
e
l
(
m
i
c
r
o
s
t
r
i
p
d
e
t
e
c
t
o
r
s
)
[
M
.
M
o
l
l
,
s
i
m
p
l
i
f
i
e
d
,
s
c
a
l
e
d
f
r
o
m
A
T
L
A
S
T
D
R
]
Notes: 7

## Slide 8: Signal degradation for LHC Silicon Sensors
Note: Measured partly under different conditions! Lines to guide the eye (no modeling)!
Strip sensors: max. cumulated fluence for LHC
Pixel sensors: max. cumulated fluence for LHC

## Slide 9: Signal degradation for LHC Silicon Sensors
Note: Measured partly under different conditions! Lines to guide the eye (no modeling)!
Strip sensors: max. cumulated fluence for LHC and SLHC
Pixel sensors: max. cumulated fluence for LHC and SLHC
SLHC will need more radiation tolerant tracking detector concepts!

## Slide 10: PART 2 Radiation damage and its impact

## Slide 11: Silicon Growth Processes
Chemical-Vapor Deposition (CVD) of Si
up to 150 mm thick layers produced
growth rate about 1mm/min
Single crystal silicon
Poly silicon
RF Heating coil
Float Zone Growth
Czochralski Silicon (CZ)
Czochralski Growth
Basically all silicon tracking detectors made out of FZ silicon [Oi ]< 5  1016 cm-3
Some pixel sensors: Diffusion Oxygenated FZ (DOFZ)silicon [Oi ]~ 1-2  1017 cm-3
Epitaxial Silicon (EPI)
The growth method used by the IC industry.
Difficult to produce very high resistivity
[Oi ] ~ 5  1017 cm-3
Float zone Silicon (FZ)

## Slide 12: Types of radiation damage
Two types of radiation damage in detector materials:
 Bulk (Crystal) damage due to Non Ionizing Energy Loss (NIEL)
- displacement damage, built up of crystal defects –
Surface damage due to Ionizing Energy Loss (IEL) - accumulation of charge in the oxide (SiO2), traps at Si/SiO2 interface –
Si
SiO2
Region affected by ionizing energy loss - surface damage
Region affected by non-ionizing energy loss - bulk damage

## Slide 13: Generation of bulk damage (I)
Imping particle hits the lattice atom and knocks it out of the lattice site.
energy of Ek>25 eV is required for formation of a Frenkel pair (point defects)
for Ek>5 keV than knocked off atom displaces further lattice atoms (cluster defects)
V
I
EK > 25 eV
Frekel pair – ( Vacancy-Interstitial pair)
EK > 5 keV
TRIM simulation of 50 keV ion
dense region of displacements - cluster
Vacancies and Interstitial migrate in the crystal and react with other V,I or impurities.

## Slide 14: Generation of bulk damage (II)
How much clusters/point defects are produced by impinging particle depends on particle type and energy.
reactor neutrons – more clusters , less point defects
24 GeV protons – both in similar share
10 MeV protons – more point defects less clusters
g with < 8 MeV – only point defects
10 MeV p
24 GeV p
1 MeV n

## Slide 15: Generation of bulk damage (III)
How do we then compare the fluences of different particles?
NIEL hypothesis – the damage effects in silicon depend only on the non-ionizing energy loss regardless of the particle type and energy.
It is wrong (not extremely) for some radiation damage effects, but correct for leakage current. Still serves as a reference point.
One can normalize different particle fluences to the equivalent fluence of 1 MeV neutrons – equivalent fluence.
0.62 (24 GeV protons)
1.85 (26 MeV protons)
1.14 (300 MeV pions)
0.92 (reactor neutrons >100 keV)

## Slide 16: Effects of bulk damage to detector operation
I. Increase of leakage current (increase of shot noise, thermal runaway)
II. Change of effective doping concentration (higher depletion voltage, under- depletion)
III Increase of charge carrier trapping (loss of charge)
IV. Increase of silicon resistivity
The resistivity of silicon bulk increases with fluence
-deep defects push Fermi level close to mid-gap and the material becomes highly resistive. The upper limit is set by intrinsic silicon.
Irradiated
silicon

## Slide 17: Effects of bulk damage to detector operation
charged defects  Neff , Vdep e.g. donors in upper and acceptors in lower half of band gap
generation  leakage current, Neff Levels close to mid-gap most effective
Trapping (e and h)  CCE shallow defects do not contribute at room temperature due to fast detrapping

## Slide 18: Signal in semiconductor detector (pad)
d
hole
electron
p+
n+
v(t)
r0
HV
What if the drift is not completed?
Ballistic deficit – short integration
Charge trapping
sensing electrode
all other electrodes
Weighting field
Qe=0.5 q
Qh=0.5 q
sensing electrode
r0

## Slide 19: Signal in semiconductor detector (strip)
sensing electrode
all other electrodes
Weighting field
q
holes
electrons
implant=18 mm
pitch=80 mm
p+-n detector
Qe=0.1 q
Qh=0.9 q

## Slide 20: Signal in semiconductor detectors (electric field)
We are really interested in the electric field:
Electrical charge density
Electrical field strength
effective space charge density
depletion voltage
Full charge collection only for VB>Vdep !
Positive space charge, Neff =[P] (ionized Phosphorus atoms)
SIMPLEST CASE OF ALL : 1D , Neff=const.

## Slide 21: Signal in semiconductor detectors (electric field)
Neff determines the electric field in the detector!
A MORE COMPLICATED CASE : 2D , Neff=const.
e.g. : 280 mm thick detector, 25 mm strip pitch, 10 mm strip width

## Slide 22: Signal in semiconductor detector - trapping
In irradiated detector there comes the trapping term. Each individual charge drifts until it is trapped – the probability that it will drift over certain distance decreases exponentially (for vd<<vth):
For point charge(s) – integral along the line of particle drift
Influence on material properties to minimize the effects of irradiation
material engineering
(PART II of the lecture)
Exploit the design of the detector to minimize the effects of trapping and increase of Neff device engineering
(PART III of the lecture)
Everything is much simpler in pad detector – suitable for material studies.

## Slide 23: Noise in semiconductor detectors
Inter-strip capacitance can change due to interface states/traps, but at typical frequencies of 1 GHz the impact is questionable.
a and b should be optimized for the readout, to render ENCp less important.
Remember we look for high Signal/noise ratio (most important quantity)

## Slide 24: PART 3 Radiation damage effects in silicon (material studies/engineering)

## Slide 25: Leakage current
Damage parameter  (slope in figure) Leakage current per unit volume and particle fluence
 is constant over several orders of fluence and independent of impurity concentration in Si  can be used for fluence measurement
80 min 60C
Change of Leakage Current (after hadron irradiation) -> increase of noise …. with particle fluence:
Leakage current decreasing in time (depending on temperature)
Strong temperature dependence
Consequence: Cool detectors during operation! Example: I(-10°C) ~1/16 I(20°C)
80 min 60C
…. with time (annealing):

## Slide 26: How do we measure Neff and Vdep?
Capacitance measurement
The capacitance measurement has been the workhorse of radiation damage studies for decades.
C-V becomes unreliable at high fluences:
Undepleted bulk becomes highly resistive
Charging and discharging the traps is frequency and temperature dependent
Vdep from looking at Cgeom
Effective doping concentration - Neff

## Slide 27: Transient current technique and space charge
red laser pulse
n-type silicon
Non-irradiated
sensor

## Slide 28
Evolution of Vdep with fluence …
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
d
x
Electric field at Vdep
RD48: Comparison of different materials with respect to oxygen/carbon concentration.
Idea! Oxygen/Carbon may influence defect formation and reduce Neff after irradiation.
The material used was produced by using a so called Float-zone silicon, which ensures the silicon with least impurities and defects.

## Slide 29
Evolution of Vdep with fluence …
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
d
x
Electric field at Vdep
-
-
-
-
-
-
-
Not only the effective acceptors are introduced by irradiation, but also the initial donors are removed.
Initial acceptors – boron - are removed also for p-type material.

## Slide 30
Evolution of Vdep with fluence …
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
d
x
Electric field at Vdep
-
-
-
-
-
-
-
-
-
-
-
-
-
-
Inversion of the detector type (Feq=1-5∙1013 cm-2)
Detector of n-type turns effectively into p-type detector. This has a major consequence on detector operation. Using detector with higher initial dopant concentration shifts the inversion point towards higher fluences.

## Slide 31: Evolution of Vdep with fluence
Feq=5∙1013 cm-2
Feq=5∙1013 cm-2
n bulk
p+
n+
Electron injection
n bulk
p+
n+
Hole injection
Remember – the shape of I gives you the shape of E
Vdep=70 V
Vdep=20 V

## Slide 32
Evolution of Vdep with fluence …
+
+
+
+
+
+
+
+
+
d
x
Electric field at Vdep
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
The increse of Vdep i.e. |Neff| is almost linear with fluence.
The donor removal is almost complete.
~0.0055 cm-1
~0.017 cm-1
oxygeneted
standard

## Slide 33
Evolution of Vdep with fluence …
d
x
Electric field at Vdep
-
-
-
-
-
-
-
-
-
-
-
-
Standard float-zone n-type silicon detector would be at the limit of the power supply (500 V for ATLAS SCT), however Vdep is not enough – low field require some over depletion to avoid ballistic deficit and reduce trapping.
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-

## Slide 34
Evolution of Vdep with fluence …
d
x
-
-
-
-
-
-
-
-
-
-
-
-
With further fluence the detector break down voltage or power supply limit becomes smaller than Vdep
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
Electric field at Vdep

## Slide 35
Evolution of Vdep with fluence …
d
x
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
Detector is not fully efficient and has to run partially depleted. Huge problem for n-type detectors.
d
x
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
Reduce the voltage = not fully depleted detector
Electric field at Vdep
Electric field at Vdep
non-depleted part

## Slide 36: What about the p-type material?
p-type FZ material:
No inversion (material stays always effectively p-type)
There is some initial acceptor removal, but is not so well studied
The rate with which the negative space charge is introduced is comparable to n-type detectors
As will be explained later p-type material is more suitable (cheaper) for building detector for very harsh radiation environments.

## Slide 37: Neutron irradiations
The neutron irradiations show:
incomplete donor removal – not all initial donors are removed
no influence of any impurity – after neutron irradiations all materials behave the same – similar to the standard material irradiated with protons.
Cluster with several hundred V has a volume of
concentration of [O]=1017-1018 cm-3
Approximately few O atoms per cluster = the density of O is simply to small to have an effect!
neutrons
24 GeV protons

## Slide 38: Add more oxygen…
If the oxygen has such a positive role why not taking the material with most oxygen – Czochralski (only recently available with high enough resistivity)
The material seem not to invert – that means it stays effectively n-type after irradiation with charged hadrons – radiation introduces effective donors
But the rate of increase is about the same as for diffusion oxygenated float zone detector.
Coincidence ?
[O]~1018 cm-3

## Slide 39: Double junction – polarization effects
This effect is present in all detector types
It gets more pronounced at high fluences
It is more pronounced for charged hadron irradiated detectors and oxygen rich material – point defects dominant?
It gets more pronounced at low temperatures
electron injection
MCz-n = not inverted
je+jh
je
jh
p+
p+
Neff>0
Neff<0
Fp=5∙1014 cm-2
electron injection
Fz-n = inverted
Fp=5∙1014 cm-2
Induced current has a non-monotonic shape – sign of different space charge
n+
n+

## Slide 40: Evolution with time - Hamburg model
d
x
Electric field at Vdep
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
Short term : reduction of negative space charge
Long term: introduction of negative space charge

## Slide 41: Evolution with time - Hamburg model
d
x
Electric field at Vdep
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
-
-
-
-
-
Short term : reduction of negative space charge
Long term: introduction of negative space charge

## Slide 42: Evolution with time - Hamburg model
d
x
Electric field at Vdep
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
-
Short term : reduction of negative space charge
Long term: introduction of negative space charge

## Slide 43: Annealing behavior of MCz-n, FZ-n detectors
end of HL-LHC at RT
1.)
2.)
3.)
4.)
5.)
Finger print of positive space charge seen in annealing
decay of acceptors -> increase of Vfd
local maximum of Vfd (plateau)
generation of acceptors -> decrease of Vfd
inversion of space charge at late stages, but Vfd never really goes to ~0 (double junction)
further generation of acceptors increase of Vfd
DOFZ-n – Neff<0, MCz-n Neff>0

## Slide 44: Trapping of drifting charge
Q=constant for V>Vdep
in the way that
correction
higher voltages(i.e. higher field)
shorter drift
less charge trapped
increase of charge(V>Vdep)
G. Kramberger et al, Nucl. Inst. Meth. A476 (2002) 645.

## Slide 45
teff = ttr that gives equal current integral above VFD (compensate the trapping)
ttr > teff - lower voltages are under weighted
ttr < teff - lower voltages are over-weighted

## Slide 46: Trapping of drifting charge
The be,h was so far found independent on material;
resistivity
[O], [C]
type (p,n)
wafer production (FZ, Cz, epitaxial)
somewhat lower trapping at Feq>1015 cm-2
be,h ~ 0 for 60Co irradiated samples
b(-10oC, t=min Vfd) [10-16 cm2/ns] | 24 GeV protons 200 MeV/c pions (average ) | reactor neutrons
Electrons | 5.3 ± 0.7 | 3.5 ± 0.6
Holes | 6.6 ± 0.8 | 4.7 ± 1
The trapping probability:
gets smaller with time for electrons
gets larger with time for holes

## Slide 47: PART 4 Radiation effects in segmented detectors Can we design a detector where the effects of the irradiation are mitigated?

## Slide 48: Drift equation for the mip signal
trapping term ( teff,e~teff,h )
drift velocity ( me~3mh )
electrons get less trapped
they should drift to the strips/pixels and
contribute most to Q (n+ readout for silicon)
drift current of a single carrier
geometry factor
peaked at electrodes
Thickness ~ 300 microns
+V
+V
-V
electric field region
n
n
p
Remember: in segmented detector one carrier type always contributes more than the other – Uw determines the difference.

## Slide 49: Influence of geometry on charge collection
pitch 80- width 20
280 mm thick @ 100V, Neff=1e12 cm-3
te=12.5 ns
th=10 ns
19% signal from holes
81% signal from electrons
81% signal from holes
19% signal from electrons
Notes: Electric field region

## Slide 50: Device engineering – n+ readout
n+
better 
p+
worse 
Segmented readout
diode
Segmented readout
good 
  How to get maximum signal?
  use of n+-n or n+-p device (electron collection) with pitch<<thickness
  implant width close to pitch (depends on FE elec. – inter-electrode capacitance)
  for a given cell size of a pixel detector
even worse: p+ readout
(p+-n detector)
even better: n+ readout
(n+-p, n+-n detector)

## Slide 51: The difference between n+ or p+ readout is obvious!

## Slide 52: Device engineering – thin detectors
If bias is too small to deplete thin detector: benefit due to weighting field!
If bias is larger the if it better to have larger field and less trapping than larger deposited charge.
p+
n+
n+
p+
V>Vdep,thin
Uw,thin
Uw,thick

## Slide 53: Device engineering – thin detectors
Examples of the thin vs. thick detector operation!
NOTE: before irradiation and up to certain (large) fluence thick detector outperforms thin!
250x150 mm2 pixel detector
MPI data
pad detectors
150 mm device

## Slide 54: 3D n+-p pixel detectors
Combine traditional VLSI processing and
MEMS (Micro Electro Mechanical Systems) technology.
Both electrode types are processed inside the
detector bulk instead of being implanted on the wafer's surface.
The edge is an electrode. Dead volume at the Edge < 5 microns! Essential for forward physics experiments and material budget
S.I. Parker, C.J. Kenny, J. Segal, Nucl. Instr. and Meth. A395 (1997) 328.

## Slide 55: 3D n+-p pixel detectors
Pros.
Better charge collection efficiency
Faster charge collection (depends on inter-column spacing)
Reduced full depletion voltage and by that the power
Larger freedom for choosing electrode configuration
Cons.
Columns are dead area (aspect ratio ~30:1)
Spatially non-homogenous CCE (efficiency=function of position)
Much higher electrode capacitance (hence noise), particularly if small spacing is desired – small drift length
Availability on large scale
Time-scale and cost

## Slide 56
CNM 3D sensor
[G. Pellegrini, et al., NIMA 592 (2008) 38].
3D sensors:
used in IBL, excellent up to Φeq = 5·1015 n/cm2, promising results also for HL-LHC,
operation at lower voltage in innermost HL‐LHC tracking layer(s)
 More in other presentations at this conference!
[S. Grinstein, NIMA 699 (2013) 61–66 ]
[S. Tsiskaradze, 19th RD50 workshop]
Test beam, CNM, sensors,
Φeq = 5·1015 n/cm2, Bias voltage = 160 V
Track efficiency > 98%
0°
15°
Track incidence angle
Work of ATLAS 3D Sensor R&D Collaboration:

## Slide 57
Trapping induced charge sharing
If drift of the carriers is not completed – the charge is induced in the neighbors:
E field is not present in entire detector
Large trapping
1st 2nd
measuring
±U
Electric field present whole volume and no trapping – the charges complete the drift. The bipolar induced current gives no net induced charge.
80 um pitch
20 um im. width
I(t)
t

## Slide 58
Trapping induced charge sharing
If drift of the carriers is not completed – the charge is induced in the neighbors:
E field is not present in entire detector
Large trapping
1st 2nd
measuring
±U
Electric field not present in the whole volume? Charges induced in the neighbors (e.g. 13% on the first, 7% on the second ones).
80 um pitch
20 um im. width
low or no E field
Large number of strips with relatively small signal – wide clusters – this is where the charge was induced if Ew∙E is small for the hit strip.

## Slide 59
Trapping induced charge sharing
If drift of the carriers is not completed – the charge is induced in the neighbors:
E field is not present in entire detector
Large trapping
1st 2nd
measuring
±U
Electric field present in the whole volume, but large trapping. The bipolar induced charge doesn’t give zero net charge.
80 um pitch
20 um im. width
There is a big difference between n+-p and p+-n !

## Slide 60
electrode
hit in the center by ionizing particle
p+ elect.
diode
n+ elect.
same polarity
opposite polarity
wider clusters
larger signals
Signals in the neighbors few % of the hit strip
Depends strongly on fluence position of the hit and electrode geometry!

## Slide 61: Trapping induced charge sharing – infra red TCT
Laser scan over the detector surface (8mm FWHM beam width – 1064 nm) :
induced charge in the central strip vs. laser position.
300 mm, 80 mm pitch, 20 mm width
1015 cm-2
different sign

## Slide 62: PART 5 Operation at very high fluences recent highlights and challenges

## Slide 63: What about operation above 1015 cm-2?
CCE measurements show excellent results – much better than predicted?
Problems to understand why:
  Vdep – CV doesn’t work
  Time resolved TCT does not work, trapping to severe
G. Casse (4th RD50 workshop, 2004, CERN)
1st observation of unexpectedly high CCE
[A.Affolder, Liverpool, NIMA 623, 2010, 177–179]
Expected signal 2-3x too low!

## Slide 64
SIMULATION BASED ON MEASURED DAMAGE PARAMETERS FAILS COMPLETELY!
Even if trapping is off - the active region assumed by depletion is not enough to reproduce the signal!
Trapping and expected Neff
No trapping and expected Neff
βe = 3.2·10-16 cm2/ns
βh = 3.5·10-16 cm2/ns
No trapping, only Neff:
Black: measured, Red: simulation
Black: measured, Red: simulation
NOTE:
Very high voltage applied
CCE >=1

## Slide 65: Charge multiplication
T. Affolder et al., IEEE NSS-MIC, Orlando, 2009.
M. Köhler, 16th RD50 workshop, Barcelona, 2010
High F
large Neff
high V
High E
Impact ionization
3D p-type detector
planar p-type detectors
Electrons undergo multiplication in electric fields >10-15 V/mm
CCE > 1 observed for all types – larger in segmented detectors due to “field focusing”
CCE=1 for thin sensors

## Slide 66: Charge multiplication
Answers to be provided:
How to see it in the induced current?
How to measure the field?
285 μm thick n-in-p FZ pixels
Expected charge of ~2.5-3 ke
is largely surpased at 1016 cm-2
Both planar and 3D detectors are capable of surviving HL-LHC fluences in terms of signal!
threshold

## Slide 67: Edge-TCT
Classical TCT: information of the field from I(t)
  Edge-TCT: information of the field from I(depth)
A narrow 8 mm beam is used to generate e-h pairs at known depth
Measured current is average over the width of the strip
Edge-TCT meritev
G. Kramberger et al., IEEE TNS, VOL. 57, NO. 4, AUGUST 2010, 2294
t=0
d
y

## Slide 68: Edge-TCT
t~0, t<<teff,e,h
d
y
Classical TCT: information of the field from I(t)
  Edge-TCT: information of the field from I(depth)
A narrow 8 mm beam is used to generate e-h pairs at known depth
Measured current is average over the width of the strip
VELOCITY PROFILE:

## Slide 69: Edge-TCT
d
y
Classical TCT: information of the field from I(t)
  Edge-TCT: information of the field from I(depth)
A narrow 8 mm beam is used to generate e-h pairs at known depth
Measured current is average over the width of the strip
Electrons finish their drift.

## Slide 70: Edge-TCT
d
y
t<tint
Classical TCT: information of the field from I(t)
  Edge-TCT: information of the field from I(depth)
A narrow 8 mm beam is used to generate e-h pairs at known depth
Measured current is average over the width of the strip
End of drift

## Slide 71: Velocity profiles
2e15 cm-2
1e16
5e14
strips
back-plane
nirr.
whole detector volume is active (velocity in the saddle-30% of vsat)
the high field region penetrates deeper in the detector than predicted

## Slide 72: Velocity profiles
N. Pacifico et al., presented at RESMDD 10
FZ-p detector irradiated to
Feq=1.6∙1015 cm-2 300 MeV pions
Almost symmetrical electric field.
Elmost saturated drift velocity in the sensor at already 500V
MCz-n detector irradiated to
Feq=3∙1015 cm-2 neutrons
symmetrical electric field.
dominant p+ side at small/moderate voltages

## Slide 73: Charge multiplication
(1)
(2)
(3)
(4)
(5)
(6)
5∙1015 cm-2
1000 V
(2)
d
y
(4)
d
y
(3)
d
y
(5)
d
y
(6)
d
y
(1)
d
y

## Slide 74: Charge multiplication and annealing
Long term annealing seem not be a problem
  Electric field present in the whole detector
  Electric field is high at the strips
  Effective trapping times beneficially anneal
  Additional acceptors even increase multiplication at high voltages
y=150 mm
700 V
Micron; FZ n-p, neutrons 5e15 cm-2
160 min
320 min
640 min
1280 min
2560 min
5120 min
Edge-TCT signal
Multiplication peak
HPK FZ n-p, neutrons 5e15 cm-2
SCT128A – Sr90

## Slide 75: Multiplication current and noise
increase of current correlated with increase of signal – thermally generated carriers are multiplied
current increase results in the increase of noise according to
HPK FZ n-p, neutrons 5e15 cm-2
SCT128A – Sr90
Noise without multiplication for the generation current I
current multiplication
shot noise with multiplication
excess factor
Current larger than expected for full volume already at low voltages.
Gain in S/N expected for small electrodes where the series noise dominates!

## Slide 76: Conclusions – Radiation Damage
Radiation Damage in Silicon Detectors
  Change of Depletion Voltage (internal electric field modifications, “type inversion”, reverse annealing, loss of active volume, …) (can be influenced by defect engineering!)
  Increase of Leakage Current (same for all silicon materials)
  Increase of Charge Trapping (same for all silicon materials)
Signal to Noise ratio is quantity to watch (material + geometry + electronics)
Approaches to obtain radiation tolerant devices:
  Material Engineering: - explore and develop new silicon materials (oxygenated Si) - use of other semiconductors (Diamond)
  Device Engineering: - look for other sensor geometries - 3D, thin sensors, n-in-p, n-in-n, …
Excellent radiation hardness of silicon detectors at HL-LHC fluences
  active bulk - velocity in the saddle can be >30% of the saturated one
  active region - penetrates deeper in the bulk than extrapolated
  Charge multiplication - increase of Neff leads to impact ionization at high bias
              - the leakage current and noise also increase – improvement in S/N requires optimization of geometry
              - long term annealing seem not to be harmful
Notes: 76
76

## Slide 77: Acknowledgements & References
Most references to particular works given on the slides
Some additional material taken from the following presentations:
  RD50 presentations: http://www.cern.ch/rd50/
  Anthony Affolder: Presentations on the RD50 Workshop in June 2009 (ATLAS fluence levels)
  Frank Hartmann: Presentation at the VCI conference in February 2010 (Diamond results)
Books containing chapters about radiation damage in silicon sensors
  Helmuth Spieler, “Semiconductor Detector Systems”, Oxford University Press 2005
  Frank Hartmann, “Evolution of silicon sensor technology in particle physics”, Springer 2009
  L.Rossi, P.Fischer, T.Rohe, N.Wermes “Pixel Detectors”, Springer, 2006
  Gerhard Lutz, “Semiconductor radiation detectors”, Springer 1999
Research collaborations and web sites
  CERN RD50 collaboration (http://www.cern.ch/rd50 ) - Radiation Tolerant Silicon Sensors
  CERN RD39 collaboration – Cryogenic operation of Silicon Sensors
  CERN RD42 collaboration – Diamond detectors
  Inter-Experiment Working Group on Radiation Damage in Silicon Detectors (CERN)
  ATLAS IBL, ATLAS and CMS upgrade groups