## Slide 1
Nuclear Physics techniques
for Cultural Heritage
and environmental monitoring
P.A.Mandò
Università & INFN,
Firenze
Notes: 1

## Slide 2
The association of Nuclear Physics to matters such as
Cultural Heritage
or
environmental protection
sounds probably surprising, and the applications in these fields are not always so well known

## Slide 3: Main contributions of Nuclear Physics in the fields of Cultural Heritage and environmental protection
3
material composition measurements with Ion Beam Analysis (IBA)
and X Ray Fluorescence (XRF)
radiocarbon (14C) measurements, for archaeological dating and carbon component origin in atmospheric aerosols
Notes: 3

## Slide 4
Material composition analysis through the “bombardment” of a particle beam from an accelerator
  typically protons or alphas (energy of some MeV)
particle accelerator
particle beam
Emission of radiation of characteristic energies (X-rays, g, particles…)
Radiation detection and spectral analysis
Ion Beam Analysis (IBA)

## Slide 5
Ion Beam Analysis (IBA)

## Slide 6
PIXE: Particle Induced X-Ray Emission
ΔE
EX = ΔE
X-ray
X-ray energy is characteristic of the element

## Slide 7
a
elastically scattered particles (PESA)
X ray emission (PIXE)
secondary particles emission or inelastic scattering of incident ions
gamma ray emission (PIGE)
Ion Beam Analysis (IBA)

## Slide 8
Pros of IBA techniques
NON destructive, NON invasive, NO damage
widely multi-elemental
(simultaneous detection of almost all elements)
reliable quantitative analysis and great sensitivity
information also on layer structure if present, as is often the case e.g. in C.H. artefacts
micro-analysis ( high space resolution) is possible

## Slide 9
great importance for:
attribution and authentication
understanding technological skills in the past
learning about materials used in a given period and production area proving e.g. trade exchanges from other areas, if the detected materials are known to be locally unaivalable
detecting deterioration processes
deciding for appropriate restoration techniques and materials
Why material analysis for C.H.?

## Slide 10
Aerosols, i.e. the fine particles suspended in the atmosphere (the “famous” PM – Particulate Matter)
Determining its composition (not only its concentration) is crucial for
Why material analysis for environmental problems?
evaluating its direct impact on human health
identifying the pollution sources, each characterised by given compositions of the directly or indirectly produced PM
therefore, deciding the most effective actions to prevent pollution problems

## Slide 11: Radiocarbon (14C)
this is the result of an equilibrium between continuously “disappearing” by radioactive decay and being continuosly produced in the troposphere (15-18 km altitude) by cosmic rays
when formed, it oxidizes to 14CO2 and as such spreads throughout the atmosphere, down to the ground level
14C is a naturally occurring radioactive isotope of Carbon, wish is present in atmosphere in a very small concentration, ~10-12

## Slide 12: Radiocarbon (14C)
Through various metabolic mechanisms,
ALL LIVING ORGANISMS PARTICIPATE IN THIS EQUILIBRIUM
and have therefore in their tissues the same 14C concentration
UNTIL LIVING

## Slide 13: Radiocarbon (14C)
photosynthesis
food chain

## Slide 14: Radiocarbon (14C)
Starting from the death of the organism, the radioactive decay of 14C is no more compensated by any uptake; there are no mechanisms of in-situ production; thus, its concentration decreases continuously after death, at a well known rate given by the radioactive decay law

## Slide 15: Radiocarbon (14C)
time from death (years)
· 10-12
14R (14C/12C ratio)
14R(t) = 14R0 · e –t/t
with 14R0 = 1.18 10-12 and t = 8266 y
t = t · ln [14R0 / 14R(t)]

## Slide 16
Most important method for
dating all materials of organic origin
(date  time from the death
of the organism of origin)
Therefore:
absolute chronological reconstruction of archaeological sequences
authentications of works of art
compatibility of alleged relics with their attribution
Why measuring 14C for C.H.?

## Slide 17
The carbon component is a large fraction of aerosols
Schematically, it can have a “natural” or a “bad” man-induced component (e.g. combustion of fossil fuels)
The latter has zero 14C, the former has the 14C concentration characteristic of the living organisms
Therefore, the radiocarbon concentration in aerosols is an indirect measurement of the fraction of the “bad” anthropogenic component of carbon
Why measuring 14C in aerosols?

## Slide 18
Also nuclear are the techniques for measuring 14C residual concentrations
the now dominant technology is
Accelerator Mass Spectrometry (AMS)
Radiocarbon (14C)

## Slide 19
Indeed, ultra-low 14C concentrations (down to 10-15) must be measured with
small uncertainty
(e.g.: 0.5% error on concentration  40 years on age)
The challenge of AMS
Attaining a huge sensitivity
still keeping high precision
.. in addition, only requiring tiny quantities of material
(few milligrams, or even less, are sufficient)
Accelerator Mass Spectrometry can do that

## Slide 20: Measuring 14C with AMS
Negative ion source (eliminates interference of 14N)
Stripping at HV terminal (eliminates interference of 13CH, 12CH2)
Magnetic + electrostatic analysis + detection systems of high energy ions (remove residual interferences)
Tandem accelerator
Multi-sample source
Analysis and detection systems

## Slide 22
22

## Slide 23
Since the mid 1980’s its “research goals” were changed to applications using Ion Beam Analysis
In Florence....
long standing tradition with PIXE
(and IBA in general) applied to Cultural Heritage and environmental monitoring
This applied physics activity
started during the Eighties
with an old 3 MV Van de Graaff
single-ended accelerator
Until then, basic nuclear physics activities had been still
carried out with this accelerator
Notes: 23

## Slide 28
move of the Physics Department and INFN Unit to a new campus
INFN and University create a new lab
new 3 MV Tandetron, designed from the beginning to perform Accelerator Mass Spectrometry (AMS) for 14C measurements, besides IBA
the new laboratory, LABEC, is operational in May 2004
2001-2003
Notes: 28

## Slide 30
LABEC will be open to public on the occasion of

## Slide 32: Ion Beam Analysis techniques for Cultural Heritage
Notes: 32

## Slide 33: An essential feature to perform IBA for C.H.
1 cm
the external-beam setup

## Slide 34
At LABEC, two dedicated external beamlines
beam size defined by collimation (Ø 0.2 ÷ 1 mm)
strong focusing system, quadrupole doublet (Ø 8÷10 mm)

## Slide 35: Using external beam set-ups we have investigated with no damage whatsoever the quantitative composition of a large variety of artworks
Notes: 35

## Slide 36
Analysis of semiprecious stone artefacts,
“Disc with star”, and jewel case, from “Collezione Medicea di Pietre Ornamentali”, Natural History Museum, Florence

## Slide 37
External-beam PIXE analysis of the frontispiece of Pl.16,22 (XV century, Biblioteca Laurenziana in Florence)
...ancient illuminated manuscripts,
...historical documents,
Inks in Galileo’s manuscripts (Florence National Library) analysed by external PIXE
Notes: 37

## Slide 38
...drawings,
PIXE-PIGE analysis of a drawing on prepared paper, by Leonardo or his school
PIXE-PIGE analysis of a drawing on prepared paper, school of Verona, XVI cent.
Notes: 38

## Slide 39
…ancient embroideries,
Micro-PIXE and –PIGE analysis of gold threads of a Renaissance embroidery based on a cartoon by Raffaellino del Garbo
…early photographs
PIXE-PIGE analysis of a print on metal plate of the XIX century
Notes: 39

## Slide 40
...paintings on wood or canvas
Micro-PIXE and -PIGE analysis of the
“Ritratto Trivulzio” by Antonello da Messina
Differential PIXE and PIGE analysis of the
Madonna dei Fusi by Leonardo
Notes: 40

## Slide 41
Giorgio Vasari
Tavoletta with S.Lucia, from Pala Albergotti, Arezzo
Andrea Mantegna
Madonna col Bambino, oil on canvas, Accademia Carrara di Bergamo
Notes: 41

## Slide 42
...metal artefacts
PIXE and PESA analysis of some gilded chalices from the Museum of Casa Siviero, Florence
...glazed terracottas,
External PIXE analysis of the “Ritratto di fanciullo” by Luca Della Robbia – before restoration at the Opificio delle Pietre Dure in Florence

## Slide 43: The “Madonna dei Fusi” by Leonardo: composition and stratigraphy of the paint layers by differential PIXE and PIGE analysis
Collaboration with the
Opificio delle Pietre Dure (Florence)

## Slide 44
IBA
Measured spots during some beam-times at the old accelerator (3 MeV max. proton energy)
Leonardo da Vinci
“Madonna dei Fusi” (1501)
(ex-Reford version)
oil on wood, 50x36 cm2
(private collection)
interdisciplinary project, aimed at discovering the “secrets” of Leonardo’s painting techniques by non-destructive analysis, with different scientific techniques

## Slide 45: Differential PIXE
exploiting the different ranges at different particle energies, one can get information on which elements belong to the surface layers and which to the deeper ones
b
a
c
E2
E2 <
E3
E3 <
E1
E1
Measurements on the same spot with different beam energies
Information on layers structure (up to 100-200 mm from surface) obtained without picking up samples!

## Slide 46
pigments identification
information on the arrangement of layers
PIXE + PIGE
detectors
Si det.
Ge det.
Combining differential PIXE and PIGE allowed us:
beam
Nuclear Instruments & Methods B239 (2005), 71
X-Ray Spectrometry, vol.34,4 (2005), 306
Nuclear Instruments & Methods B219-220 (2004),48

## Slide 47
Ca
Fe
Pb
Original blue area
Ca
Fe
Pb
Zn
Fe
Pb
Co
Ca
Restored blue area
PIXE
PIGE
2.8 MeV
2.8 MeV
2.8 MeV
Na-g
Na-g
lapis-lazuli + lead white
cobalt blue + zinc white

## Slide 48: External scanning microbeam line
magnetic scan of areas within the window aperture
list-mode (E,x,y) DAQ
includes detection systems for PIXE, PIGE,
backward and forward particle scattering,
< 10 mm beam size on target
ion induced luminescence (IBIL)
beam
Nuclear Instruments & Methods A 576 (2007), 266
Nuclear Instruments & Methods B 190 (2002), 276

## Slide 49
2 mm
max
min
2 mm
Diagnostics of ink elements distribution in a XVII century document
damage precursor?

## Slide 50
Au Lα
Pb Lα
Sn K
Fe
Au Lα
Al
Si
Pb Lα
2 mm
2 mm
Mantegna, Madonna col Bambino (1460)
Accademia Carrara (Bergamo)

## Slide 51
AMS 14C dating at LABEC
Distribution of analysed materials

## Slide 52
Archaeological diggings in downtown Florence (Palazzo Vecchio and surroundings)
Etruscan site diggings in Southern Tuscany
River sediments – the Abak Creek layers in Ethiopia
Notes: 52

## Slide 53
Artemidorus papyrus
The Rosano Crucifix
The frame of a tryptic by Ambrogio Lorenzetti
Notes: 53

## Slide 54
AMS dating of St.Francis’ relics in Cortona and Florence
Nuclear Instruments & Methods B266 (2008), 2251
Notes: 54

## Slide 55
55
Results

## Slide 56
2
Notes: 56

## Slide 57: Exploiting the effect of nuclear explosions in atmosphere during the cold war
57
pMC (percent of Modern Carbon)
Reference curve for the Boreal Emisphere

## Slide 58
Many intersting applications in forensics and biology,
but these large variations of 14C concentration during the past 60 years might also be exploited to discover recent fakes of contemporary art, claimed instead to have been produced during e.g. the first half of the XX century

## Slide 59
May 14C be used
to date contemporary art?
Nuclear Instruments & Methods B 294 (2013), 662

## Slide 60
Yes...if the painting support is only compatible with a later period...
129.05 ± 0.68 pMC
90
100
110
120
130
140
150
160
170
180
190
200
1940
1945
1950
1955
1960
1965
1970
1975
1980
1985
1990
1995
2000
year AD
pMC
A canvas sample from a painting initially attributed to Fernand Legér
Legér died in 1955!

## Slide 61
Atmospheric Aerosol
Impact on climate changes
Impact on health
Impact on Cultural Heritage
solid and liquid particles with a diameter from 10-3 to 102 μm
(PM  Particulate Matter)
natural or anthropic sources
direct or secondary origin

## Slide 62
What is needed to study aerosols (PM)
A wealth of data concerning:
concentration and composition
size distribution
optical properties
time and space evolution
Identification and quantification of PM emission sources
Contribution to climatic models to evaluate the role of atmospheric aerosol in the “radiative forcing”
Contribution to strategies of pollution abatement to improve air quality

## Slide 63
Research projects of the LABEC group
Local impact:
Study of PM10, PM2.5 e PM1 in Tuscany (PATOS, PATOS 2) and in the most important Italian cities
Global impact:
EPICA - European Project for Ice Coring in Antarctica
TALDICE - TALos Dome Ice CorE
ANDRILL - Antarctic Geological Drilling
AMMA - African Monsoon Multidisciplinary Analysis
MAIL - Marine Aerosol in the Island of Lampedusa
DIRIGIBILE ITALIA (multidisciplinary study of climate change in the Arctic region)
Environmental monitoring in sites relevant for Cultural Heritage
Indoor pollution/ personal exposure:
HEARTS - Health Effects And Risks of Transport Systems

## Slide 64: Measurements of “daily” samples
Multiple sample-holder
Beam scan over the filter to average the whole collection area
47 mm
PM1 PM2.5 PM10
Sequential Samplers
Notes: Analizzare tanti campioni raccolti con campionatori standard per lunghe campagne di misura
Fondamentale per ottenere risultati rappresentativi e affidabili
(spesso studi poco seri sui giornali)
QUESTE SLIDES SUI SETUP TE LE MANDA PIù BELLINE MASSIMO

## Slide 65: Measurements of “hourly” samples
100 mm
PM2.5
PM2.510
Kapton foils
Nuclepore
Continuous sampler (“streaker”)
Beam size: 1 mm x 2 mm, corresponding to the impact area of one hour sampling
Notes: Oraio solo con PIXE,
fondamentale per sorgenti

## Slide 66: Hour-by-hour trend (V.le Gramsci, Firenze): Cu e Zn, tracers of traffic

## Slide 67: Industrial emissions
Bla bla
Industrial emissions at Montelupo Fiorentino:
artistic glass and ceramics production
Notes: Emissioni industriali notturne

## Slide 68: Impact of tourists on Cultural Heritage Cortile del Michelozzo (Palazzo Vecchio)
Bla bla
closed to visitors
Notes: Risollevamento (elementi del suolo) durante le ore del giorno dovuto a visitatori
(non c’è infatti per il primo dell’anno)
Ti può fare comodo come collegamento ai BBCC

## Slide 69
July 9-10, 2006: fireworks to celebrate Italian soccer team victory at the World Championship

## Slide 70: PATOS Project
urban backgr.
urban traffic
urban backgr.
urban backgr.
urban backgr.
PM10 average composition
regional backgr.
Notes: Caratterizzazione media chimica
Soil dust e marino con pixe
E traccianti importanti di sorgenti ... Slide dopo

## Slide 71
Identification of pollution sources through multivariate statistical models
Daily samples, Capannori (Lucca), 2005-2006
Notes: Identificazione sorgenti tramite modelli statistici
Esempio riportato:
Sito più inquinato
E quale è la sorgente più importante quando si hanno superamenti? combustione della legna!!!!
Come siamo sicuri?
Slide dopo

## Slide 72: Saharan dust
important contribution in the Mediterranean area
one should distinguish its contribution from
the one of pollution sources (also for legal regulations)
Notes: Tema importante su cui pixe è unica perchè vede bene tutti i crostali
Ad es. In questo episodio il pm10 ha superato il limite dei 50 ug/m3 in tutta la regione e il contribuuto del sahara è stato più del 50% e quindi determinante (sconto comunità europea)

## Slide 75: Contribution to exceeding the limits of PM10
Indeed, Saharan dust was sometimes the reason for exceeding the limit in June. However, other events of limit exceeding are due to other sources
PM10 concentration (mg/m3)
Saharan dust
other components
Notes: Puoi saltare

## Slide 76: Not only accelerator-based techniques
XRF (X Ray Fluorescence) exploits the same principle of PIXE, i.e. the emission of characteristic X rays, to get information on elemental composition
In XRF it is however a beam of primary e.m. radiation, rather than of particles, to produce inner shell ionisation (by photoelectric effect)

## Slide 77
The transportable XRF spectrometer of LABEC
● 2 X ray tubes (30 kV max, 1 mA max) with two different anodes (typically Mo e Ti; W if needed)
● SDD detector
● helium flow in front of both tubes and detector
● 2 laser beams for accurate positioning
● interchangeable collimators; typical beam diameter 0.5 mm
Measurement head
Controller
● data acquisition, He flow, X-Y-Z displacement and video camera remotely controlled (via Ethernet)
X Ray Spectrometry, Vol.40 (2011), p.107

## Slide 78
Affresco della Resurrezione
Piero della Francesca
Sansepolcro,
Museo Civico
Notes: 78

## Slide 79
79

## Slide 80
Crucifix by Maestro di Figline
Santa Croce
Notes: 80

## Slide 81
Santa Croce, Bardi and Peruzzi Chapels cycle of frescoes by Giotto
Notes: 81

## Slide 82
Madonna del Granduca
Raffaello
Galleria Palatina
Notes: 82

## Slide 83
83
The Chimera of Arezzo
Museo Archeologico Firenze

## Slide 84
Beato Angelico, Crocifissione Capitolare, San Marco, Firenze

## Slide 85
Thank you for your attention!
Notes: 85