## Slide 1
Rivelatori Termici basati su Grafene
SIGLA: GTD
(Graphene-based Thermal Detector)
Paolo Falferi
INFN – TIFPA (Trento Institute for Fundamental Physics and Applications)

## Slide 2
Suspended graphene shows "rippling" of the flat sheet, with amplitude of about one nanometer
These ripples may be intrinsic (instability of two-dimensional crystals) or may be extrinsic (from the dirt, substrate… )
Graphene
one-atom thick layer of carbon atoms arranged in a regular hexagonal pattern to for a 2D crystal

## Slide 3
Production Methods
Exfoliated graphene
From graphite and adhesive tape to repeatedly split graphite crystals into increasingly thinner pieces. The tape with graphene is dissolved in acetone, and, then some monolayers can sediment on a silicon wafer (Geim and Novoselov, Manchester 2004). Best quality.
Epitaxial growth on silicon carbide
From silicon carbide (SiC) at high temperatures (>1,100 °C) under low pressures (~10−6 torr).
Dimensions dependent upon the size of the SiC substrate (wafer).
The face of the SiC used (Si or C) influences thickness, mobility and carrier density of the graphene.
Epitaxial graphene on SiC can be patterned using standard microelectronics methods.
Epitaxial growth on metal substrates
The atomic structure of a metal substrate to seed the growth of the graphene.
High-quality sheets of few-layer graphene (>1 cm2) via chemical vapor deposition (CVD) on thin nickel films with methane as a carbon source. These sheets can be transferred to various substrates.
Improvement with copper foil; at very low pressure, the growth of graphene automatically stops after a single graphene layer forms, and arbitrarily large graphene films can be created.
When methane is replaced by ethane or propane growth of bilayer graphene.
Other methods (Graphite oxide reduction, Growth from metal-carbon melts, Pyrolysis of sodium ethoxide…)

## Slide 4
General Properties of Graphene
Electron transport
High electron mobility at room temperature (200,000 cm2·V−1·s−1, achieved = predicted) limited by scattering by the acoustic phonons
Resistivity = 10−6 Ω·cm (less than the resistivity of silver)
Optical phonons of the substrate (ex. SiO2 ) limits the mobility to 40,000 cm2·V−1·s−1. Also dopant and ripples increase the resistivity
Optical
Electrons behave as massless two-dimensional particles => wavelength-independent absorption (=2.3%) for normal incident light below ~ 3 eV (very high opacity for an atomic monolayer)
Mechanical
Young modulus of 1TPa (steel 200GPa) and intrinsic strength of 130GPa (very close to theory) (carbon fiber 4GPa)
Thermal
Record high thermal conductivity and can sustain extremely high densities of electric current (million times higher than copper)

## Slide 5
Integrated circuits
Electrochromic devices
Transparent conducting electrodes
Ethanol distillation
Desalination
Solar cells
Single-molecule gas detection
Circuit interconnects
Quantum dots
Transistors
Frequency multiplier
Optical modulators
Additives in coolants
Reference Material
Thermal management materials
Ultracapacitors
Electrode for Li-ion batteries (microbatteries)
Engineered piezoelectricity
Biodevices
Potential Applications
Graphene appointed an EU Future Emerging Technology flagship
The European Commission has chosen Graphene as one of Europe’s first 10-year, 1,000 million euro FET flagships. The mission of Graphene is to take graphene and related layered materials from academic laboratories to society, revolutionize multiple industries and create economic growth and new jobs in Europe.

## Slide 6
Thermal Detectors
t = Ctot/G
Temperature Rise
Recovery Time
Signal
Absorber
Heat Bath
Thermometer
Radiation
Weak Thermal Link
The advantage of the thermal detector with respect to the conventional semiconductor ionization detectors is that , if you can wait, the absorption of a photon ends up in thermal excitations and the details of the down-conversion are less important

## Slide 7
Thermal Detectors
N = number of phonons
with mean energy kBT
N ≈ CtotT/kBT
dN = √N
dErms = dNkBT = √(kBT2C)
Noise
Thermometer
Resistive
Metallic
Paramagnet
Doped
Semiconductors
Superconducting
Transition-Edge
SQUID
Readout
Low Temperature
Small Heat Capacity
Better Performance
Thermodynamic Fluctuation Noise

## Slide 8
Graphene-based Thermal Detector
Graphene 2D electron gas at very low temperature is a nearly ideal thermal detector
very low heat capacity (electron specific heat C  T)
very fast thermalization
very low coupling (Gtot= Ge-ph+Gphoton≈ αT3+kBB)
weak coupling to some substrates (SiO2, SiC, hBN…) => these graphene layers retain the two dimensional electronic band structure of isolated graphene
Pbm: for pristine graphene weak temperature dependence of easy-to-measure properties
Sol: Noise Thermometry
Temperature measurement from the thermal (Johnson) noise of a resistor

## Slide 9
Precision of the Temperature Measurement
Mi
Mf
Rf
R
Room Temperature
Mixing Chamber Temperature
SQUID Electronics
VTh
Li
For hn/kBT<<1
R independent of w and T
w = 2pn, t = Lt/R, Lt = Li+Ls, Ls is any stray inductance in the SQUID input circuit
Current Noise
tM is the measuring time
TN = noise temperature of the thermometer
SQUID advantage
Low dissipation
Low thermometer noise temperature
SQUID Noise Thermometry
Graphene-based Thermal Detector

## Slide 10
Measuring Time tM=130s
DT/T≈0.4% is temperature independent
SQUID Noise Thermometry: an example
Graphene-based Thermal Detector
P. Falferi and R. Mezzena,
IEEE Trans. Appl. Supercond., 21 (2011) 48

## Slide 11
Vout
A
Li
R
Li
R
C
Ls
Li
L
R
C
ELECTRICAL RESONATOR + SQUID
From low-pass to band-pass
SQUID Noise Thermometry
Graphene-based Thermal Detector

## Slide 12
Mi
Mf
Rf
Rgraph
Room Temperature
Dilution Refrigerator
Temperature
SQUID Electronics
VTh
Li
SQUID
Impedance
Matching
Transformer
1st measurement scheme: SQUID amp, low-pass
Graphene-based Thermal Detector

## Slide 13
Rgraph
HEMT
LC matching network
AMP
100 mK
Tamb
4 K
Graphene-based Thermal Detector
2nd measurement scheme: HEMT amp, band-pass

## Slide 14
Rgraph
HEMT
LC matching network
AMP
100 mK
Tamb
4 K
Graphene-based Thermal Detector
3rd measurement scheme: MSA + HEMT amp, band-pass
Microstrip
SQUID
Amplifier

## Slide 15
L1
C1
Rgraph
L2
C2
Rgraph
Graphene-based Thermal Detector
HEMT
Possible frequency multiplexing scheme
LC Matching Network

## Slide 16
Expected Performance (Graphene 3x3 mm2)
Single Photon
Energy Resolution
NEP vs Measurement Bandwidth
and operating temperature
DE/E = 1% for 1THz Photon !
Fong & Schwab, Caltech, PRX 2 031006 (2012)
McKitterick, Prober, & Karasik, JPL & Yale, JAP 113, 044512 (2013):
“We identify the optimum conditions and find that single-photon detection at terahertz frequencies should be feasible”
Graphene-based Thermal Detector

## Slide 17
Applications interesting for INFN
Scintillating bolometers for Dark Matter and Double Beta Decay experiments (CRESST, ROSEBUD, LUCIFER, AMoRE, the future project EURECA, and the R&D research on ZnMoO4)
In non-scintillating materials relevant for DBD, the particle identification can be achieved through the detection of the much weaker Cherenkov light
Spurious events with the same amount of deposited heat can be identified thanks to the different light yield => background control
Cosmic Microwave Background (if the 60-600 GHz range will be achieved)
Not only Astrophysics and Cosmology but also Fundamental Physics from CMB
Near infrared fluorescence to detect Ultra High Energy Cosmic Rays (NIRFE)

## Slide 18
Sinergie
E’ partito (sta partendo) il TIFPA la cui attività sarà supportata da 4 partner (INFN, Università Tn, FBK, Protonterapia): è opportuno avviare un maggior coinvolgimento di FBK in attività INFN (quindi non solo come produttore di dispositivi ma come attore nell’attività di ricerca)
E’ partito il grande progetto europeo Graphene Flagship 3+7 anni in cui FBK è presente. Appuntamento importante fra 3 anni per riassegnazione obiettivi
È prevedibile un forte sviluppo della tecnologia del graphene nei prossimi 10 anni

## Slide 19
Attività:
Grafene da FBK o da partner della Graphene Flagship o acquistando da produttori (Pbm: purezza, dimensione cristalli, substrato, …)
Caratterizzazione grafene in FBK (XPS, Raman…)
Microfabbricazione su grafene in FBK (pbm: contatti, pulizia…)
Verifica proprietà grafene a T ultracriogeniche (es. Ge-ph vs T)
Misure ultracriogeniche di rumore termico da resistenza in grafene (lettura SQUID)
Misure ultracriogeniche di rumore termico in risonanza con HEMT e poi con MSA (Microstrip SQUID Amplifier)
Studio di possibili implementazioni di frequency multiplexing
Studio di strategie tecnologiche per aumentare la quantum efficiency (es. più strati o uso cavità ottica (linea di ricerca dell’ IFN-CNR di Trento))
Possibili applicazioni su detector tipo DBD (E. Previtali)

## Slide 20
Apparati strumentali utilizzati Refrigeratore a diluizione, liquefattore di elio, Camera pulita (microfabbricazione), X-ray and ultraviolet photoelectron spectroscopy, Raman spectroscopy, strumentazione microonde e SQUID
Istituzioni esterne partecipanti Istituto di Fotonica e Nanotecnologie CNR - FBK di Trento
Dipartimento di Ingegneria Civile, Ambientale e Meccanica e
Dipartimento di Fisica dell’Università di Trento
Centro Materiali e Microsistemi - FBK di Trento
Durata esperimento 3 anni
Sezioni partecipanti Trento (TIFPA) (dal terzo anno eventualmente Padova e/o Milano Bicocca)

## Slide 21
Ricercatori (attività) FTE Istituto
Paolo Falferi (coordinamento, SQUID) 0.5 FBK
Renato Mezzena (ultracriogenia, microonde) 0.5 UniTn
Giorgio Speranza (prod. e carat. grafene) 0.5 FBK
Ricercatore a contratto FBK (SQUID, microonde) 1 FBK
Claudia Giordano (microfabbricazione) 0.5 FBK
Benno Margesin (microfabbricazione) 0.2 FBK
Nicola Pugno (carat. grafene) 0.3 UniTn
Tot 3.5

## Slide 22
 | 2014 | 2015 | 2016 | tot | 
Interno | 1.0 | 1.0 | 2.00 | 4.0 | Visite presso lab della Graphene Flagship, il terzo anno per eventuale test su rivelatore (LNL o Milano)
Estero |  | 4.00 |  | 4.0 | LTD-16 workshop (in Europa)
Consumo | 10.0 micro 3.0 elio 5.0 graphene 3.0 Two- stage SQUID 3.0 cryospares 2.0 materiale/componenti per officine m/e | 25.0 micro 3.0 elio 5.0 graphene 4.0 MSA 5.0 Mw Pass Comp | 25.0 micro 3.0 elio 5.0 graphene | 101.0 | Microfabbricazione (maschere, reattivi, substrati, cariche evaporazione, photoresist), elio liquido, graphene, SQUID e MSA (microwave SQUID amp), Microwave passive components (circulators, directional couplers, attenuators, filters, coaxial cables…), cryospares,
Manutenzione | 2.0 | 2.0 | 2.0 | 6.0 | Refrigeratore cryogen free, pompe, xps (anodo X), raman, elettronica
Inventario | 15.0 |  |  | 15.0 | Scheda acquisizione veloce, HEMT amp
tot | 44.0 | 49.0 | 37.0 | 130.0 | 

## Slide 23
Fine