## Slide 1: OUTLINE
Attivita’ periodo 15 settembre 2012 – 15 giugno 2013
  Test beam, novembre 2012
  Produzione THGEM
    Uniformita’
    Confronto THGEM grandi e piccole
  Verso il test del rivelatore ibrido
    Anodo resistivo
    Strato di micromesh
  Costruzione del Leopard
  Coordinemanto del progetto
  Documentazione

## Slide 2
Attivita’ periodo 15 settembre 2012 – 15 giugno 2013
  Test beam, novembre 2012

## Slide 3: TEST BEAM
CERN PS, T10

## Slide 4
RESULTS, only a flavour
  Effect of the reverse
  bias on MIP detection
  Response of the large-size prototype
TEST BEAM

## Slide 5: OUTLINE
Attivita’ periodo 15 settembre 2012 – 15 giugno 2013
  Produzione THGEM
    Uniformita’
    Confronto THGEM grandi e piccole

## Slide 6: THGEM PRODUCTION – thickness uniformity
September 2012, status
GAIN
Max/Min
= 2.9

## Slide 7
THGEM PRODUCTION – thickness uniformity
Selection of the fiberglass plates (with Cu)
January 2013, status
50 cm
(mm)
50 cm

## Slide 8
THGEM PRODUCTION – thickness uniformity
Different material:
  Permaglas, machinable (~ Stesalite)
BUT: ELTOS could not glue the Cu layers with standard pre-preg
Glued at CERN, now back to Eltos
May 2013, status
Thickness: 0.8 mm
Thickness: 1 mm
5.3 %
2.1 %
5.2 %
5.3 %
3.8 %
2.6 %
2.5 %
2.5 %

## Slide 9
THGEM PRODUCTION – thickness uniformity
THGEMs from selected boards:
April 2013, status
GAIN
Max/Min
= 1.6

## Slide 10: THGEM GAIN: LARGE vs SMALL
The 300 x 300 mm2 chamber exhibits the same
response of the small ones (300 x 300 mm2),
but it cannot reach the same maximum gain
January 2013, status
Max GAIN
small / large = 10
(best small assumed)
300 x 300

## Slide 11
THGEM GAIN: LARGE vs SMALL
Design and production of non-standard THGEMs
dedicated to these studies
Large and small in the same PCB
The role of the segmentation
April 2013, status

## Slide 12
THGEM GAIN: LARGE vs SMALL
Silvia DALLA TORRE
CERN, COMPASS TB meeting, 8/5/2013
Chart: Pashchen Curve
| 2.8585099999999999E-2 | 5.9146600000000001E-2 | 0.117537 | 0.18329799999999999 | 0.28585100000000002 | 0.59146600000000005 | 1.17537 | 1.8329800000000001 | 3.0990500000000001 | 6.15848 | 11.7537 | 17.604099999999999 | 29.763500000000001 | 59.146599999999999 | 122.38200000000001 | 176.041 | 309.90499999999997
 | 4052.61 | 674.108 | 410.449 | 366.046 | 380.286 | 426.417 | 624.569 | 727.576 | 987.359 | 1446.18 | 2467.55 | 3102.51 | 5095.45 | 8055.22 | 15411.5 | 20914.2 | 37073.3
April 2013, status
Understand the role of the Paschen curve
The breakdown Vbd depends on
P
d (electrode distance)
the specific gas
d = 0.4 mm  Vbd = 2270 V
Dd = 20 mm  DVbd= 100 V
DP = 20 mbar  DVbd= 35 V

## Slide 13
THGEM GAIN: LARGE vs SMALL
THGEM production, after drilling
  ELTOS (industrial poroducer) : microetching, brushing
  CERN workshop, brushing
These defects (due to brushing?) are (almost) non present in the small THGEMs
Irregularities are gone, but still the Max Vbd is far from Paschen’s curve … related to surface irregularities ?

## Slide 14
THGEM GAIN: LARGE vs SMALL
THGEM production, after drilling
  NEW: in Trieste
    1. polishing (Hinrichs Pumice Powder)
    2. cleaning with high pressure water to remove all pumice residuals
    3. ultrasonic bath (~1 h) @ 50-60 oC in Sonica PCB solution (pH11)
    4. washing with demineralized water plus oven at 180 oC
    for 24 h
  All w/o adequate equipments and tools !
April 2013, status

## Slide 15
THGEM GAIN: LARGE vs SMALL
April 2013, status
initial
final
summarising

## Slide 16
THGEM GAIN: LARGE vs SMALL
Does the new procedure pay ?
this and the following tests in AIR
April 2013, status
63 % | 99 %
300 X 300 Single Sector #1 (before treatment) | 300 X 300 Single Sector #1 (After treatment)
1390 V | 2180 V
Paschen limit =
2190.76V
% of the Paschen limit

## Slide 17
THGEM GAIN: LARGE vs SMALL
Does the new procedure pay ?
out of the box | 1410 | 1220 | 1610 | 1430 | 1410 | 1450
After first treatment | 2140 | 1980 | 1940 | 2120 | 2110 | 2100
After second treatment 24/4 | 2200 | 2190 | 2140 | 2120 | 2220 | 2180
Chart: Isola #8
Sector 1 | 1410 | 2140 | 2200
Sector 2 | 1220 | 1980 | 2190
Sector 3 | 1610 | 1940 | 2140
Sector 4 | 1430 | 2120 | 2120
Sector 5 | 1410 | 2110 | 2220
Sector 6 | 1450 | 2100 | 2180
April 2013, status

## Slide 18
THGEM GAIN: LARGE vs SMALL
Does the new procedure pay ?
 | A | B | C
1 |  | 1690 (1540) | 
2 |  | 1810 (1610) | 
3 |  | 1660 (1570) | 
4 | 1470 (1410) | 1470 (1410) | 1470 (1410)
5 | 1510 (1490) | 1510 (1500) | 1510 (1500)
6 | 1590 (1580) | 1590 (1550) | 1590 (1500)
 | A | B | C
1 |  |  | 
2 |  | 1137 | 
3 |  |  | 
4 |  |  | 
5 | 312 | 335 | 350
6 | 581 | 474 | 
TABLE I:
Maximum ∆V scan with & without source
Without source
(With Source)
TABLE II:
Gain measurement @ highest
∆V of the sectors
Now in
Ar/CO2 : 70-30%
Gains in the same range !
April 2013, status

## Slide 19: OUTLINE
Attivita’ periodo 15 settembre 2012 – 15 giugno 2013
  Verso il test del rivelatore ibrido
    Anodo resistivo
    Strato di micromesh

## Slide 20: THE HYBRID DETECTOR – MICROMESH
A first resistive anode produced
  Obtained modifying an existing anode
  Using lithographic masks already available
    Useful surface: 100 x 100 mm2
April 2013, status

## Slide 21: THE HYBRID DETECTOR – MICROMESH
A first resistive anode produced
April 2013, status

## Slide 22: THE HYBRID DETECTOR – RESISTIVE ANODE
Micromesh “production”
  A learing session at Seritech services SA (Montrex)
April 2013, status
Micromesh:
G Bopp & Co AG
  18mm f , hole: 45 mm
SEFAR
Tensocheck 100-R
GLUES
Thick: SAATIchem Ultrafix SB2
Thin: SEFAR NYTAL Cyanacrylat Kleber

## Slide 23: THE HYBRID DETECTOR – RESISTIVE ANODE
Silvia DALLA TORRE
CERN, COMPASS TB meeting, 8/5/2013
Micromesh “production”
  A learing session at Seritech services SA (Montrex)
April 2013, status
Tensioning the mesh
(15N/cm ± 1N/cm)
Glueing onto the TRANSPORT frame
Glueing onto the FINAL frame (with reinforcement)

## Slide 24: OUTLINE
Attivita’ periodo 15 settembre 2012 – 15 giugno 2013
  Costruzione del Leopard

## Slide 25: LEOPARD CONSTRUCTION
A few images to remind about the LEOPARD
G.Hamar and D. Varga, NIMA 694(2012)16
Gain map
Efficiency
map

## Slide 26: LEOPARD CONSTRUCTION
The CAD design
January 2013, status

## Slide 27: LEOPARD CONSTRUCTION
Leopard mechanics and stepping motors computer control ready
April 2013, status
fine x & y movement
large x & y movement

## Slide 28: OUTLINE
Attivita’ periodo 15 settembre 2012 – 15 giugno 2013
  Coordinemanto del progetto

## Slide 29: 1st PROJECT MEETING
Trieste, 21/1/2013
Attendance (25 in total):
Aveiro: C.Santos, C.Azevedo, J.Veloso
Freiburg: M.Büchle, H.Fischer, F.Herrmann, S.Schopferer
Liberc: K.Novakova, L.Steiger, M.Sulc
Matrivani: S. Dasgupta
Prague: M.Finger,M.Finger, J.Novy
Trieste: M.Alekseev, F.Bradamante, R.Birsa, A.Bressan,
P.Ciliberti, S.Dalla Torre, S.Levorato, A.Martin,
G.Menon, G.Sbrizzai, F.Tessarotto

## Slide 30: Trieste, 21/1/2013 - AGENDA
Introduction (Silvia) Session: Test beam session Set-up and preparation (Carlos)
FE performance (Maxim)
Data analysis (Stefano)
Session: More information THGEM read-out (Max) THGEM read-out FE (Maxim) Cherenkov photons from quartz radiators (Miroslav) The hybrid detector (Stefano) The "leopard" (Fulvio)
CsI QE vs time in the present detectors (slides by Federica shown by Silvia)
Session: planning
Next 6 month planning in Trieste (Fulvio) General Discussion

## Slide 31: OUTLINE
Attivita’ periodo 15 settembre 2012 – 15 giugno 2013
  Documentazione

## Slide 32: THGEM: DOCUMENTAZIONE ATTIVITA’
CONFERENZE:
13th Vienna Conference on instrumentation Pisa Meeting on Advanced Detectors (VCI 2013), 11-15/2/2013, Vienna, Austria
THGEM-based Photon Detectors for the upgrade of COMPASS RICH-1
F. Tessarotto
5th IEEE International Workshop on Advances in Sensors and Interfaces (IWASI 2013), 13-14/6/2013, Bari, Italy
A Hybrid photon sensitive detector based on MPGD (relazione su invito)
S. Levorato
3rd International Conference on Micro-Pattern Gaseous Detectors (MPGD 2013), 1-4/7/2013, Zaragoza, Spain
MPGDs developments: Historical Roadmap and Recent Progresses in Consolidating
MPGDs (relazione su invito)
S. Dalla Torre
Status and progress of the novel photon detectors based on THGEM and hybrid
MPGD architectures
F. Tessarotto
ARTICOLI :
M. Alexeev et al., NIMA 695 (2012) 159.
M. Alexeev et al., JINST 8 (2013) P01021.
The development of Thick GEM-based photon detectors for COMPASS RICH-1 (submitted to NIMA)