## Slide 1
Anna Macchiolo
Max-Planck-Institut für Physik
Sviluppo di rivelatori a pixel per gli upgrades del tracciatore di ATLAS
Seminario di Gruppo I, INFN Firenze, 30 Ottobre 2013

## Slide 2
Content
The path for the ATLAS tracker upgrade
Phase II: what are the physics motivations
The performance of present ATLAS pixel detectors
IBL: new technologies for the first upgrade
Requirements of the ATLAS Pixel system in Phase II
Planar Pixel Sensor developments for Phase II
Vertical Integration Technologies and new 3D module concepts

## Slide 3
Silicon Pixels
Silicon Strips (SCT)
Transition Radiation Tracker (TRT) up to 36 points/track
2T Solenoid Magnet
Tile Calorimeter
Liquid Argon calorimeter
TRT
Pixel Detector
SCT
Solenoid Magnet
Muon Detector
Toroid Magnet
The tracking system of the ATLAS detector

## Slide 4
New insertable b-layer (IBL)
New Al beam pipe
New pixel services
Fast TracKing (FTK) for level2 trigger
All new tracker (baseline:
long strips /short strips / pixels)
ATLAS Tracker Upgrade Plan

## Slide 5
Why Phase II after the discovery of the Higgs boson?

## Slide 6
HL-LHC Physics Programm (I)
With LHC 13/14 TeV data until 2022 (~300 fb-1)
  Measure the Standard Model scalar boson properties
    Mass, JCP
    Individual couplings with 5-15% precision
  Search for new physics at higher mass scale (new energy region)
    SUSY, Exotics
With HL-LHC 14 TeV data until 2032 (~3000 fb-1)
  High precision SM scalar boson measurements
    Couplings <5%, study rare decays, self-coupling
Higgs triple self coupling
P. Wells, Lepton Photon 2013

## Slide 7
HL-LHC Physics Programm (II)
Study VV scattering
  Verification that Higgs boson cancel divergences in VBF
Direct searches of BSM particles
  HL-LHC increases the discovery reach by ~400-500 GeV
ATLAS simplified model with zero mass LSP
P. Wells, Lepton Photon 2013

## Slide 8
The present ATLAS Pixel system

## Slide 9
The present ATLAS Pixel system
Sensors and modules:
• 250 μm thick n-on-n type silicon, with typical pixel granularity of 50 mm x400 μm.
• 16 FE-I3 chips per module bump-bonded to a single sensor
1456 modules in the barrel region and 288 modules in the three end-cap discs per side
FE-I3 chip

## Slide 10
Tracker Performance today
ATLAS
Up to 4000 tracks per event every 25 ns
Up to ~70 interaction /BX
ATLAS was designed for 23 evt /BX but continues to do an excellent job with 35
99.9 % Pixel data taking efficiency in 2012
Hit-to-track association efficiency ~99%
95% of modules are active during data taking in 2012
Inoperable fraction gets addressed in LS1 repair (is now ~ 1%)
E. Stanecka, Vertex 2013

## Slide 11
Pixel Detector Performance today
ATLAS
Threshold tuned to 3500 e, with 40 e dispersion
Time Over Threshold: time in which signal is above threshold in units of BC, 25 ns
Tuning target is 30 BC for a charge of 20,000 e (most probable value for m.i.p.)
Advantages:
  improved position resolution (shared hits)
  energy loss proportional to deposited charge ➞ particle identification
11
p
k
p
d
T. Ince, Siena 2013

## Slide 12
The Insertable B-layer

## Slide 13
Phase 0 Upgrade: the Insertable B-Layer
Designed to let ATLAS cope with L=3x1034 cm-2 s-1
New 4th pixel silicon barrel layer with r = 3.3 cm, 12 MegaPixel
  Needs small radius (r = 2.35 cm) beam pipe
  14 staves with Φ = 14° tilt angle & no z overlap
Redundancy to control the fake rate
Improve b-tagging
Good performance with IBL and pile-up  as good or better as for the current ATLAS without pile-up

## Slide 14
The ATLAS Insertable B-layer
130 nm CMOS
150 μm thickness
Charge by 4 bits ToT
160 Mb/s readout
Power 200 mW/cm2
Total dose tested up to 750 MRad
New FE-I4 chip, 2x2 cm2, pitch 50x250 mm2

## Slide 15
Pixel electrodes on surface of bulk
Proven ATLAS Pixel Detector technology and vendor: CIS
Very high yield (90% accepted for IBL production)
From old pixel system to IBL:
  Pixel size 50x400 μm2 → 50x250 μm2
  Thickness 250 μm → 200 μm
  Inactive edge 1 mm→ 200 μm
Vertical 2E electrodes
Reduced operational voltage after irradiation
230 μm thickness
Two 3D sensor vendors (CNM and FBK)
Acceptable yield (60% for IBL)
Planar n-in-n oxygenated Si sensor
3D double sided silicon sensors
Pixel Sensors for the IBL

## Slide 16
N-in-n pixels for IBL – Slim edge
Study of edge efficiency in beam tests for for FE-I4 n-in-n modules (IBL type)
Before and after irradiation a clear dependence on the bias voltage is visible
reduction of the inactive edge to ~200 mm demonstrated
CIS production of IBL sensors
Pixel on front-side
GR Back-side
other 100 mm to the edge
T. Wittig, Pixel 2012

## Slide 17
3D pixel sensors
First proposed by S. Parker et. al. in NIMA 395 (1997), 328
Columns etched with Deep Reactive Ion Etching

## Slide 18
3D pixel sensors
ADVANTAGES
Electrode distance and substrate thickness decoupled
High speed
Good charge collection efficiency  good radiation hardness
DISADVANTAGES
Non uniform response due to electrodes
Complicated technology
Higher capacitance with respect to planar
First proposed by S. Parker et. al. in NIMA 395 (1997), 328

## Slide 19
3D pixel sensors for IBL
Slim-edge: Dead region along the beam axis < 225 mm
CNM sensors, Vbias=160 V, F=5x1015 neq cm-2
C. Gemme, Vertex 2013

## Slide 20
The ATLAS Pixel System in the Phase II Upgrade
Proton-proton collision energy √s=14 TeV
● Instantaneous luminosity of L=5x1034 cm‑2s‑1
● Average number of 'pile-up' collisions per
event <μ> = 130-140
● Integrated luminosity 3000 fb-1 over the entire run
I. Gregor, DESY

## Slide 21
Development of planar pixel sensors
for Phase II

## Slide 22
The layout proposed in the LoI provides 14 points/track to |n| < 2.7
Pixel: 4 layers + 6 disks
Phase II Pixel System Layout and requirements
2 Outer Barrel Layers / Disks
2 Inner Barrel Layers
Probably planar n-in-p
Sensor thickness 150 mm
Pixel size 50x250 mm2
2x2 (Quad) and 2x3 (Hex) chip modules
Sensors: different materials and technologies possible
Radiation hardness up to 2x1016 neq/cm2
Thickness: 150 mm or lower
Pixel size 25x150 mm2  FE-chip in 65 nm CMOS technology
H. Hayward, Hiroshima 2013

## Slide 23
Comparison between n-in-n and n-in-p technologies
M. Benoit et al., IEEE Trans. On Nuclear Science, VOL. 56, NO. 6, DECEMBER 2009
Standard Guard-Ring
double sided
slim edges down to 200 mm possible
n-in-n technology
Depletes from the segmented side
Single sided process
30-40% cheaper than n-in-n
More foundries and available capacity world-wide
Easier handling-testing due to lack of patterned back-side implant
230 mm
n-in-p technology

## Slide 24
Sensor-chip isolation techniques for n-in-p pixels
Danger of sparks between the chip and the sensor edges at HV
  distance of the order of the bump height ~ 30 mm
3 mm of Benzocyclobutene (BCB) on the sensor surface, litography needed  No sparks observed up to 1000V
Parylene-C deposited all over the module (5-10 mm per side)  tested up to 650V, no sparks.
  Some hints of radiation damage from preliminary studies on test-structures. Parylene-N seems more resistant
Silicon adhesive on the wire bonding side  no sparks observed up to 1000V
HV

## Slide 25
n-in-p performance – FE-I3 modules
MPP/HLL design produced by CiS on 285 mm FZ. n-irradiated up to 1016 neq/cm2
Charge exceeds threshold by a factor of 2
Testbeam with Eudet telescope
Hit efficiency of 97.2% at highest fluence, 600V and threshold of 2 ke (98.1% in central region)
Main losses in punch through and corners for perpendicular tracks

## Slide 26
FE-I3 samples n-in-n
250 mm thickness
PbSn bump-bonded
1000 V
F=1.4x1016 neq/cm2, p irr.
n-in-n performance – FE-I3 modules
26
T. Wittig, Pixel 2012

## Slide 27
designed and produced by MPP/HLL
6” wafers with FE-I4 sensors interconnected with bump-bonding at IZM
irradiated up to 4x1015 neq/ cm2 in KIT and Los Alamos
FE-I4 modules 150 mm thick

## Slide 28
Hit efficiency at different h incidence
99.1 %
96.6 % hit efficiency for the full module at perpendicular incidence (500V)
FE-I4 150 mm thick, irradiated to 4x1015 neq/cm2 in Los Alamos
bias voltage: 500 V, Threshold:1600 e-
28

## Slide 29
Hit efficiency at different h incidence
99.0 %
98.4 % hit efficiency for the full module at q=30o (h=0.55) incidence (500V)
FE-I4 150 mm thick, irradiated to 4x1015 neq/cm2 in Los Alamos
bias voltage: 500 V, Threshold:1600 e-

## Slide 30
Hit efficiency at different h incidence
99.5 %
99.5 % hit efficiency for the full module at q=45o (h=0.88) incidence (500V)
FE-I4 150 mm thick, irradiated to 4x1015 neq/cm2 in Los Alamos
bias voltage: 500 V, Threshold:1600 e-

## Slide 31
Hit efficiency at different h incidence
99.8 %
99.8 % hit efficiency for the full module at q=85o (h=3.1) incidence (500V)
FE-I4 150 mm thick, irradiated to 4x1015 neq/cm2 in Los Alamos
bias voltage: 500 V, Threshold:1600 e-

## Slide 32
Sensor thickness and occupancy at high eta
Mean cluster width along the beam direction as a function of the pseudo-rapidity
Assumed FE-I4 chip pitch along z: 250 mm
Reduced cluster size along the beam direction for thin sensors at high eta!

## Slide 33
Active area design optimization
Poly-Silicon
Punch through
No Bias
Type (1, 9)
Type (2, 10)
Type (3, 11)
Type (4, 12)
Type 17
Type 18
Type 19
New KEK-HPK productions of FE-I4 sensors
Study of different pixel biasing schemes : Punch-through and poly-silicon
Yoshinobu UNNO, KEK
p-stop

## Slide 34
Slim edges planar pixel sensors - Overview
Active edges for n-in-p pixels: Deep Reactive Ion Etching + Side implantation
IBL design
Design optimization of the n-in-n sensors: GR on backside opposite to pixels on the front

## Slide 35
Active edge planar pixels
n-in-p pixels on FZ and MCZ material
100 mm and 200 mm thickness together with the active edges makes these sensors very attractive candidates for the inner layers in Phase II
p-spray isolation method transferred from HLL to VTT
Flip-chipping performed at VTT after removal of support wafer

## Slide 36
Active edge: geometry and IV characterization
125 mm edge implemented In FE-I3 and FE-I4 sensors: Bias Ring + floating Guard Ring
50 mm implemented only in FE-I3 sensors: Floating Guard Ring
Very low leakage current level, < 100 nA for FE-I3 and FE-I4 sensors
Breakdown voltage at 100-110V, much higher than depletion voltage ~ 15V

## Slide 37
FE-I3, 125 mm edge,
Vbias=20V
Global Efficiency in beam test
Edge Tracking Efficiency in Beam Tests at SPS
Hit efficiency in the edge region
99-100% hit efficiency on the area of the pixel implant of the edge column
% efficiency in the last 50 mm of the sensor edge, beyond last pixel implant
FE-I3, 50 mm edge,
Vbias=20V

## Slide 38
F= (0 -1) e15
F=2 e15
FE-I3 100 mm thick sensor with 125 mm slim edge, threshold 1500 e-  87% CCE at 300 V for both all and edge pixels after irradiation at KIT (1x1015 neq/cm2)
p-type MCZ FE-I4, 100 mm thick sensor, with 125 mm slim edge, threshold 1100 e-  compatible charge collection properties between edge and internal pixels
F= (0 - 5) e15
Active edge: CCE after irradiation

## Slide 39
F= (0 -1) e15
F=2 e15
Active edge: CCE after irradiation
FE-I3 100 mm thick sensor with 125 mm slim edge, threshold 1500 e-  87% CCE at 300 V for both all and edge pixels after irradiation at KIT (1x1015 neq/cm2) and in Ljubljana (5x1015 neq/cm2)
p-type MCZ FE-I4, 100 mm thick sensor, with 125 mm slim edge, threshold 1100 e-  compatible charge collection properties between edge and internal pixels
F= (0 - 5) e15
F= (0 - 5) e15
39

## Slide 40
Charge collection for pixels of different thickness
F= 2 e15
F= 4-5 e15

## Slide 41
Charge collection for pixels of different thickness
The 100-150 mm thick sensors show higher charge collection up to a fluence of 4-5x1015 neq / cm2
At higher fluences the effect of charge trapping tends to equalize the charge collection efficiency for all thicknesses
F= 2 e15
F= 4-5 e15
F= 10 e15

## Slide 42
Ref: Diode: J.Lange et al, 16th RD50 Workshop, Barcelona
Strip: G. Casse et al., NIMA 624, 2010, Pages 401-404
3D: M.Koehler et al., 16thRD50 Workshop, Barcelona
Charge Multiplication observed and characterized after high levels of irradiation with different techniques and in several different types of devices
Diodes (Feq=1016 cm-2)
Leakage Current & Charge Collection
Strip sensors (Feq=5×1015 cm-2, 26 MeV p)
Charge Collection (Beta source, Alibava)
3D sensors (Feq=1-2×1015 cm-2)
Charge Collection (test beam)
140 mm thick device
300 mm thick device
Charge multiplication

## Slide 43
Vertical Integration Technologies
and 3D sensors for Phase II

## Slide 44
Vertical Integration Technologies
New demanding specifications for experiments at new machines:
Improve resolution  shrink pixel size and pitch, down to 20 mm or even less
Preserve or even increase pixel-level electronic functions: handling of high data rates (hit rates > 10 MHz/mm2), analog-to digital conversion while reducing the pixel size
Decrease amount of material  thin sensor and electronics chips, “zero mass” cooling
100-200 mm total module thickness
3D electronics: “the vertical integration of thinned and bonded silicon integrated circuits with vertical interconnects between the IC layers”

## Slide 45
No roadmap, room for new ideas: monolithic sensors, 3D integration
Evolutionary roadmap:
nanoscale CMOS
Evolution of Micro-Electronic Technologies
Through Silicon Vias
Micro-channel cooling
Monolithic sensors
Valerio Re, Vertex 2013

## Slide 46
Via first, Via middle: Vias are part of wafer processing at the CMOS foundry, and are inserted before or right after the fabrication of transistors
 High density TSVs (few mm pitch) through thinned wafers, allow multiple connections at the cell (pixel) level between transistor layers
Via last: Vias are fabricated on fully processed CMOS wafers, at a facility outside the CMOS foundry
 Low density TSVs (tens of mm pitch) through unthinned wafers or partially thinned wafers, allow connectivity at the pad level in the chip periphery
Through Silicon Vias: Via First or Via Last
Valerio Re, Vertex 2013

## Slide 47
Through Silicon Vias
TSV on front-side
TSV on back-side
TSV on back-side
FE-I3 chip: TSV (3x10 mm2) etching the chip front-side
Processing sequence:
Via- and trench etching in Bosch-process, TSV cross-sect. of 3x10 mm2
insulation with TEOS (low T)
filling of vias with Tungsten
attachment to handle-wafer on the top side and thinning to desired thickness of chip ~ 60 mm
redistribution layer on the backside
SLID-interconnection to sensor wafer.
Failure of tungsten filling

## Slide 48
Through Silicon Vias
TSV on front-side
TSV on back-side
TSV on back-side
FE-I3 chip: TSV (3x10 mm2) etching the chip front-side
Processing sequence:
Via- and trench etching in Bosch-process, TSV cross-sect. of 3x10 mm2
insulation with TEOS (low T)
filling of vias with Tungsten
attachment to handle-wafer on the top side and thinning to desired thickness of chip ~ 60 mm
redistribution layer on the backside
SLID-interconnection to sensor wafer.
Failure of tungsten filling
No tungsten adhesion within the TSV

## Slide 49
Through Silicon Vias
TSV on front-side
TSV on back-side
TSV on back-side
FE-I3 chip: TSV (3x10 mm2) etching the chip front-side
FE-I4 chip: TSV (~10x30 mm2) etching the chip back-side
TSV

## Slide 50
SLID Interconnection
Alternative to bump bonding (less process steps “lower cost” (EMFT)).
Small pitch possible (~ 20 mm, depending on pick & place precision).
Stacking possible (next bonding process does not affect previous bond).
Wafer to wafer and chip to wafer possible.
Successful interconnection run with FE-I3 chips and sensors with 75 mm active thickness
Stable SLID interconnection after irradiation and thermal cycling
Good Charge Collection efficiency after irradiation up to 1016 neq/cm2

## Slide 51
3D pixel sensors for Phase II
Development of active edges with the use of a handle wafer
3D Pixels for Phase II: first indications of good radiation resistance up to a fluence of 2x1016 neq/cm2
R&D for Phase II:
  Thinner sensors
  Active edges
Etched trench + electrode
Charge Collection by X-ray beam
Cinzia Da Via’, Hiroshima 2013

## Slide 52
Micro-channel cooling
3D Pixels for Phase II: embedded micro-channels with CO2 cooling
Chip footprint
Holes for fluidic inlet and outlet
35 micro-channels
50 mm x 50 mm separated by 200 mm walls
Cinzia Da Via’
Hiroshima 2013

## Slide 53
Micro-channel cooling
3D Pixels for Phase II: embedded micro-channels with CO2 cooling
Target for new 65 nm chip: 400 mW/cm2
Power dissipation for 3D sensor at 2x1016 neq/cm2  450-500 mW/cm2
Total power: 850-900 mW/cm2
Cinzia Da Via’ Hiroshima 2013

## Slide 54
3D diamond sensors
RD42 Collaboration
Holes drilled with 800 nm femto-second laser
93% efficiency for column etching
Diamond sensor 500 mm thick
Cr-Au electrodes connecting a row of electrodes into a strip
Read-put by the VA2 chip
Columns are conductive ~1 W cm
S. Schnetzer, Vertex 2013

## Slide 55
Summary and Outlooks
For outer pixel layers:
Standard hybrid pixel detectors most likely planars, with
advanced concepts to save material (TSV, SLID, thin sensors, …)
ATLAS pixel detector is essential for the experiment and will be upgraded in the future:
• A 4th pixel layer (IBL) is well under construction and will be installed in spring 2014 during LS1 of LHC.
• Upgrade to luminosities of 5x1034cm-2s-1 and ~250 pile up events pushes the challenges for pixel detectors in new directions.
Looking to the phase 2 plans of the ATLAS pixel detector is difficult now, but
For inner pixel layers:
• hybrid pixels either with FE electronics in 65nm or 3D integrated electronics; sensors could be planar, 3D or diamond
A lot more R&D is needed!

## Slide 56
Additional material

## Slide 57
3D pixel sensors for IBL
FBK: temporary metal for testing
CNM: Guard Ring without connection to single pixels
FBK
CNM
Wafers are selected for UBM if at least 3 tiles out of 8 are good (Vbk >25 V)
CNM yield significantly higher than FBK but FBK measurement on full device, CNM on Guard Ring only.
230mm thick 3D sensors
Produced without handle wafer
C. Gemme, Vertex 2013

## Slide 58
Active edge: IV after irradiation
Active edge modules irradiated up to a fluence of 5x1015 neq/ cm2 have a breakdown voltage above the saturation voltage of the charge collection
Lower breakdown voltages with respect to thin pixel devices with standard GR structure irradiated at the same fluence
100 and 200 mm thickness, active edge
75 mm thickness, standard guard ring
150 mm thickness, GR with 450 mm inactive edge

## Slide 59
Active edge: charge collection with a 90Sr a source
FE-I3
50 mm edge
Vbias=15 V
FE-I4
125 mm edge
Vbias=15 V
Edge pixels show the same charge collection properties as the central ones

## Slide 60
DESY test-beam – Active edge sensors
VTT 100 mm MCz
threshold: 1600 e, F=2x1015neq/cm2
97.3% global efficiency at 350 V
VTT 200 mm Float Zone (FZ)
threshold: 1100 e, F=2x1015neq/cm2
98.9% global efficiency at 350 V
VTT 100 mm FE-I3 Float Zone
125 mm slim edge, threshold: 1500 e
F=5x1015neq/cm2
Vbias=400V
global hit efficiency
97.5 ±0.3%

## Slide 61
Smaller pitches for internal layers
25 mm x 500 mm pitch
Test for Rf pitch of 25 mm, as foreseen for inner layers of phase II upgrade in ATLAS
Longer pixels in the z direction (500 mm) to restore compatibility with the FE-I4 chips
MICRON – Liverpool University
Values of the residual are approximately what is expected for pitch / √12
H. Hayward, Liverpool
Hiroshima Symposium 2013

## Slide 62
High eta cluster analysis
FE-I4 150 mm thick, irradiated to 4x1015 neq/cm2 in Los Alamos
85O track incidence ( h=3.1)
bias voltage: 500 V
threshold: 1.6 ke (MPV 9.5 ke)
~ 7.8
Mean cluster width expected along the tilted direction for different incidence angles
Cluster distribution along the tilted direction.
Distribution mean = 6.7

## Slide 63
Power dissipation -3D
At 2x1016 and T=-10C  power disspation =400 mW/cm2

## Slide 64
Power dissipation - Planar
At 2x1016 current=1 mA
Vbias=1500 V
T=-15C on the sensor
Power dissipation 1.5 W

## Slide 65
Alternative to bump bonding (less process steps “lower cost” (EMFT)).
Small pitch possible (~ 20 mm, depending on pick & place precision).
Stacking possible (next bonding process does not affect previous bond).
Wafer to wafer and chip to wafer possible.
EMFT SLID Process
FE-I3
Sensor
27 mm
Cu3Sn
Cu6Sn5

## Slide 66
Chip-sensor interconnection technologies
Solder bump-bonding with different companies:
  IZM Berlin, HPK : SnAg bumps
  VTT (ADVACAM), SnPb bumps
  IZM, HPK: chip thickness down to 150 mm with the use of a glass substrate
  VTT: chip thickness down to 200 mm
Alternative interconnection technologies – Micro-Cu Pillars
Cu post / SnAg solder
50 mm pitch
25 mm diameter
8-12 mm thickness
FE-I4B with micro-pillars
Glasgow-LETI-ADVACAM collaboration
C. Butter, Hiroshima Symposium 2013

## Slide 67
Smaller pitches for internal layers
25 mm x 500 mm pitch
Test for Rf pitch of 25 mm, as foreseen for inner layers of phase II upgrade in ATLAS
Longer pixels in the z direction (500 mm) to restore compatibility with the FE-I4 chips
One bias dot every four pixels
MICRON - Liverpool
CIS - MPP
Type 21
Type20
PT No offset
END1
END2
KEK – HPK
Confidential for ATLAS (and CMS)

## Slide 68
n-in-p performance – FE-I4 modules
KEK-HPK n-in-p FE-I4 sensors, 150 mm thickness
Bump-bonded at HPK
Irradiated at F=1e16 neq/cm2, Vbias=1200 V
Poly-Si, p-stop
Poly-Si, p-spray
PT, p-spray
> 99.7 % already at 600V in the electrode region of each sample
Overall hit efficiency = 96.3%
Overall hit efficiency = 97.1%
Overall hit efficiency = 97.6%
Kazuki MOTOHASHI
Hiroshima Symposium 2013

## Slide 69
F= (0 -1) e15
Charge collection efficiency after irradiation
Landau distribution obtained at the DESY test-beam with 4 GeV electrons
F= (0 - 5) e15
FE-I3 100 mm thick sensor with 125 mm slim edge, threshold 1500 e-  irradiated in Ljubljana at 5x1015 neq/cm2

## Slide 70
Test-beam results – 100 mm thick sensors
VTT MCZ, 100 mm thick, F=2e15  total efficiency 97.3% at 350 V
98.8 %
VTT FZ, 100 mm thick, not irradiated  total efficiency 99.7% at 40 V
Test-beam results from DESY test-beam 6 GeV electrons, EUDET telescope  due to multiple scattering the analysis of the edge efficiency is not possible
Tuning Threshold=1600 e, 6 ToT@6ke, beam at perpendicular incidence

## Slide 71
Edge efficiency after irradiation
not irradiated
threshold: 1500 e
PPS test-beam with 120 GeV pions
68 ±1% hit efficiency between the last pixel implant and the Bias Ring
125 mm slim edge FE-I3 module with Bias Ring
F=5x1015 neq/cm2
400 V
threshold: 1500 e
DESY test-beam with 4 GeV e-
56±4% hit efficiency between the last pixel implant and the Bias Ring

## Slide 72
SCP: Scribe Cleave Passivate
Diamond stylus
Laser
XeF2 Etch
DRIE Etch
Saw cut (with cleanup step)
Tweezers (manual)
Loomis Industries, LSD-100
Dynatex, GTS-150
Native SiO2 + UV light or high T
PECVD SiO2
PECVD Si3N4
ALD “nanostack” of SiO2 and Al2O3
ALD of Al2O3
N-type P-type (Qf > 0) (Qf < 0)
All Treatment is post-processing & low-temp (Etch-scribing can be done during fabrication)
Basic requirement: <100> wafers (for rectangular side cleaving) with reasonably good alignment between sensor and lattice.
V. Fadeyev
Santa Cruz Institute for Particle Physics
Hiroshima Symposium 201

## Slide 73
SCP: Scribe Cleave Passivate
Diamond stylus
Laser
XeF2 Etch
DRIE Etch
Saw cut (with cleanup step)
Tweezers (manual)
Loomis Industries, LSD-100
Dynatex, GTS-150
Native SiO2 + UV light or high T
PECVD SiO2
PECVD Si3N4
ALD “nanostack” of SiO2 and Al2O3
ALD of Al2O3
N-type P-type (Qf > 0) (Qf < 0)

## Slide 74
Reduction of the inactive region on the chip side
Project within AIDA WP3, in collaboration with Fraunhofer EMFT, to develop Inter Chip Vias to show the feasibility to transport signals and services on the backside using the existing FE-I4 chip
Inter-Chip-Vias to be etched on each wire bonding pad, cross section ~ 10x30 mm2
Chip and sensor connected using SLID technology

## Slide 75
Inter Chip Vias in the FE-I4 chip
Most of the eight FE-I4 metal layers are present in the wire bonding pads  not possible to etch ICV from the front-side
Design and test of the ICV layout on test-wafers in on-going: target cross-section 10x30 mm2 with a global chip thickness of 100-150 mm
SEM analysis of the FE-I4 wire bonding pad

## Slide 76
Multi-chip modules
6” wafers from different producers – CIS is also starting the transition from 4” to 6” line
Quad and HEX modules
CIS n-in-n
MICRON n-in-p
FE-I4 2-chip pixels
FE-I4 1-chip pixels
FE-I3 1-chip pixels
FE-I3 4-chip pixels
HPK n-in-p
CIS n-in-p

## Slide 77
Multi-chip modules read-out systems
USBPix (Bonn) + STControl (Gö)
SEABAS (KEK))
RCE (SLAC)
3 different DAQ systems available in ATLAS for simultaneous steering and reading of 4-chip modules

## Slide 78: L1Track Trigger
Adding tracking information at Level-1 (L1)
  Move part of High Level Trigger (HLT) reconstruction into L1
  Goal: keep thresholds on pT of triggering leptons and L1 trigger rates low
Triggering sequence
  L0 trigger (Calo/Muon) reduces rate within ~6 μs to ≳ 500 kHz and defines RoIs
  L1 track trigger extracts tracking info inside RoIs from detector FEs
Challenge
  Finish processing within the latency constraints