## Slide 1: Sezione di Roma Università degli studi di Cassino e del Lazio meridionale1 ENEA centro ricerche «Casaccia»2 Sezione di Padova Università degli studi di Padova3 Irraggiamenti su dispositivi GaN C. Abbate1, S. Baccaro2, G. Busatto1, S. Fiore2, S. Gerardin3, F. Iannuzzo1, A. Sanseverino1, G. Spiazzi3, F. Velardi1
Roma, 9 Dicembre 2013 Workshop conclusivo esperimento APOLLO Dipartimento di Fisica, Università degli studi “La Sapienza” ROMA
Gruppo V APOLLO
Alimentatori di POtenza per aLti Livelli di radiaziOne

## Slide 2: GaN HEMTs: Devices
GaN High Electron Mobility Transistors
  Enhancement-mode GaN transistors
  Manufactured by Efficient Power Conversion (EPC)
  Blocking voltage 40/200 V
  Maximum IDS is 12/33 A continuous, 60/150 A pulsed
From EPC website

## Slide 3: GaN HEMTs: Potential for Radiation Hardness
Material
  GaN is quite hard to displacement effects. Minimum energy to displace GaN atoms is larger than in Si and GaAs, close to SiC
Heterostructure
  Channel is formed through band engineering
  In principle, no dielectric layers are used underneath the gate, so tolerance to total dose is expected to be excellent
From EPC website

## Slide 4: GaN HEMTs: Potential for Radiation Hardness (2)
Questions marks
  No information are provided as to how enhancement-mode has been achieved
  Some additional layers have been probably introduced to engineer the positive threshold voltage
  What’s the impact on radiation hardness?
From EPC website

## Slide 5: Irradiation campaigns on GaN
Gamma rays1
Heavy ions2
Combined Gamma/Heavy ions1,2
Protons3
Facilities:
ENEA Calliope
Tandem LNL
CN LNL

## Slide 6: Combined Gamma/Heavy ions
Irradiation campaigns on GaN

## Slide 7: Sample preparation
Device: EPC 2015
ratings: 40V 33A
Detail of the used PCB (device is not EPC2015)

## Slide 8: Gamma irradiations
Dose steps:
  0 Gy (Fresh)
  570 Gy
  1.1 kGy
  1.7 kGy
  5.2 kGy
  10.8 kGy
Bias conditions:
  Vgs=+4V
  Vds=0

## Slide 9: Heavy ion irradiation
Species
  127I at 276MeV
Irradiated samples:
  Fresh
  annealed Fresh
  annealed 1.1kGy
  annealed 1.7kGy
  annealed 5.2kGy
  annealed 10.8kGy

## Slide 10: Experimental setup for heavy ion irradiations
RDS is very critical for GaNs:
  high values (≈1MW) slow down pulses (plenty of double pulses that frustrate statistics) and degrades S/N ratio
  low values (≈50W) filters out the pulse signals

## Slide 11: Measurement procedure
Collected waveform population at Vds=30V
Scatter plot
Average charge

## Slide 12: Results (1)
Annealed fresh
  sample-to-sample variability!
D1A
D2A
D4A

## Slide 13: Results (2)
Increasing gamma doses
570Gy
1.72kGy
5.15kGy
10.9kGy
Difficult interpretation, but no rupture

## Slide 14: Gamma irradiation: conclusions
New experimental setup allowed acquiring large quantity of samples for the sake of statistics
Sample-to-sample variability is to be faced
Hardly interpretable dependence of the generated charge on the applied voltage
Further analyses with higher surface energy loss (less range?) should be performed in the future
Tested device appear to be very hard to combined irradiation

## Slide 15: PROTON IRRADIATIONS
Irradiation campaigns on GaN

## Slide 16: Proton irradiations
Low-energy proton irradiation at Laboratori Nazionali di Legnaro
  3-MeV protons
  Fluence up to 4∙1014 p/cm2
  Energy is too low, to give rise to secondary particles  no indirect SEE
  Ionization and displacement damage

## Slide 17: Proton irradiations (2)
DC parameters have been measured before and after 1.8 MeV proton irradiation
Observed effects include:
  Increase in gate current
  Threshold voltage reduction
  Transconductance drop
We investigated damage dependence on
  proton fluence
  blocking voltage

## Slide 18: Post-rad Gate Current – EPC2010
Device exposed to 1014 p/cm2 in unbiased conditions
Increase in gate current at all voltages, up to one order of magnitude
More pronounced for negative voltage
Some room temperature annealing

## Slide 19: Post-rad Drain Current
Unexpected decrease in threshold voltage (1V)
Degraded substreshold slope
Modest room-temperature annealing
Device exposed to 1014 p/cm2 in unbiased conditions

## Slide 20: Post-rad Transconductance
Peak transconductance drop, more than 30%
Drain current almost unchanged: threshold voltage reduction offset transconductance degradation
Device exposed to 1014 p/cm2 in unbiased conditions

## Slide 21: Literature Data (1)
Drain current decrease is typically reported on depletion-mode devices in the literature, in contrast with the behavior of EPC samples
Difference due to unknown process steps or introduction of dielectric layers?
From Karmakar et al., IEEE-TNS 2004

## Slide 22: Literature Data (2)
From Weaver et al., IEEE-TNS 2012
Compilation of several test data over the course of ten years for GaN HEMTs
All devices show decreases in drain current

## Slide 23: Proton irradiation: conclusions
Small dependence of degradation on blocking voltage: 40V vs 200V
Small dependence of degradation on proton fluence
Sample-to-sample variability
Possible superimposition of displacement effects and ionization effects
Unbiased conditions may not be the worst-case, if ionization effects are present
Degradation only at very high fluence of low-energy protons (worst-case condition for ionization and displacement)