## Slide 1
The SPES Target
Ion Source complex
Alberto Andrighetto
LNL-INFN
2° SPES workshop, 26 May 2014

## Slide 3
The TIS device
7 UCx coaxial disks:
thickness: 1.3 mm
diameter: 40 mm
Graphite box:
external diameter: 49 mm
average length: 200 mm
3 graphite dump disks
Tantalum tube:
external diameter: 50 mm
thickness: 0.35 mm
length: 200 mm
Ionizer & transfer tube:
thickness: 1 mm
height: 34 mm
Inner diameter: 3 mm
SPES Heater, Ionizer & Chamber
SPES Target :
Optimized for 8 kW power dissipation
(E= 40 MeV, I= 200 μA)
Aluminum target unit

## Slide 4
The target calculations
SPES
in
-
target yields (10
13
fissions
per
second)
a) Thermo Mechanical
c) Isotopes Effusion
b) Neutronics & Isotopes Yield

## Slide 5
ILine= 200A -> 600A max
ITarget= 700A -> 1200A max
The target & ion source complex

## Slide 6
The SPES off-line Front end
(working since 2010 - evolution of ISOLDE FE6)

## Slide 7
WG-1: Target and Ion Sources
-> M. Manzolaro
WG-2: Target Materials
-> S. Corradetti
WG-3: Laser
-> D. Scarpa
WG-4: Handling
-> M. Calderolla
WG-5: Front End
-> A. Monetti
The SPES-RIB prod. Working Groups

## Slide 8
HT LNL Lab
Test Bench LNL Lab
Carbide Chemistry LNL Lab
UCx Chemistry PADOVA Lab
New ‘class A’ LNL Lab
Pavia laser Lab
New LNL laser Lab
The SPES-RIB prod. Laboratories

## Slide 9
 | 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 18
1 | 1 H | 2 |  |  |  |  |  |  |  |  |  |  | 13 | 14 | 15 | 16 | 17 | 2 He
2 | 3 Li | 4 Be |  |  |  |  |  |  |  |  |  |  | 5 B | 6 C | 7 N | 8 O | 9 F | 10 Ne
3 | 11 Na | 12 Mg | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 Al | 14 Si | 15 P | 16 S | 17 Cl | 18 Ar
4 | 19 K | 20 Ca | 21 Sc | 22 Ti | 23 V | 24 Cr | 25 Mn | 26 Fe | 27 Co | 28 Ni | 29 Cu | 30 Zn | 31 Ga | 32 Ge | 33 As | 34 Se | 35 Br | 36 Kr
5 | 37 Rb | 38 Sr | 39 Y | 40 Zr | 41 Nb | 42 Mo | 43 Tc | 44 Ru | 45 Rh | 46 Pd | 47 Ag | 48 Cd | 49 In | 50 Sn | 51 Sb | 52 Te | 53 I | 54 Xe
6 | 55 Cs | 56 Ba | 57 La | 72 Hf | 73 Ta | 74 W | 75 Re | 76 Os | 77 Ir | 78 Pt | 79 Au | 80 Hg | 81 Tl | 82 Pb | 83 Bi | 84 Po | 85 At | 86 Rn
7 | 87 Fr | 88 Ra | 89 Ac | 104 Unq | 105 Unp | 106 Unh | 107 Uns | 108 Uno | 109 Une | 110 Unn |  |  |  |  |  |  |  | 
Main fission (p-> 238U) fragments
surface ionization mechanism
laser ionization mechanism
electron impact ionization mechanism
not extracted
target + Re hot-cavity ion source
target + Ta hot-cavity ion source
target + FEBIAD ion source
WG-01

## Slide 10
Ion Source Developments
> The Ion Source adopted for the SPES facility
The SIS Ion source
Efficiency measurements at different temperatures (1600°C, 1800°C, 2000°C, 2200°C) for Cs, Rb, Sr, Ba
screen support
screen
The PIS Ion source
Ionization efficiency measured for Ar; Kr and Xe beams has been produced
WG-01

## Slide 11
> Emittance measurements for SIS and PIS (@ 25kV extraction voltage)
Ion Source Developments
WG-01
Chart: electrode - ion source distance (mm)
| 85.3 | 73.699999999999989 | 62.1 | 50.5 | 38.900000000000006 | 27.299999999999997 | 15.700000000000003
emittance RMS | 7.31 | 4.8287 | 5.4297 | 7.4467 | 9.8723 | 13.0907 | 14.9177
PIS (Ar beam)
RMS ≈ 10 π mm mrad (90% ≈ 40 π mm mrad)
Chart: electrode - ion source distance (mm)
| 109.4 | 97.800000000000011 | 86.2 | 74.600000000000009 | 63.000000000000014
emittance RMS | 3.8575 | 2.9645 | 2.872 | 2.63 | 2.8755
SIS (Cs beam)
RMS ≈ 5 π mm mrad (90% ≈ 20 π mm mrad)

## Slide 12
Ion Source Developments (SIS)
Ta - SIS efficiency data (off-line measurements)
> Efficiency measurements for SIS
T = 2200 °C
WG-01

## Slide 13
Ion Source Developments (PIS)
Ionization efficiency measurements for Ar (25 kV)
- Anode voltage = 150 V
- Anode magnetic field ≈ 300 G
- Total beam current ≈ 3 µA
> Efficiency measurements for PIS
WG-01
Cathode Improvement

## Slide 14
1) scaled (d = 13 mm) SiC SPES tested @ ORNL (2007), – 40 MeV, 12 mA p beam, for thermal & release study
2) scaled (d = 13 mm) UCX SPES tested @ ORNL (2010-2011) – 40 MeV, 50 nA p beam, for relase study
 | 2010 Standard UCX | 2011 Low density UCX
Density (g/cm³) | 4.25 | 2.59
Diameter (mm) | 12.50 | 13.07
Thickness (g/cm²) | 0.41 | 0.41
Calculated porosity (%) | 58 | 75
Experimental test 1/3
WG-02
Chart: Graphite Container Temperature
| 300 | 400 | 500 | 550 | 600 | 600 | 650 | 700 | 750
Experimental - With shields | 1173 | 1382 | 1605.3333 | 1734.6667 | 1813 | 1871
FEM - With shields | 1932 | 1815 | 1669

## Slide 15
3) scaled (d = 14 mm) UCX-CNT discs tested @ CERN (2009) and IPNO (2013) for release efficiency studies
Test @ IPNO (2013)
Test @ CERN (2009)
 | UCX-CNT (synthesis at CERN, 2009)
Density (g/cm³) | 1.30
Diameter (mm) | 14.10
Thickness (mm) | 1.30
Calculated porosity (%) | 88
Experimental test 2/3
WG-02
Actilab ENSAR JRA collaboration

## Slide 16
On-line testing of the SPES target architecture @ iThemba (May 2014)
4) Full scale (40 mm.) SiC @ Ithemba, p=66 MeV, 60 microA for thermal dissipation studies
Experimental test 2/3
WG-02
iThemba LABS: funded to build an RIB target/ion-source like SPES

## Slide 17
FC
Wien Filter
Quadrupoles Deflectors
IS
Laser
Ions
WG-03

## Slide 18
LNL Laser Laboratory
In 2013 a new SPES laser laboratory was build
WG-03
A tunable dye laser system ready for atomic spectroscopy study

## Slide 19
SPES Horizontal Handling system
WG-04

## Slide 20
Horizontal device (AGV based)
Devices under construction at the LNL mechanical workshop
WG-04

## Slide 21: On-line FE design RAD-HARD version
WG-05
before
after
Critical material List
Teflon with glass fibres -> alumina
Polyethylene -> peek
Viton O-rings -> EPDM
Plastic cable insulator -> air (close the target)
Normal motors -> RAD HARD motors

## Slide 22: Radiation damage test Use of the LENA reactor for material testing (collaboration under discussion..)
WG-05
Reactor for research TRIGA Mark II (250 kW) – LENA since 1965

## Slide 23
SPES
TIS
UNIPV
UNIPD
UNITN
DIM
DSC
DEI
ION SOURCES
MATERIALS
DIM
DSC
HANDLING
CONTROLS
The SPES : collaboration network
CERN- ISOLDE
GANIL-SPIRAL 2
ORSAY-ALTO
ITHEMBA
ORNL- HRIBF
RISP-KOREA
European Project:
ENSAR (2010-2014):
JRA Actilab (target material)
ENSAR2 (next call):
JRA Resist (laser technology)
JRA Beamlab (TIS technology)
Since 2004: 52 thesis performed in the frame of target SPES activities
INFN- Pavia
INFN- Milano
INFN- LNS
INFN- Bologna
INFN- Padova
SPES TIS papers
(About 39 contributions since 2004)
UNISI
DSF
LASER
Notes: 26/05/2014
23

## Slide 24
Thanks for your attention!
The SPES-TIS group