## Slide 1
Active edge sensor
low density peripheral TSVs
high density interconnects
Bond pads
low density bump bond
bump bonding
high density TSVs
front-end + ADC
Readout chip
Active edge sensor
memory + digital readout
PARAMETER OPTIMIZATION
Trench
Contact holes
GR1
GR2
GR3
GR4
Active Edge
Layouts for different border terminations
4 Guardring structure
6 Guardring structure
8 Guardring structure
10 Guardring structure
Breakdown voltage versus the oxide thickness in a 4-GR edge termination with different oxide charge densities and Junction Depths
Breakdown voltage versus the oxide charge density for different edge terminations
Best trade-off with 4 GRs, oxide thickness, tox ~ 300nm, Field-plate width, lFP ~ 5µm, and Junction depth Xj=2,4µm
It allows for VBD > 400V at all radiation doses within ~155 mm
Aim: Optimization with TCAD simulation
in order to find best trade-off between edge region size and breakdown voltage.
Four-side buttable module for the assembly of large area detectors
STRUCTURE & LAYOUT
Design and TCAD simulation of planar p-on-n active-edge pixel sensors for the next generation of FELs
Gian-Franco Dalla Betta, on behalf of the PixFEL Collaboration (UniPI, UniPV, UniTN, INFN)

## Slide 2: An alternative design with slim edge
Wafer layout
Rectangular Slim Edge trenches
Columnar Slim Edge trenches
Columns
GR1
GR2
GR3
GR4
Scribe Line
Scribe Line
Trenches
GR1
GR2
GR4
GR3
Scribe Line
Scribe Line
TCAD 3D structure
Structure Layout
IV-curves of a 4-GR edge termination with Slim Edge for different oxide charge densities
Advantages:
Get rid of the support wafer (simpler technology)
Entrance window at low energy can be optimized
Disadvantages and risks
Reduction of VBD
More dead space on border
Final layout of a 6-inch wafer including active edge and slim edge pixel sensors under fabrication at FBK (Trento, Italy)
Structure layout and simulation domain to investigate the Slim Edge approach with TCAD
Structures in the layout:
- Standard test structures
- Pixel-cap extraction structures
- Large diodes with different border
terminations
- Strip sensors with different border
terminations
- The 8x8 Pixel arrays
- The 32x32 Pixel arrays
- The 64x64 Pixel arrays
DASHED TRENCH APPROACH