## Slide 1: R&D Pixel Phase-2 CMS INFN Activities Update
Marco Meschini
on behalf of
Bari, Firenze, Milano B., Perugia, Pisa, Torino
CMS Tracker Week, Phase-2 pixel, Nov 2014

## Slide 2: Pixel Sensors R&D in Italy
Pixel R&D with FBK Trento under INFN agreement
    N in P sensors on 6” wafer production ine
    DWB 6”diam. ~600um total thickness wafers
  Three batches funded:
    The first planar batch is a test to qualify 6” substrates, production line, process quality, cost shared with ATLAS-Italy. Now in production
    The 3D batch will be launched early 2015, cost shared with ATLAS-Italy
    Active Edge batch will follow closely, layouts should be prepared and discussed with FBK by end of 2014. Cost relies on CMS-Italy, 10 Lithographic steps funded
  Thinning after processing and isolation treatment have to be planned as needed
  Bump Bonding of single chip at different companies
  Irradiation campaign
  Test beams

## Slide 3: 6” Wafers
55 wafers Float Zone Si-Si DWB from Icemos Tec. (UK):
  P type
  CZ Handle wafer, very low resistivity, 500mm thick
  FZ Sensor wafer resistivity > 3kOhm cm
  2 thicknesses: 100mm (25 wafers) and 130 mm (30 wafers), to be used for planar, 3D, AE batches
Epitaxial Wafers:
  Extremely difficult to find 6” Epi wafers producers
  At present only one found: Shin-Etsu (Japan). They do not sell directly to CERN, a proxy is needed
  Resistivity range 700-2500 Ohm cm. Possibility to get Res. >1000 Ohm cm
  According to specs Epi layer has large thickness variations from wafer to wafer (130 ± 15 mm). To be checked
  Price is in the high range
  Japan wafer Outer Flat Length standards are different from those of EU foundries, to be followed. Order not yet placed. Epi to be used for 3D and AE if possible

## Slide 4: Planar Batch in Production at FBK
DWB 100 and 130 mm wafers and Float Zone 275 mm wafers
DWB is a new material, hence Float Zone is used as a “Reference”
   verify performance of DWB vs FZ on standard, known pixels before going to 3D pixel production on DWB
Three P_Spray isolation doses (Hi, Medium, Low) will be used on different wafers
P_Spray Central Dose will be used on DWB_100, DWB_130 and FZ_275 to make possible direct comparison of the same dose on different materials
We have designed standard PSIdig sensors with and without P_stop implant to study the performance and isolation
Production status is advanced, delivery expected by end of November

## Slide 5: Planar Batch in Production at FBK Trento, Italy
CMS
ATLAS
FBK QA test structures
ATLAS sensors
(FE-I4)
CMS sensors (PSI_dig)
Wafer periphery filled with common TS from CMS, FBK, ATLAS
TS will be used to qualify the process, to compare with previous productions made elsewhere, to study “simple diode” case, etc.
P_Spray process
P_Stop only where required
Layout finalization at FBK: G. Giacomini, M. Boscardin, N. Zorzi

## Slide 6
Pixels with P_stop
4 replicas MAPSL, KIT
Increasing number of Guard Rings
Pixels without P_stop
The CMS Side of the Moon
Each sensor is replicated from 1 to 5 times in each wafer
Large number of sensors and TS to be measured!
Layout in production at FBK
G. Bolla pixels
55x55um2
30x100um2
50x100um2
translated at FBK from N_in_N to N_in_P
(by G. Giacomini)

## Slide 7: What Can you Find in This Layout?
32 single chip sensors suitable to be bonded to PSI46dig
4 MAPSL sensors for PS modules
5 small pitch sensors
7 different Guard Ring protection designs
  4 from ATLAS from slim edge geometry studies
  1 CMS PSI-like, not present in currently installed detector
  1 FBK according to their technology
  1 HPK large protection ring
  GR’s interleaved with P_Stop rings
Structures to study inter-pixel capacitance down to 50x50um2
A large number of other Test Structures (~50) to study material properties and to make comparisons with known pixels from other vendors/productions
8 single + 1 double chip sensors for ATLAS FE-I4, just in case…

## Slide 8: Planar Batch: 32 CMS_PSI + 5 Small Pitch test Sensors

## Slide 9: Planar Batch: ~50 Test Structures

## Slide 10: MaPSL Sensor
PS Module Outer Tracker
Macro Pixel (M. Dragicevic and M. Printz) version of June 3rd 2014
MaPSA Light project see this week talk by D. Ceresa in
https://indico.cern.ch/event/341319/session/11/contribution/9/material/slides/0.pdf
8 x 12.2 mm2

## Slide 11: “A Displaced Sensor”
Full sensor shifted towards the cut line at right and bottom.
Two versions: 300um and 400um distance between outer GR and cut line
300um
680um

## Slide 12: Open P_Stop Sensor
Pixel with opening in the P_Stop enclosure
No Punch Through implant structure

## Slide 13: Bump Bonding and Related Matters
Bump Bonding: start a.s.a.p., provided quality checks on planar batch are satisfactory
  Contacts with IZM (CMS) and Selex (ATLAS)
Spark Isolation on planar pixels
  BCB? Parylene? To be discussed with BB companies
Sensor Thinning still to be decided

## Slide 14: Towards 3D Pixel Single Side Batch at FBK
Layout studies (ATLAS+CMS) already started, trying to include:
  New pitches: 100x30, 50x50, 25x100 mm2 if possible
  Standard PSI and FE-I4 pixels
  New metal design to read only a few small pitch pixel with PSI (or FE-I4)
P- Epi layer /
P- High Ω•cm wafer
P++ Low Ω•cm wafer
-Vb
Charge Amp.
Bump-bond
metal
Thin-down
Single side 3D process
p++ col
n++ col
Epi – SiSi DWB
100÷150µm
The base idea:
Single side process on Si_Si DWB
Ohmic columns reaching the low resistivity substrate
Junction columns slightly shorter than the active bulk
Reduction of hole diameter down to 5 um
Partial filling with poly
Compatible with edgeless

## Slide 15
P col.
N col.
3D cell layout 1: 50 x 50
50 mm
Bump
pad
50 mm
15 mm
50x50um2 cell design looks feasible

## Slide 16
P col.
N col.
3D cell layout 2: 25 x 100
25 mm
50 mm
Bump
pad
100 mm
~56 mm
100x25um2 cell design looks more risky

## Slide 17
PSI46 compatible test pixels 50 x 50
Single cells 50x50 + grid
100um
100um
Small Pitch sensors: as of today no ROC suitable for readout, we have to imagine alternative solutions for testing

## Slide 18
Double cells 50x100 + grid
PSI46 compatible test pixels 50 x 50

## Slide 19
PSI46 compatible test pixels 25 x 100
Single cells 25x100 + grid

## Slide 20: News from FBK: 3D Double Side Pixels on 6” wafer
Ready by Dec 2014
Sensor will be used for PPS project (Torino)
BB planned together with planar batch
CMS Single chip (24x)
(1E, 2E, 3E, 4E)
CMS Quads (6x)
(2E, 3E)
MEDIPIX2 (4x)
NA62 test chip (20x)
ATLAS
FE-I4
(13x)
From G.F. Dalla Betta, M. Boscardin
Double-sided process
Passing through ohmic columns
Partially-through junction columns
Columns diameters about 10mm
Temporary metal for electrical characterization before bump-bonding
275 mm wafer thickness

## Slide 21: Thin Si-3D : DRIE test
Test on DRIE: recipe optimization
  Nominal Hole diameter 5micron
  On wafer hole diameter = 5.3 micron on top and on botton of hole
Depth 117 micron
Good uniformity of depth on wafer diameter
M. Boscardin
117 m
Tests ongoing
Results needed before starting 3D single side production
(S. Ronchin, FBK)

## Slide 22: ROC Wafers and Chips
We joined the first Phase-1 PSIdig common order:
  Two wafers from the first delivery of 48 ROCs (expected in November)
  Three next year
  These 5 wafers will be used for both pixel R&D and PPS project
We have also ordered 2 FE-I4 wafers, no time estimates yet
FNAL 100x30 chip
  How many can we get?
  Bump Bonding: where to do it? Join efforts? What about cost?
PSI ROC4sens chip 50x50 um
  any news?
  BB as above
RD53 small prototype: we need the bump pad floor-plan by end of year

## Slide 23: Planar Active Edge Batch
The AE batch will follow the same philosophy of 3D for pitch and layout
Most of the wafer area will be available for CMS (at present ATLAS-Italy is not interested in planar AE, maybe some interest from foreign Institutes)
It is a good opportunity to submit common CMS designs
We are open to collaborators

## Slide 24: Conclusions
Planar batch is close to completion at FBK, wafer test should be available by beginning of December
3D Double Side batch is expected to be complete before end of year (or even sooner)
We are establishing plans for test and Bump Bonding
3D Single Side and Active Edge Batches are in the layout design stage
There is a lot of wafer area in 3D and especially in AE batch: why not start a collaboration?
INFN is participating in the transanational proposal AIDA-2020
  WP7: Advanced hybrid pixel detectors
    Detector validation for tracking devices

## Slide 25: BACKUP
colonne, in generale
piani 3d ae tempi lunghi
disegni con e senza pstop
GR con e senza pstop
we’re planning BB and BCB

## Slide 26: Altre Attività Specifiche 2015
Nel 2015 si prevede:
  BB del batch 3D parzialmente in comune con ATLAS
  BB Batch Active Edge solo CMS
  Partner industriale BB secondo convenienza (IZM, Selex)
  Assemblaggi moduli planari, 3D, Active Edge
  Test Beam
  Primi irraggiamenti planari
  DAQ laboratorio con Digital Test Board CMS e con USBpix3 ATLAS

## Slide 27: Open P_Stop Sensor

## Slide 28: Open P_Stop Sensor
Pixel with opening in the P_Stop enclosure
No Punch Through implant structure