## Slide 1: Moire’ patterns in graphene
Annalisa Fasolino
Institute for Molecules and Materials
Radboud University Nijmegen, The Netherlands

## Slide 2: Moire’ patterns in graphene
graphene and van der Waals heterostructures
rotations and lattice mismatch → moire` patterns
rotations: graphene on graphene
mismatch: graphene on h-BN
effects on electronic structure
With thanks to
Merel van Wijk, Annelot Schuring
Guus Slotman, Shenjun Yuan, Misha Katsnelson
Annalisa Fasolino
Institute for Molecules and Materials
Radboud University, Nijmegen, The Netherlands

## Slide 3: graphene: till 2004 the missing structure
Graphite
Diamond
Graphene
3D
Curl, Kroto, Smalley 1985
Nobel prize 1996
Fullerenes
Carbon
Nanotubes
Multi-wall 1991
Single-wall 1993
0D
1D
2D
Novoselov et al., 2004
Nobel prize 2010

## Slide 4: graphene: why so special
Many superlatives
transparent and light conductor
- large out of plane fluctuations:
stable at finite temperature
due to anharmonic effects,
thermal ripples
scaling behaviour of elastic properties
Science, 2008

## Slide 5: graphene on h-BN
- ripples are a source of scattering
- hexagonal Boron Nitride (h-BN) keeps graphene flat
and improves mobility
- insulator, small lattice mismatch (1.8 %)

## Slide 6
Silicene
and many more 2D crystals
up to now mostly produced by exfoliation, more reactive, semiconductors, very active field of research
….. and many more

## Slide 7: van der Waals heterostructures
A. K. Geim,I. V. Grigorieva, Nature 4 9 9 , 4 1 9 (2013)
new structures
lots of new effects
weak (van der Waals) interlayer interactions create tunable periodic modulation
modulation: (in)commensurability on demand

## Slide 8: moire’ patterns
graphene on substrates with different orientation or lattice constant
leads to beautiful moiré patterns with large periodicity
30 nm
many STM observations

## Slide 9: moire` silk
silk, used in traditional clothes
in the Netherlands
as status symbol

## Slide 10: moire’ patterns: geometric constructions
30 nm

## Slide 11: moire’ patterns: graphene on graphite
Size determined by relative angle
M.M. van Wijk et al., 2D Mater. 2, 034010 (2015) (arxiv:150.02540)
apparent periodicity
≠
true one:
difficult determination
of angle from exp.
two different
moirons in one cell

## Slide 12: lattice relaxations minimize energy
Kolmogorov-Crespi
Brenner
competing interactions
numerical energy minimization by accurate potentials for carbon (Lammps)

## Slide 13: lattice relaxation: graphene on graphite substrate
displacements reduce area with unfavourable AA stacking

## Slide 14: moire’ patterns: graphene on graphite
Size determined by relative angle
Structure due to atomic displacements
to minimize energy

## Slide 15: out of plane displacements z
modulation sinusoidal → localized between flat domains
colour
gives z
y
x

## Slide 16: out of plane displacements z
modulation sinusoidal → localized between flat domains
colour
gives z
y
x
zav
zmin
zmax
M.M. van Wijk et al., 2D Mater. 2, 034010 (2015) (arxiv:150.02540)

## Slide 17: out of plane displacements z
modulation sinusoidal → localized between flat domains
colour
gives z
y
x
zav
zmin
zmax
M.M. van Wijk et al., 2D Mater. 2, 034010 (2015) (arxiv:150.02540)
extrapolation to θ=0 fails

## Slide 18: graphene on hexagonal Boron Nitride (h-BN)
h-BN
- insulator,
- 1.8 % larger lattice
parameter
graphene
C-BN interactions unknown
moire` patterns may reveal interlayer interactions
(weak van der Waals interactions difficult to measure and to calculate)

## Slide 19: experiment: graphene on h-BN

## Slide 20: exp: graphene on h-BN, comm-incomm transition
~0°/ 14 nm
~1.5°/ 8 nm
Woods et al., Commensurate incommensurate transition in graphene on hexagonal boron nitride, Nature Physics 10, 451 (2014)
0.98
1.0
center
stretched
Notes: Relative bond lengths. Competing energy terms.

## Slide 21: constructing a graphene-hBN supercell
rigid substrate
mobile graphene
interaction potential is unknown:
begin by modeling model h-BN as stretched graphene
0°: 13322 atoms
38°: 86254 atoms
lattice mismatch 56 x 56 on 55 x 55 1.8 %
+ angle

## Slide 22: different displacement distributions
Small angle / large moiré pattern
Large angle / small moiré pattern
100 Å
100 Å
1.4 Å
1.4 Å
1.395 Å
1.395 Å
0°
38°
eq.
(exp 1.42 Å)

## Slide 23: not quite as in experiment
Small angle / large moiré pattern
100 Å
1.4 Å
1.395 Å
center
stretched
center
compressed
0°
eq.
(exp 1.42 Å)
0.98
1.0

## Slide 24: C-B interaction from =CN interaction to zero
Θ=0º
C-B interactions < ½ C-N interactions needed for experimental results

## Slide 25: moire` as magnifying glass

## Slide 26: moire magnifies interlayer interactions
M. M. van Wijk, A. Schuring, M. I. Katsnelson, and A. Fasolino Phys. Rev. Lett. 113, 135504 (2014)
C-B interaction from =CN interaction to zero

## Slide 27: effect of moire` patterns on electronic structure
lattice mismatch → large supercells
relax structures with atomistic
simulations using empirical potentials
obtain tight-binding parameters
using the relaxed structure
perform calculations of electronic
properties using the tight-binding
propagation method
S. Yuan et al. Phys. Rev. B, 82, 115448 (2010)

## Slide 28: tight binding parameters

## Slide 29: density of states (DOS)
relaxation lead to additional Dirac points, depending of the rotation angle Θ
depth of minima can be tuned
by including the local gap term ΔU = <|Δvi|>,
which changes the on-site potential drastically
G. Slotman et al. arXiv:1507.03146 (2015).

## Slide 30: magnetic field: Landau levels
2D Landau levels
pristine graphene
2D Landau levels
graphene-hBN
due to moire’
G. Slotman et al. arXiv:1507.03146 (2015).

## Slide 31: Moire’ patterns in graphene
graphene and van der Waals heterostructures
rotations and lattice mismatch → moire’ pattern
rotations: graphene on graphene
mismatch: graphene on h-BN
effects on electronic structure
With thanks to
Merel van Wijk, Annelot Schuring
Guus Slotman, Shenjun Yuan, Misha Katsnelson
Annalisa Fasolino
Institute for Molecules and Materials
Radboud University Nijmegen, The Netherlands

## Slide 32: out of plane displacements z
z-displacement along diagonal
sinusoidal
localized between
flat domains

## Slide 33: Atomistic vs DFT
AB stacking
AA stacking
K. Uchida et al. PRB 90, 155451 (2014)
M.M. van Wijk et al., 2D Mater. 2, 034010 (2015) (arxiv:150.02540)

## Slide 34: graphene is extremely stiff
Graphene piece, micron long attached on one side does not collapse nor scroll

## Slide 35: stacking energy
regions of most favourable stacking adapt to h-BN lattice parameter

## Slide 36: scale down CB interactions
Sachs et al, PRB 84, 195414 (2011)

## Slide 37: magnetic field: Landau levels
2D Landau level

## Slide 38: magnetic field: Landau levels
2D Landau levels
pristine graphene