## Slide 1
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
TES as NIR Photon Number Resolving Detector (PNRD)
Silvia Giomi
Istituto Nazionale di Ricerca Metrologica (INRiM)

## Slide 2
What is a Transition-Edge Sensor (TES)?
TES is a device made by a superconducting film operated in the temperature region between the normal and the superconducting state
Active area
10 µm x 10 µm
Active area
5 µm x 5 µm
Active area
2 µm x 2 µm
Active area
1 µm x 1 µm
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
1/15

## Slide 3
TES is a device made by a superconducting film operated in the temperature region between the normal and the superconducting state
How does TES work?
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
Ti TES 1 µm x 1 µm
Rtes
T (mK)
(mΩ)
RN
Tc : Critical Temperature
RN: Normal Resistance
2/15
RN /2
Tc
Ti/Au 10 µm x 10 µm

## Slide 4
How does TES work?
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
(mΩ)
Rtes
T (mK)
Voltage bias
Ibias
Ites
Rsh
Rtes
Rp
Lin
Vout
DC-SQUID sensor
Lout
Rout
3/15

## Slide 5
How does TES work?
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
Ibias
Ites
Rsh
Rtes
Rp
Lin
Vout
Lout
Rout
(µA)
(µA)
Ites
Ibias
Rtes
T (mK)
(mΩ)
4/15

## Slide 6
How does TES work?
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
Rtes
Working Point
(mΩ)
(µA)
(µA)
Ites
Ibias
Working Point
5/15
T (mK)

## Slide 7
t (µs)
T (mK)
Rtes
How does TES work?
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
6/15
(mΩ)
Ites (µA)

## Slide 8
Energy Resolution
How well TESs count photons?
Working at higher Tc
shorter Response Time
Smaller size TESs
higher Energy Resolution
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
7/15
Effective Response Time

## Slide 9
Experimental set-up
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
Active area
10 µm x 10 µm
Active area
20 µm x 20 µm
Optical Fiber
8/15

## Slide 10
Experimental set-up
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
0 photons
1 photon
2 photons
3 photons
9/15

## Slide 11
How well TESs count photons?
Ti/Au TES 10 µm x 10 µm
eff = 4 µs
ΔEFWHM= 0.113 eV
@1570 nm
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
Tc~ 106 mK
10/15
L.Lolli et al arXiv:1306.5385v1 [physics.ins-det], June 2013

## Slide 12
How well TESs count photons?
Ti/Au TES 10 µm x 10 µm
eff = 186 ns
ΔEFWHM= 0.263 eV @1535 nm
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
Tc~ 300 mK
11/15
L.Lolli et al IEEE Trans.Appl.Supercond., vol.23, n.3, June 2013

## Slide 13
How well TESs count photons?
eff = 168 ns
ΔEFWHM= 0.19 eV @1545 nm
Ti TES 2 µm x 2 µm
Tc~ 470 mK
12/15
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
C.Portesi et al IEEE Trans.Appl.Supercond., vol.25, n.3, June 2015

## Slide 14
How well TESs count photons?
eff = 147 ns
ΔEFWHM= 0.12 eV @1545 nm
Ti TES 1 µm x 1 µm
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
Tc~ 470 mK
13/15
C.Portesi et al IEEE Trans.Appl.Supercond., vol.25, n.3, June 2015

## Slide 15
Future with photons
14/15
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma

## Slide 16
Which applications are TESs useful for?
Quantum metrology
Quantum optics
Quantum imaging
Quantum mechanics
Quantum information
Material analysis
Astronomy
Characterization of single photon source NV centers in nano-diamond from PTB
W. Schmunk et al, METROLOGIA (2012) 49, 56-160
Validation of first experimental tomography of
the positive operator-valued measure (POVM)
G. Brida et al, New J. Phys. (2013) 14 085001
Characterization of single photon source in Quantum Optics Group
L. LOLLI et al, Int. J. Quantum Inform. (2011) 09, 405
Validation of innovative absolute calibration technique
A. Avella et al, Optics Express (2011) 19, 23249-23257
@INRiM
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
15/15

## Slide 17
S.Giomi - CI Congresso Nazionale SIF, 21-25/09/2015, Roma
Thanks for your attention