## Slide 1
L. Del Bianco, E. Bonfiglioli, F. Chinni, M. Tamisari, F. Spizzo
Dipartimento di Fisica e Scienze della Terra,
Università di Ferrara, Italy
lucia.delbianco@unife.it
Re-entrant antiferromagnetism in the exchange-coupled IrMn/NiFe system

## Slide 2
Objective
Description of the dynamic magnetic behavior of the antiferromagnet in exchange-coupled FM/ AFM NiFe/IrMn bilayers
From the continuous NiFe/IrMn film to dot arrays: spatial confinement and exchange coupling mechanism
Re-entrant antiferromagnetism
We exploit the exchange coupling with a soft FM as a tool to gain an insight into the magnetic properties of the AFM
We study the magnetic properties of the AFM phase to gain an insight into the exchange coupling mechanism
(exchange bias effect)

## Slide 3
Si / Cu[5 nm] / Py[5 nm] / IrMn[6 nm] / Cu [5 nm]
Deposition by dc-magnetron sputtering
Ar atmosphere, deposition rate  0.2 nm/s
Hdep = 400 Oe
Py: Ni80Fe20 IrMn: Ir25Mn75
NiFe/IrMn film
Reference film: Si / Cu[5 nm] / Py[5 nm] / Cu [5 nm]

## Slide 4
Hysteresis loops
(5-400 K temperature range)
Change of magnetic regime at T ~ 100 K

## Slide 5
5 K
400 K
step 1: FC@ Hcool =500 Oe
step 2: M vs T @ Hinv
Magnetization reversal study -
SQUID measurement procedure

## Slide 6
Py
Measurement on reference Py film in H = 50 Oe
Pronounced magnetization decrease in the bilayer is ascribed to the reduction of the exchange magnetic anisotropy in the Py layer

## Slide 7
Py
AFM film consists of non-interacting nanograins

Distribution of effective anisotropy energy barriers DE
We obtain information on the anisotropy energy barrier distribution of the AFM as it is felt by the FM component
F. Spizzo et al., J. Phys.: Condens. Matter 25, 386001 (2013)

## Slide 8
Py
IrMn
bulk AFM nanograins
spin-glass-like
behavior
V = 25 kTB/KIrMn
 size ~ 10 nm
KIrMn = 1.8  106 erg/cm3
Notes: grani: magnetically uncorrelated

## Slide 9
(a)
Cu
IrMn
NiFe
10 nm
Si
(a)
(b)
Si
Cu
Existence of a disordered AFM region at the interface with the NiFe phase
TEM results confirm our prediction on the structure of the AFM phase

## Slide 10
Hex decreses and finally the EB effect disappears
T< 100 K
AFM interfacial spins are frozen and subjected to a high effective anisotropy.
Hex is maximized
Only the interfacial AFM spins tightly anchored to the spin lattice of the bulk AFM nanograins contribute to Hex
T
T > 100 K
No chance to observe EB effect at the temperature above which the AFM bulk nanograins enter the superparamagnetic regime
T ~ 100 K
The frozen collective state breaks up.
Polarizing action of bulk AFM spins on the interfacial ones prevents the development of a paramagnetic state.
Re-entrant antiferromagnetism

## Slide 11
Si / Cu[5 nm] / IrMn[10 nm] / Py [5 nm]
Electron beam lithography and lift-off
dc-magnetron sputtering
(Hdep = 400 Oe)
From the continuous film to dot arrays
FM
AFM
FM
AFM
spatial confinement

## Slide 12
A = 1000 nm
B = 500 nm
C = 300 nm
MOKE - FC hysteresis loops
(Hcool = 500 Oe;
10-300 K temperature range)
(Oe)
(Oe)

## Slide 13
At low temperature
The correlation length among the AFM interfacial spins increases with reducing T
(Oe)

## Slide 14
Object Oriented MicroMagnetic Framework
FM
AFM
F. Spizzo et al., Phys. Rev. B 91 (2015) 064410
Dot size = 1200 nm
OOMMF cell size = 10 nm
KAFM = 2  107 erg/cm3 cells:
FM/AFM exchange interaction = 10-7 erg/cm
Different cell size:
10, 20, 100, 200, 300 nm
l
Dependence of Hex on the
AFM correlation length l

## Slide 15
Object Oriented MicroMagnetic Framework
Dependence of Hex on the
AFM correlation length l
Dot size = 1200 nm
All the AFM cells with
high K (100% pinning centers)
Different cell size:
10, 20, 100, 200, 300 nm
(Oe)
Hex increases as
D/l 1

## Slide 16
At low temperature
Correlated AFM spins exert a stronger pinning action as
D/l 1
(Oe)
Spin correlation effect

## Slide 17
Conclusions
Re-entrant antiferromagnetism  Passage from the glassy to the AFM state
Re-entrant magnetic regime: the magnetism of AFM interfacial spins is sustained by stable nanograins.
Exchange coupling mechanism
Low temperature: collective freezing of the disordered AFM spins  high Hex.
High temperature: FM/AFM coupling governed by a fraction of interfacial AFM spins.
Spatial confinement  spin correlation effect
MIUR FIRB2010 - NANOREST
A. Gerardino, A. Notargiacomo
IFN-CNR, I-00156 Roma, Italy
G. Barucca
Univ. Politecnica delle Marche,
I-60131 Ancona, Italy
Thanks for attention