## Slide 1: Ledge-type Co/L10-FePt exchange-coupled composites
G. Varvaroa, A. M. Testaa, E. Agostinellia, S. Lauretia, V. Nappia, D. Peddisa, G. Baruccab, Th. Speliotisc, G. Giannopoulosc, D. Niarchosc, W.F. Lid, G. Hadjipanayisd and D. Fiorania
a ISM-CNR, Area della Ricerca RM1, Via Salaria Km 29,300, P.B. 10-00015, Monterotondo Scalo, Roma, Italy
b SIMAU, Università Politecnica delle Marche, via Brecce Bianche, Ancona, Italy
c Institute of Materials Science, NCSR Demokritos, Athens, Greece
d Department of Physics, University of Delaware, Newark, DE 19716, USA

## Slide 2: INTRODUCTION
EXCHANGE COUPLED COMPOSITE (ECC) SYSTEMS: FUNDAMENTALS and APPLICATIONS
FM HARD
FM SOFT
ECC systems consist of ferromagnetic (FM) hard and soft phases exchange coupled through their common interface.
Varying the intrinsic and extrinsic properties of the two components and the strength of the interface coupling is possible to finely tune the magnetic properties of the composite.

## Slide 3: INTRODUCTION
Magnetic Recording Media
D. Goll and T Bublat, Phys. Status Solidi A 210 1261 2013
ECC media allows improving the writability without compromising the thermal stability.
ECC media are used in current recording media based on the CoCrPt alloy and are envisaged for next generation PMR media (areal density > 1 Tbit/in2) based on hard materials (e.g. L10-FePtX alloys, ku ~ 5 MJ/m3).
Permanent Magnets
Spin Torque Oscillators
Enhancement of (BH)max (up to 900 kJ/m3 for an ideal NdFeB/Fe bilayer).
Reduction of rear-earth elements by hard phase dilution.
Varying the thickness of the soft layer allows modulating the tilt angle.
→ fine tuning of magneto-dynamic properties.
T.N Nguyen et al., APL 98 172502 2011
L. Lewis et al., Met. Mat. Trans. A 44 S2 2013
B. Balamurugan et at., Scrip. Mat. 67 542 2012
J. Winterlik et al., Adv Mater. 24 6283 2012
O. Gutfleisch et al., Adv. Mat. 23 821 2011
EXCHANGE COUPLED COMPOSITE (ECC) SYSTEMS: FUNDAMENTALS and APPLICATIONS

## Slide 4: INTRODUCTION
Magnetic Recording Media
D. Goll and T Bublat, Phys. Status Solidi A 210 1261 2013
ECC media allows improving the writability without compromising the thermal stability.
ECC media are used in current recording media based on the CoCrPt alloy and are envisaged for next generation PMR media (areal density > 1 Tbit/in2) based on hard materials (e.g. L10-FePtX alloys, ku ~ 5 MJ/m3).
Permanent Magnets
Spin Torque Oscillators
Enhancement of (BH)max (up to 900 kJ/m3 for an ideal NdFeB/Fe bilayer).
Reduction of rear-earth elements by hard phase dilution.
Varying the thickness of the soft layer allows modulating the tilt angle.
→ fine tuning of magneto-dynamic properties.
T.N Nguyen et al., APL 98 172502 2011
L. Lewis et al., Met. Mat. Trans. A 44 S2 2013
B. Balamurugan et at., Scrip. Mat. 67 542 2012
J. Winterlik et al., Adv Mater. 24 6283 2012
O. Gutfleisch et al., Adv. Mat. 23 821 2011
EXCHANGE COUPLED COMPOSITE (ECC) SYSTEMS: FUNDAMENTALS and APPLICATIONS

## Slide 5: INTRODUCTION
EXCHANGE COUPLED COMPOSITE SYSTEMS for MAGNETIC RECORDING
Type of interface
Sharp interface.
A non magnetic layer can be present to modulate the interface coupling.
The interface is an extend region where the anisotropy gradually varies from high to low values along the thickness.
Different ECC designs have been proposed, the difference being in the type of interface and section shape of soft and hard components.
Section shape
Conventional ECC systems
Ledge-type ECC system
F. Casoli et al., Ch. 5 in “Ultra-High-Density Magnetic Recording: Storage Materials and Media Designs”, G. Varvaro and F. Casoli Eds., Pan Stanford Publishing (In preparation - 2015)
G. Varvaro et al., JMMM 368 415 2014
D. Goll and T. Bublat, Phys. Status Solidi A 210 1261 2013; D. Goll and S. Macke, APL 93 152512 2008
D. Suess et al., JMMM 321 545 2009; A. Y Dobin et al., APL 89 062512 2006
Exchange-Spring systems
The cross sectional shape is identical for the hard and soft phases
Z
K
Kh
Ks
Hard FM
Non magnetic interlayer
Soft FM
K
Kh
Ks
z
tG
Hard FM
Soft FM
Single-element structures
Nano-patterned geometries
Hard
Soft
Graded systems
Single-element structures
Nano-patterned geometries
The section size of the soft phase is more extended.

## Slide 6: INTRODUCTION
Type of interface
Sharp interface.
A non magnetic layer can be present to modulate the interface coupling.
The interface is an extend region where the anisotropy gradually varies from high to low values along the thickness.
Section shape
Conventional ECC systems
Ledge-type ECC system
Exchange-Spring systems
The cross sectional shape is identical for the hard and soft phases
Z
K
Kh
Ks
Hard FM
Non magnetic interlayer
Soft FM
K
Kh
Ks
z
tG
Hard FM
Soft FM
Single-element structures
Nano-patterned geometries
Hard
Soft
EXCHANGE COUPLED COMPOSITE SYSTEMS for MAGNETIC RECORDING
Graded systems
Single-element structures
Nano-patterned geometries
The section size of the soft phase is more extended.
Different ECC designs have been proposed, the difference being in the type of interface and section shape of soft and hard components.
F. Casoli et al., Ch. 5 in “Ultra-High-Density Magnetic Recording: Storage Materials and Media Designs”, G. Varvaro and F. Casoli Eds., Pan Stanford Publishing (In preparation - 2015)
G. Varvaro et al., JMMM 368 415 2014
D. Goll and T. Bublat, Phys. Status Solidi A 210 1261 2013; D. Goll and S. Macke, APL 93 152512 2008
D. Suess et al., JMMM 321 545 2009; A. Y Dobin et al., APL 89 062512 2006

## Slide 7: Aim
Deposition | Sputtering
Structural & Microstructural Investigation | XRD - SAED
 | TEM/HRTEM
Magnetic Measurements | Vector VSM
 | SQUID
L10-FePt
Co
MgO (100) Substrate
Investigation of structural, microstructural and magnetic properties of Co(soft)/L10-FePt(hard) ledge-type ECC systems as a function of Co thickness.
Previous works focused on FePt-based ledge type ECC systems where Fe is used as soft component
D. Goll and T. Bublat, PSS A 210 1261 2013
L.S. Huang et al., JAP 114 173903 2013
B. Ma et. al., JAP 109 083907 2011
B. Ma et al., IEEE Trans. Magn. 46 2345 2010
A. Breitling et al., PSS-RRL 3 130–132 2009
D. Goll and A. Breitling, APL 94 052502 2009
F. Casoli et al., APL 92 142506 2008
D. Goll and S. Macke, APL 93 152512 2008
Co soft phase was already successfully used in different conventional ECC systems:
SmCo/Co (E.E. Fullerton et al., PRB 12193 1998; P. Chowdhury et al., JMMM 342 74 2013)
L10-CoPt/Co (D.C. Crew et al., JMMM 233 257 2001)
L10-FePt/Co (Wang et al., JAP 115 133908 2014)
Using Co allows in principle the magnetization reversal in the two phases to be carefully investigated by using elemental specific measurement techniques.

## Slide 8: Experimental
Co/L10-FePt ledge–type samples were prepared by sputtering (@ NCSR Demokritos, Athens - Greece)
L10-FePt
Co
MgO (100) Substrate

## Slide 9: Experimental
L10-FePt
MgO (100) Substrate
D. Goll and T Bublat, Phys. Status Solidi A 210 1261 2013
SEM
easy
axis
1
T. Shima et al., APL 81 1050 2002
V. Alexandrakis et al., JAP 109 07B729 2011
Tdep = 700 °C
Nominal thickness = 3.5 nm
MgO (100) substrate
HARD FePt phase with an island-type nanostructure (Volmer-Weber growth mode) consisting of isolated (001) L10-FePt particles (ku ~ 5 MJ/m3) with perpendicular anisotropy.
Co/L10-FePt ledge–type samples were prepared by sputtering (@ NCSR Demokritos, Athens - Greece)

## Slide 10: Experimental
L10-FePt
MgO (100) Substrate
1
HARD FePt phase with an island-type nanostructure (Volmer-Weber growth mode) consisting of isolated (001) L10-FePt particles (ku ~ 5 MJ/m3) with perpendicular anisotropy.
Co/L10-FePt ledge–type samples were prepared by sputtering (@ NCSR Demokritos, Athens - Greece)
Tdep = RT
Nominal thickness (thCo)
3, 6.5, 9.5, 20 nm
SOFT Co phase
2
T. Shima et al., APL 81 1050 2002
V. Alexandrakis et al., JAP 109 07B729 2011
Tdep = 700 °C
Nominal thickness = 3.5 nm
MgO (100) substrate

## Slide 11: Morpho-Structural Properties
X-RAY ANALYSIS
(@ NCSR Demokritos, Athens - Greece)
thCo = 0
thCo = 3 nm
thCo = 6.5 nm
thCo = 9.5 nm
thCo = 20 nm
A magnetically hard L10-FePt phase (fct) with a (001) orientation (i.e. the easy axis oriented perpendicular to film surface) was obtained.
The presence of the (003) superlattice reflection is a remarkable sign of a high chemical order degree.
Any reflection peaks related to the Co phase was observed even at the largest soft layer thickness
Fe
[001]
easy-axis
Pt

## Slide 12: Morpho-Structural Properties
L10-FePt
Co
20 nm
20 nm
20 nm
L10-FePt
Co
Co
tCo = 3 nm
tCo = 9.5 nm
tCo = 20 nm
TEM ANALYSIS
(@ SIMAU, Ancona – Italy; Un. Delaware – DE, USA)
MgO (100) Substrate
MgO (100) Substrate
MgO (100) Substrate
The HARD FePt phase forms with an island-type nanostructure (Volmer-Weber growth mode) consisting of isolated L10-FePt particles.
Island lateral size: 25 – 35 nm
Island height: ~ 10 nm
Spacing: 5 – 10 nm
thCo < FePt island height (~ 10 nm)
Half-filled ledge-type structure.
thCo > FePt island height (~ 10 nm)
Filled ledge-type structure.
L10-FePt

## Slide 13: Morpho-Structural Properties
L10-FePt
Co
5 nm
20 nm
5 nm
L10-FePt
Co
L10-FePt
Co
L10-FePt
Co
TEM ANALYSIS
(@ SIMAU, Ancona – Italy; Un. Delaware – DE, USA)
Co [001]
MgO [001]
L10-FePt [001]
4°
[100]
[001]
HRTEM
L10-FePt
Co
L10-FePt
Co
MgO (100) Substrate
MgO (100) Substrate
MgO (100) Substrate
The formation of L10-FePt particles with a (001) orientation is confirmed.
The presence of a Co fcc phase with a (001) orientation was observed.
<100>Co // <100>FePt ;
{001}Co // {001}FePt
{001}FePt // {001}MgO ;
<010>FePt // <010>MgO
tCo = 3 nm
tCo = 9.5 nm
tCo = 20 nm
SAED

## Slide 14: Magnetic Properties
HYSTERESIS LOOPS (f = 90°)
H
Sample plane
f
x
z
(@ ISM – CNR, Roma - Italy)
Hc ~ 4.5 T

## Slide 15: Magnetic Properties
HYSTERESIS LOOPS (f = 90°) – Dependence of Hc,┴ on the Co thickness (thCo)
(@ ISM – CNR, Roma - Italy)

## Slide 16: Magnetic Properties
HYSTERESIS LOOPS (f = 90°) – Dependence of Hc,┴ on the Co thickness (thCo)
Improved Writability
(@ ISM – CNR, Roma - Italy)

## Slide 17: Magnetic Properties
HYSTERESIS LOOPS (f = 90°) – Dependence of Hc,┴ on the Co thickness (thCo)
Improved Writability
(@ ISM – CNR, Roma - Italy)
Half-filled ledge type structure
Perpendicular anisotropy
Significant reduction of Hc

## Slide 18: Magnetic Properties
RECOIL CURVES (f = 90°) – REVERSAL MECHANISM
(@ ISM – CNR, Roma - Italy)
D. Goll and S. Macke, APL 93 152512 2008
Reversal mechanism
Domain wall-assisted switching model
D. Suess et al., JMMM 321 545 2009
A.Yu. Dobin and H.J. Richterb, APL 89 062512 2006
Nucleation of a domain wall in the soft phase. It becomes pinned near the soft/hard interface where it compresses (reversible reversal)
Displacement of the domain wall into the hard part. Reversal of the whole system (irreversible switching).
Reversible
reversal
Irreversible
Reversal
Numerical simulation
Recoil loops were measured by removing and reapplying a demagnetizing (reverse) field (Hrev), which is successively increased.

## Slide 19: Magnetic Properties
RECOIL CURVES (f = 90°) – REVERSAL MECHANISM
Irreversible processes appear due to the reversal of the hard phase
Reversible
reversal
D. Goll and S. Macke, APL 93 152512 2008
Reversal mechanism
Domain wall-assisted switching model
D. Suess et al., JMMM 321 545 2009
A.Yu. Dobin and H.J. Richterb, APL 89 062512 2006
Nucleation of a domain wall in the soft phase. It becomes pinned near the soft/hard interface where it compresses (reversible reversal)
Displacement of the domain wall into the hard part. Reversal of the whole system (irreversible switching).
Reversible
reversal
Irreversible
Reversal
Numerical simulation
(@ ISM – CNR, Roma - Italy)

## Slide 20: Magnetic Properties
RECOIL CURVES (f = 90°) – REVERSAL MECHANISM
Irreversible processes appear due to the reversal of the hard phase
Reversible
reversal
The system behaves as an exchange-coupled composite
D. Goll and S. Macke, APL 93 152512 2008
Reversal mechanism
Domain wall-assisted switching model
D. Suess et al., JMMM 321 545 2009
A.Yu. Dobin and H.J. Richterb, APL 89 062512 2006
Nucleation of a domain wall in the soft phase. It becomes pinned near the soft/hard interface where it compresses (reversible reversal)
Displacement of the domain wall into the hard part. Reversal of the whole system (irreversible switching).
Reversible
reversal
Irreversible
Reversal
Numerical simulation
(@ ISM – CNR, Roma - Italy)

## Slide 21: Conclusions
4°
[100]
[001]
<100>Co // <100>FePt ;
{001}Co // {001}FePt
{001}FePt // {001}MgO ;
<010>FePt // <010>MgO
Co(fcc)/FePt(fct) ledge-type systems were prepared and investigated.
The crystallographic relationship among the different phases was disclosed.
The systems present a preferential perpendicular anisotropy up to thCo = 9.5 nm
Hc reduces with the increase of thCo.
The exchange coupled composite behaviour was demonstrated.
Reversible
reversal
Irreversible processes appear
Improved Writability

## Slide 22
THANK YOU FOR THE ATTENTION

## Slide 23
The book reports on the most recent progresses and developments in data storage from the recording medium perspective. Theoretical, experimental as well as technological aspects are presented, with special emphasis on the materials’ features for next generation perpendicular recording media. The book also reports on emerging magnetic memories, which are potential candidates for future information storage devices.
Chapter 1. Fundamentals of Magnetism
P. Allia, G. Barrera
Chapter 2. Hard Disk Drives: Fundamentals and Perspectives
G. Bertero, G. Guo, S. Dahandeh, A. Krishman
Chapter 3. Conventional Perpendicular Magnetic Recording Media
H.-S. Jung
Chapter 4. Energy Assisted Magnetic Recording
E. Gage, K.-Z. Gao, J.-G. Zhu
Chapter 5. L10-FePt Granular Films for Heat Assisted Magnetic Recording Media
K. Hono, Y.K. Takahashi
Chapter 6. Exchange-Coupled Composite Media
F. Casoli, L. Nasi, F. Albertini, P. Lupo
Chapter 7. Bit Patterned Magnetic Recording
D. Makarov, P. Krone, M. Albrecht
Chapter 8. Magnetic Characterization of Perpendicular Recording Media
G. Varvaro, A.M. Testa, E. Agostinelli, D. Peddis, S. Laureti
Chapter 9. New Trends in Magnetic Memories
R. Bertacco, M. Cantoni
Notes: Upcoming relaese

## Slide 24
Additional Information

## Slide 25: Exchange Coupled Composite Media
Ledge-Type Systems
Nano-patterned geometries
Nano-patterned geometries
Single-element structures
D. Goll and S. Macke, APL 93 152512 2008
TYPE | 
Single elements | 
Cube | 1.57
Mushroom | 1.71
Gamma | 1.45
Capped | 1.18
Nanopatterns | 
Half-filled | 1.23
Filled | 1
Capped | 1
GAIN FACTOR (ξ)
ξ =1 Single S-W Hard Phase
ξ >1 Exchange Coupled System

## Slide 26: Magnetic Properties
ANGULAR REMANENCE CURVE (Mr/Ms vs. f)
medium-axis – [110]
hard-axis – [100]
easy-axis – [111]
Co
FCC (001)
easy-axis
L10-FePt
FCT (001)
[100]
[001]
[010]
(100) plane
f
(@ ISM – CNR, Roma - Italy)
thCo = 9.5 nm
The symmetry is essentially two folds
→ The system behaves as a uniaxial perpendicular media
Lobes of weaker intensity appear around 0° and 180°

## Slide 27: Magnetic Properties
ANGULAR REMANENCE CURVE (Mr/Ms vs. f)
Co
FCC (001)
easy-axis
L10-FePt
FCT (001)
[100]
[001]
[010]
(100) plane
f
Magneto crystalline anisotropy
L10-FePt (FCT): Uniaxial
Co (FCC): Cubic (k1 and K2 are both negative)*
Shape anisotropy
Interface exchange coupling
Angular Remanence Curve depends on
(@ ISM – CNR, Roma - Italy)
thCo = 9.5 nm
thCo = 20 nm
Six-folds symmetry
→ Multi-axial system
The symmetry is essentially two folds → The system behaves as a uniaxial perpendicular media.
Lobes of weaker intensity appear around 0°and 180°
*J.E. Fisher and J. Goddard, J. Phys. Soc. Jap. 25 143 1968
M. Getzlaff , “Magnetic Anisotropy Effects” in Fundamental of Magnetism, M. Getzlaff Ed., Springer, 2007
medium-axis – [110]
hard-axis – [100]
easy-axis – [111]

## Slide 28: Trend in digital data storage capacity
Volume of data has been increasing by 40% annually
Storage devises have been continuously improved in terms of capacity, performance, reliability and cost
Optical Disk Drives (ODDs)
PROS Reliability, Life-time, Cost, Transportability
CONS Reusability, Writing-time, Capacity
Hard Disk Drives (HDDs)
PROS Cost, Capacity, Availability
CONS Reliability, Write/Read speed
Solid State Drives (SSDs)
PROS Write/Read speed, Reliability
CONS Capacity, Life-time, Cost
Flash memory other that SSDs
PROS Transportability, Reliability
CONS Capacity, Life-time

## Slide 29: Hard Disk Drives
Current HDDs
Recording Density: ~ 700 Gb/in2
HDD sold in 2014: ~ 557 million
Cost/Gb: 0.03 $
Leading technology for massive digital data storage
"All that data stored in the cloud isn't on droplets of airborne water. It's stored on hard disk drives."

## Slide 30: Hard Disk Drives
Areal Density Evolution
Disk Medium
Head
Spindle Motor
Voice Coil
Motor
Encoder
&
Decoder
High-Ku materials,
EAMR, ECC, BPMR, STMR, TDMR
?
Longitudinal Recording
Perpendicular Recording
Current HDDs
Perpendicular technology
Recording Density: ~ 700 Gb/in2
HDD sold in 2014: ~ 557 million
Cost/Gb: 0.03 $
▲2011 DEMO
[Co/Pd]n BPM – 1T/in2
TERAMAGSTOR EU-Project

## Slide 31: Hard Disk Drives
Recording Medium
Substrate
Hard Ferromagnet
→ It can be permanently magnetized permitting information to be retained over time.
Magnetic Medium

## Slide 32: Hard Disk Drives
Recording Medium
Sputtering
Dip-coating
Diamond Like Carbon – DLC – & CNx
Provides chemical and mechanical protection
AlTi, CtTi, NiTa
Improve the adhesion of SUL
Improve corrosion robustness of the substrate
Co(Fe)TaZr-based
Helps in conducting the flux form the writing pole of the head and the connector pole
AlMg (Server & Desktop), Glass (Laptop)
Performs the role of support (hard, stiff, inert, smooth)
Ni-(X,Y)/Ru or Ru-(X,Y)/Ru (X, Y = Cr, Mn, W)
Exchange-decouples the SUL and the magnetic layer
Favours the epitaxial growth of the magnetic layer
PFPE
Reduces friction and wear during the head-disk contact
Substrate
Adhesion layer
Soft Underlayer (SUL)
Intermediate Layer
Overcoat
Lubricant
Recording layer
IBD, PE-CVD, Sputtering

## Slide 33: Hard Disk Drives
Recording Medium – Recording Layer
Recording layer
Sputtering
Dip-coating
Diamond Like Carbon – DLC – & CNx
Provides chemical and mechanical protection
AlTi, CtTi, NiTa
Improve the adhesion of SUL
Improve corrosion robustness of the substrate
Co(Fe)TaZr-based
Helps in conducting the flux form the writing pole of the head and the connector pole
AlMg (Server & Desktop), Glass (Laptop)
Performs the role of support (hard, stiff, inert, smooth)
Ni-(X,Y)/Ru or Ru-(X,Y)/Ru (X, Y = Cr, Mn, W)
Exchange-decouples the SUL and the magnetic layer
Favours the epitaxial growth of the magnetic layer
PFPE
Reduces friction and wear during the head-disk contact
Substrate
Adhesion layer
Soft Underlayer (SUL)
Intermediate Layer
Overcoat
Lubricant
IBD, PE-CVD, Sputtering

## Slide 34: Hard Disk Drives
Recording Medium – Magnetic Layer (1st Generation – 2005 –)
Granular Microstructure (d ~ 10 nm)
CoCrPt@SiO2
Ku = 0.2 – 0.5 106 J/m3
SiO2 : promotes grain isolation
Stoner-Wolfarth like system
Single domain grains
Weakly exchange coupled grains
Uniaxial perpendicular anisotropy Ku
Smooth surface (Ra roughness ~1 nm)
CoCrPt@SiO2
easy-axis
Core: Co-rich
(magnetic)
Boundary: SiO2
(non-magnetic)
Bit Pattern
d
DE0
Hard Disk Surface
Ground
NANOSLIDER
R/W
Head
20 – 40 m/s
~5 nm
~0.3 mm

## Slide 35: Hard Disk Drives
Recording Medium – Magnetic Layer (1st Generation – 2005 –)
Granular Microstructure (d ~ 10 nm)
Stoner-Wolfarth like system
Single domain grains
Weakly exchange coupled grains
Uniaxial perpendicular anisotropy Ku
Smooth surface (Ra roughness ~1 nm)
CoCrPt@SiO2
easy-axis
Core: Co-rich
(magnetic)
Boundary: SiO2
(non-magnetic)
Bit Pattern
d
H2
H1
H2 > H1
CoCrPt@SiO2
Ku = 0.2 – 0.5 106 J/m3
SiO2 : promotes grain isolation
Hard Disk Surface
Ground
NANOSLIDER
R/W
Head
20 – 40 m/s
~5 nm
~0.3 mm

## Slide 36: Hard Disk Drives
Evolution of Perpendicular Magnetic Recording Media
Single
CoCr(Pt,Ta,B) Layer
EXCHANGE COUPLED COMPOSITE MEDIA
Multilayer structures consisting of CoCrPt-Oxide magnetic layers (ML) with different anisotropy (K) separated by a non magnetic breack layer (BL, e.g. Pt)
Improved writability
Reduction of magnetic layer thickness
1st (2005)
7st (2013)
Generation
ML (K2)
ML (K1)
K1 > K2
K1 > K2 > K3
K1 > K2 > K3 > K4
ML (K1)
BL
ML (K3)
ML (K2)
ML (K1)
ML (K3)
ML (K2)
ML (K4)

## Slide 37: Hard Disk Drives
Evolution of Perpendicular Magnetic Recording Media
Substrate
Adhesion layer (5 nm)
SAF – SUL (50 nm)
Intermediate Layer (15 nm)
Overcoat (< 2 nm)
Lubricant (~ 1 nm)
Recording layer (15 nm)
Single
CoCr(Pt,Ta,B) Layer
EXCHANGE COUPLED COMPOSITE MEDIA
Multilayer structures consisting of CoCrPt-Oxide magnetic layers (ML) with different anisotropy (K) separated by a non magnetic breack layer (BL, e.g. Pt)
Improved writability
Reduction of magnetic layer thickness
1st (2005)
7st (2013)
Generation
ML (K2)
ML (K1)
K1 > K2
K1 > K2 > K3
K1 > K2 > K3 > K4
ML (K1)
BL
ML (K3)
ML (K2)
ML (K1)
ML (K3)
ML (K2)
ML (K4)
NANOSLIDER
R/W
Head
1.5 nm
Ra Rough. 3.5 Å

## Slide 38: Hard Disk Drives
Towards 1 Tbit/in2 and Beyond – Recording Trilemma
Number of grains per bit
Longitudinal Magnetic Recording (LMR) Media
The areal density has been increased by continuously reducing the in-plane size of the grain in order to maintain an adequate SNR.
Higher areal density require smaller grains (D)

## Slide 39: Hard Disk Drives
Towards 1 Tbit/in2 and Beyond – Recording Trilemma
Perpendicular Magnetic Recording (PMR) Media
The in-plane size of the grain has been kept almost constant and higher areal densities have been obtained reducing the number of grains per bit (up to 15 – 20) without compromising the SNR.

## Slide 40: Hard Disk Drives
Towards 1 Tbit/in2 and Beyond – Recording Trilemma
Perpendicular Magnetic Recording (PMR) Media
The in-plane size of the grain has been kept almost constant and higher areal densities have been obtained reducing the number of grains per bit (up to 15 – 20) without compromising the SNR.
To go in the Tbit regime the grain size must be reduced to maintain an adequate SNR.

## Slide 41: Hard Disk Drives
SNR
Higher areal density require smaller grains (D)
Towards 1 Tbit/in2 and Beyond – Recording Trilemma
Number of grains per bit
D

## Slide 42: Hard Disk Drives
SNR
Higher areal density require smaller grains (D)
Towards 1 Tbit/in2 and Beyond – Recording Trilemma
Number of grains per bit
D
DE0
Grain Volume
Uniaxial Anisotropy Constant
Stoner-Wolfarth system
STABILITY FACTOR
10 Years
THERMAL
STABILITY

## Slide 43: Hard Disk Drives
SNR
Higher areal density require smaller grains (D)
Towards 1 Tbit/in2 and Beyond – Recording Trilemma
Number of grains per bit
D
DE0
Grain Volume
Uniaxial Anisotropy Constant
Stoner-Wolfarth system
STABILITY FACTOR
10 Years
THERMAL
STABILITY
Recording Medium Material | Ku (106 J/m3)
SmCo5 | 10 – 20
L10 FePt | 7 – 10
L10 CoPt | ~ 5
Co/Pt(Pd) | ~1
CoCrPt | 0.2 – 0.5
Thermally stable at D = 3 nm

## Slide 44: Hard Disk Drives
SNR
Higher areal density require smaller grains (D)
Towards 1 Tbit/in2 and Beyond – Recording Trilemma
Number of grains per bit
D
DE0
Grain Volume
Uniaxial Anisotropy Constant
Stoner-Wolfarth system
STABILITY FACTOR
10 Years
THERMAL
STABILITY
Recording Medium Material | Ku (106 J/m3) | Write Head Material | Bs (T)
SmCo5 | 10 – 20 | Co35Fe65 | 2.4
L10 FePt | 7 – 10 → m0Hsw ~ 5-6 T | CoNiFe | 2.0
L10 CoPt | ~ 5 | Ni45Fe55 | 1.5
Co/Pt(Pd) | ~1 |  | 
CoCrPt | 0.2 – 0.5 |  | 
Writing Field
Switching Field
WRITABILITY