## Slide 1: Compensazione termica dei difetti superficiali delle ottiche per interferometri di Onde Gravitazionali
A. Allocca, R. A. Day, G. Cella

## Slide 2: Outline
Detecting Gravitational Waves with interferometers
The problem of mirror aberrations and the corrective thermal compensation devices for GW detectors
New idea for thermal compensation: CHRAC
Conclusions

## Slide 3: Outline
Detecting Gravitational Waves with interferometers
The problem of mirror aberrations and the corrective thermal compensation devices for GW detectors
New idea for thermal compensation: CHRAC
Conclusions

## Slide 4: Gravitational Waves and their detection
Einstein’s Theory of General Relativity foresees the existence of Gravitational Waves
Effect of a GW on free-falling masses
Very weak amplitude:
The distance between two masses separated by ~Km will change by m
x
y
z
L
L’
“That is comparable to a hair’s-width change in the distance from the Sun to Alpha Centauri, its nearest star”.

## Slide 5: Michelson Interferometry to detect GWs
Use an interferometer as a transducer: convert displacements into optical signals
Enhance the signal
Suspended mirrors to reproduce the free-fall condition
A differential variation of the arm lengths is revealed at the antisymmetric port of the interferometer
Free-falling
masses

## Slide 6: Michelson Interferometry to detect GWs
Use an interferometer as a transducer: convert displacements into optical signals
Enhance the signal
Fabry-Perot cavity for “longer arms”
Recycling mirror to recover the power reflected from the arms
Recycling mirror to enhance GW audio sidebands
Heterodyne detection to get a signal linearly proportional to the GW amplitude
Suspended mirrors to reproduce the free-fall condition

## Slide 7: Advanced Virgo
125 W
F = 450
Interferometer working point: dark fringe condition
(destructive interference between beam recombining at the Beam Splitter)
To reach the design sensitivity it’s necessary to limit effects preventing the perfect destructive interference between recombining beams

## Slide 8: Outline
Detecting Gravitational Waves with interferometers
The problem of mirror aberrations and the corrective thermal compensation devices for GW detectors
New idea for thermal compensation: CHRAC
Conclusions

## Slide 9: Mirror aberrations
Mirror aberrations (cold and thermal defects) can spoil the sensitivity of the interferometer
Mode mismatch – beam intensity profile and phase don’t match that of the resonator
Scattering – the cavity beam is scattered by a rough surface can bring higher order modes into resonance and produce diffuse light
Frequency splitting – modes of the same order see a different overall radius of curvature, and their resonance frequencies result to be different.
Mechanisms reducing sensitivity
Residual mirror RMS 0,5 nm RMS to fulfill the requirements of Advanced Virgo

## Slide 10: Mirror aberrations
Mirror aberrations (cold and thermal defects) can spoil the sensitivity of the interferometer
Mode mismatch – beam intensity profile and phase don’t match that of the resonator
Scattering – the cavity beam is scattered by a rough surface can bring higher order modes into resonance and produce diffuse light
Frequency splitting – modes of the same order see a different overall radius of curvature, and their resonance frequencies result to be different.
Mechanisms reducing sensitivity
Residual mirror RMS 0,5 nm RMS to fulfill the requirements of Advanced Virgo

## Slide 11: Scattering
At low angle  can bring into resonance High Order Modes (HOMs) which could be close to the resonance
At large angle  can introduce losses in the intra-cavity power and diffuse light
At intermediate angle  can excite HOMs whose spatial extension is as large as the mirror size and also induce clipping losses

## Slide 12: One possible solution: in-situ thermal compensation
A different mode content in the two arms prevents a perfect distructive interference between the beams recombining at the beam splitter

## Slide 13: The principle of thermal compensation
Use an auxiliary heat source to induce controlled thermal effects in the optics and therefore correct the beam phase aberrations
Thermo-elastic deformation
Thermo-refractive effect
Elasto-optic effect

## Slide 14: Existing thermal compensation devices
Thermally Deformable Mirrors to improve mode matching
Ring heater and CHRoCC to change the mirror Radius of Curvature

## Slide 15: Thermal compensation devices
CO2 laser to correct High spatial Frequency defects
Double axicon for symmetrical aberrations
Scanning system for
non-symmetrical defects

## Slide 16: Outline
Detecting Gravitational Waves with interferometers
The problem of mirror aberrations and the corrective thermal compensation devices for GW detectors
New idea for thermal compensation: CHRAC
Conclusions

## Slide 17: A new thermal compensation system: the CHRAC
All aspects must be accurately analyzed in order to be able to design the whole system from scratch
Correction of high spatial frequency defects with CHRAC
Matrix of actuators emitting thermal radiation
Optical telescope to image the matrix on the mirror surface
Very simple system!
Central Heating Residual Aberration Correction
Thermo-elastic deformation

## Slide 18: One pixel full characterization
Temperature increase of about 1°C for 6 mW absorbed
Deformation of about 15 nm for 6 mW absorbed
Wavefront deformation sensed with a wavefront sensor

## Slide 19: CHRAC matrix first prototype
61 actuators
1 cm
Deformation of about 70 nm PtV (same order of magnitude as in simulation)
About 30mW absorbed per pixel
Simulated
Measured

## Slide 20: Effect of the correction on a single table-top Fabry-Perot cavity operated with Laguerre-Gauss modes LG33 (ANR-Laguerre project at APC in Paris)
reduce astigmatism of about 42%
enhance astigmatism of about 58%
Astigmatism
Ideal beam shape
By projecting a thermal pattern e were able to:
Cavity transmitted beam used as error signal

## Slide 21: Outline
Detecting Gravitational Waves with interferometers
The problem of mirror aberrations and the corrective thermal compensation devices for GW detectors
New idea for thermal compensation: CHRAC
Conclusions

## Slide 22: Conclusions
The CHRAC is a simple system of contact-less thermal compensation
It seems to work very well! The experimental results obtained so far were only limited by the power provided by the specific source. There’s room for more investigation.

## Slide 23: Thanks for your attention