## Slide 1: SOI wafers: summary of relevant aspects
Gian-Franco Dalla Betta
University of Trento and TIFPA INFN, Trento, Italy
gianfranco.dallabetta@unitn.it

## Slide 2
Fixed parameters
After interactions with ICEMOS, the following aspects
can be considered as fixed:
  same starting substrates as SiSi wafers, both in terms
  of thickness(es) and of doping concentrations
  possibly use standard SOI ICEMOS process
  provide it ensures 200 nm oxide layer
  external service for back-side Boron implant
  external service for B implant profile measurement

## Slide 3
p++ low Wcm wafer
P- high Wcm wafer
To be thinned down
P- high Wcm wafer
To be thinned down
p++ low Wcm wafer
SiSi vs SOI for 3D
SiO2
SiSi
SOI
Similar process except for the etching of the ohmic columns
  - FBK demonstrated the feasibility
  But is it possible to manage both variants as a process split ?
  If YES, what would be the best process strategy/schedule ?
On the back-side of the FZ wafer, 3D-SOI requires a p-spray layer
to reduce the electric field at the interface
p-spray

## Slide 4
p++ low Wcm wafer
P- high Wcm wafer
To be thinned down
P- high Wcm wafer
To be thinned down
p++ low Wcm wafer
SiSi vs SOI for PAE
SiO2
SiSi
SOI
Similar process except for the etching of the trenches
  Is it possible to manage both variants as a process split ?
  If YES, what would be the best process strategy/schedule ?
On the back-side of the FZ wafer, PAE-SOI requires a p+ layer
for “ohmic contact” (optimal bias voltage distribution)
p+

## Slide 5
Relevant aspects for decision
Time
  SOI wafers will likely require at least 2 months
  for delivery
  Can 3D batch wait so long ?
  Can it start with SiSi and later add SOI ?
Complexity
  Is it wise to mix the two 3D process options ?
  Is it better to try SOI first with PAE ?