## Slide 1: Membrane gas separation: Fundamentals and applications Giuseppe BARBIERI Institute on Membrane Technology (ITM-CNR), National Research Council, c/o The University of Calabria, Cubo 17C, Via Pietro Bucci, 87036 Rende CS, Italy g.barbieri@itm.cnr.it giuseppe.barbieri@cnr.it School for PhD LTL-2015 Science and Instrumentation Technologies at UNICAL Rende June 8-12, 2015

## Slide 2: Main sources of CO2
 | Source | Separation
Flue gas streams | Power plants, coal gasification plants, Steel factory Cement factory, Transportation | CO2/N2
Natural Gas | Sweetening of Natural gas, etc. | CO2/CH4
Biogas | Various | 
Inventory of U.S. Greenhouse Gas Emissions and Sinks (2008), EPA

## Slide 3: Flue gas emissions by….
Power plant
Steel factory
Cement factory
Coal gasification plant

## Slide 4
CO2/CH4 mixtures by….
BIOGAS
NATURAL GAS SWEETENING

## Slide 5
OxyFuel combustion

## Slide 6
Competing technologies in gas separation
Aaron D., Tsouris C., Separation Science and Technology, 40, (2005), 321-
ABSORPTION
Absorption is a process that relies on a solvent’s chemical affinity with a solute to dissolve preferably one species into another. It is widely proposed for CO2 separation where generally, monoethanolammine or a solid absorbent is used. High amount of energy consumed is for solvent(MEA) recovery (3-4 units)

## Slide 7
Competing technologies in gas separation
Aaron D., Tsouris C., Separation Science and Technology, 40, (2005), 321-
ADSORPTION
The PSA process is based on the capacity of some adsorbents (zeolites, etc.) in adsorbing such gases at high gas-phase partial pressure. Proper selection of the adsorbents is critical for both the performance of the unit and adsorbent life-time. For instance, the CO2 is adsorbed at higher partial pressure and then desorbed at lower partial pressure. High pressure is required (3-4 units).

## Slide 8
Competing technologies in gas separation
Aaron D., Tsouris C., Separation Science and Technology, 40, (2005), 321-
Low temperature separation process. The difference in boiling temperatures of the feed components affects the separation. One of the main advantages is the ability to produce separated hydrocarbon streams rich in C4+, ethane/propane, etc. One of the main drawbacks is the presence of H2O in the gaseous stream that can strongly affect the separation performance; the gaseous stream to be treated needs to be completely dehydrated prior to be cooled. High energy intensity. Pre-treatment stages of the up-stream. (2 units)
CRYOGENIC

## Slide 9: …
Separations with membranes
  Experiments, simulations, upper limits evaluation, etc.
Conversion using membranes
  Experiments, simulations, thermodynamics, etc.
Membranes and other technologies
  Mass and energy intensity
  Design/process parameters
  Integration of membrane separation/reaction in producing cycles
  Mass and energy intensity
  Design/process parameters

## Slide 10: Some separations investigated
CO2/N2 separation
  Involved streams have not a value
  Pressure is required only for separation
  The final stream is the permeate (at low pressure)
  Low CO2 feed concentration (10-30%)
CO2/CH4 separation
  A value product (CH4) containg stream
  Pressurised stream
  The final stream is the retentate (high pressure)
O2/N2 separation for oxygen enriched air
  Feed stream need a pretreatment for powder
  Low O2 concentration (21%)

## Slide 11
What is a membrane?
A membrane is a physical device able to separate selectively one ore more components in a mixture while rejecting others.

## Slide 12: Advantages of membrane technology
efficiency and operational simplicity…
high selectivity and permeability for the transport of specific components…
low energetic requirement…
good stability and compatibility between different membrane operations…
environment-compatibility…
large flexibility and easy scale-up…
advanced levels of automation and remote control …

## Slide 13: The most important operations for membrane gas separation
H2 purification and production
CO2 capture and sequestration
N2/O2 separation
N2 production
Natural gas sweetening
Biogas separation and conversion

## Slide 14
Rubbery Polymers | Glassy Polymers
Fluoro elastomers Neoprene Nitrile rubber Poly(dimethylsiloxane) Polyethylene chlorine sulfonated Polyvinilchloride plasticized Polyuretane | Aromatic Polyamides Cellulose Acetate Perfluorodioxoles Polyacetilenes Polycarbonates Polyimides Poly(phenileneoxide) Polysulfone Poly(1-trimethysilyl-1-propyne) Polymer of intrinsic microporosity (PIM) Thermally rearranged polymer(TR)
Most important glassy and rubbery polymers used in membrane GS

## Slide 15: Permeation mechanisms
Sorption-diffusion: e.g. metal membranes, dense polymeric membranes
Molecular sieve: e.g. Ceramic membranes, zeolite, microporous polymeric membranes
Viscous flow: e.g. microporous polymeric membranes in enzyme loaded membrane reactors
Through pore flow: e.g. zeolite membranes, microporous polymeric membranes in enzyme loaded membrane reactors

## Slide 16
Transport mechanism through POROUS membranes
Knudsen flow
Surface diffusion
Capillar condensation
Viscous flow
H. Strathmann, L. Giorno, E. Drioli, An introduction to membrane science and technology, Publisher CNR Roma, ISBN 88-8080-063-9, 2006

## Slide 17: Gas transport by the sorption-diffusion mechanism
In a dense membrane, the mass transport so-called sorption-diffusion consists of three relevant steps:
sorption of the various components from a feed mixture according to their partition coefficient between the gas and polymer phase;
diffusion of the individual components within the membrane phase according to their activity gradients; and
desorption of the components from the membrane in the permeate gas phase.

## Slide 18: Conventional dual mode sorption
Henry:
Langmuir:
Dual Mode Sorption:

## Slide 19
  Variables and Units
  Permeability: Mass permeating a unit surface area of the membrane, per unit of time, under a unit of pressure, per unit of THICKNESS
  Permeance: Mass permeating a unit surface area of the membrane, per unit of time, under a unit of pressure, for the whole membrane THICKNESS

## Slide 20: Selectivity
The separation capacity of a membrane is a crucial parameter.
The selectivity of a membrane for various components of a mixture is defined by the ratio of the permeability (Permeance, etc.)

## Slide 21
  Variables and Units

## Slide 22: Experimental analysis

## Slide 23: Experimental analysis

## Slide 24: Experimental analysis
FotoRiduCO2

## Slide 25
F. Falbo, F. Tasselli, A. Brunetti, E. Drioli, G. Barbieri, Brazilian Journal of Chemical Engineering, vol 31 n°4, pp 1023-1034 (2014)
F. Falbo, A. Brunetti, G. Barbieri, E. Drioli, F. Tasselli, Applied Petrochemical Research (2015), submitted.
Membrane gas transport properties
FotoRiduCO2

## Slide 26: Thermal rearranged polymer membranes
METT

## Slide 27: Polymeric membranes generally undergo a trade–off limitation between permeability and selectivity: as permeability increases, selectivity decreases, and vice-versa.
Robeson trade-off
Robeson L.M., Journal of Membrane Science, 320, (2008), p.390
*TR, thermally re-arranged

## Slide 28: Polymeric membranes generally undergo a trade–off limitation between permeability and selectivity: as permeability increases, selectivity decreases, and vice-versa.
Robeson trade-off
Robeson L.M., Journal of Membrane Science, 320, (2008), p.390
*TR, thermally re-arranged

## Slide 29: Polymeric membranes generally undergo a trade–off limitation between permeability and selectivity: as permeability increases, selectivity decreases, and vice-versa.
Robeson trade-off
Robeson L.M., Journal of Membrane Science, 320, (2008), p.390

## Slide 30: Polymeric membranes generally undergo a trade–off limitation between permeability and selectivity: as permeability increases, selectivity decreases, and vice-versa.
Robeson trade-off
Robeson L.M., Journal of Membrane Science, 320, (2008), p.390

## Slide 31
In the equations jCO2, jN2 are the dimensionless molar flow rate, for CO2 and N2, respectively and z is the dimensionless module length.
Qi and f are the parameters affecting the performance of a one stage membrane system, the permeation number and the feed to permeate pressures ratio, respectively.
Qi expresses a comparison between the two main mass transport mechanisms involved: the permeating one through the membrane and the convective flux of the feed stream.

## Slide 32
  Separation analysis by Mathematical Modelling

## Slide 33
  Separation analysis by Mathematical Modelling

## Slide 34
  Separation analysis by Mathematical Modelling

## Slide 35: 14%

## Slide 36
14%

## Slide 37
14%

## Slide 38
20%

## Slide 39
20%

## Slide 40
20%

## Slide 41
Comparison among some important design parameters
 | Membrane System | Absorption | Adsorption | Cryogenic
Operating flexibility | High (%CO2>20%) Low (%CO2<20%) | Moderate | High | Low
Response to variations | Instantaneous | Rapid (5-15 minutes) | Rapid (5-15 minutes) | Slow
Start up after the variations | Extremely short (10 minutes) | 1 h | 1 h | 8-24 h
Turndown | down to 10% | down to 30% | down to 30% | down to 30-50%
Reliability | 100% | Moderate | Moderate | Limited
Control requirement | Low | high | high | high
Ease of expansion | Very high (modularity) | Moderate | Moderate | Very low

## Slide 42
 | Absorption | Adsorption | Cryogenic | Membrane System
CO2 in the feed, (% molar) | >5 | >10 | >5 | >10
CO2 purity, % | >95 | 75-90 | 99.99 | 80-95(*)
CO2 recovery, % | 80-95 | 80-95 | 99.99 | 60- 80(*)
Energy requirement, MJ/kgCO2 | 4-6 (Favre 2007) | 5-8 (Aaron 2005) | 6-10 (Eide et al., 2005) | 0.5-10 (Favre 2007)
CO2 capture cost, $/ton | 40-100 (Merkel et al, 2010) | - | - | 23** (Merkel et al, 2010
*Considering a CO2/N2 selectivity of 50 in one stage process
**Considering a multistage process
The selection of the separation process may be driven by specific considerations, strictly related to the output to be obtained. The feed composition (CO2%), the feed conditions (pressure and temperature), the product purity and the final destination of the product strongly affect the choice
[1] Favre E., Journal of Membrane Science, 294, (2007), p.50
[2] Brunetti A., Scura F., Barbieri G., Drioli E., 2010, Membrane technologies for CO2 separation, Journal of Membrane Science, 359, 115–125
[3] Aaron D., Tsouris C., Separation Science and Technology, 40: 321–348, 2005
[4] Eide L.I., Anheden M., Lyngfelt A., Abanades C., Younes M., Clodic D., Bill A.A., Feron P.H.M., Rojey A., Giroudière F., Oil & Gas Science & Technology, 60, (2005), p.497
[5] Bounaceur R., Lape N., Roizard D., Vallieres C., Favre E., Energy, 31, (2006), p.2556.
[6] Merkel T., Lin. H., Wei X., Baker R., Journal of Membrane Science, 359, (2010), 126-139

## Slide 43: Selection guidelines for some applications
Process application | Feed conditions | Membrane System | PSA | Cryogenic
Catalytic reformer off-gas | 70-90%vol H2 30-10% C1 to C6+ ppv of aromatics and HCl Pressure: 15-30 bar Room Temperature | H2 purity: 98%. Final destination: uses such as catalyst regeneration | H2 purity: 99+% H2 recovery: 82-90% Final destination: primary source of make up hydrogen for hydrocracker | Not used due to the necessity of pretreatment for aromatic removals
Hydroprocessor purge gases | High pressure purge gas: 75-90%vol H2 Hydrocarbon balance Pressure: 50-200 bar Room Temperature | H2 purity: 92-98% H2 pressure: 20-40 bar H2 recovery: 85-95% Final destination: make-up hydrogen compressor | Not used because of the high feed pressure | Not used due to the low flow rates
 | Low pressure purge gas: 50-75%vol H2 Hydrocarbon balance Pressure: 5-20 bar Room Temperature | Not used because of the low feed pressure | H2 purity: 99% H2 pressure: 1 bar H2 recovery: 80-90% Final destination: primary source of make up hydrogen for hydrocracker | 
FCC off-gas and other refinery purge streams | 15-50%vol H2 Hydrocarbon or olefins balance Pressure: 5-20 bar Room Temperature | Feed compression: > 25 bar H2 purity: 80-90% H2 pressure: 5-20 bar H2 recovery: 50-85% Final destination: low pressure hydrotreaters The tail gas is sent to downstream hydrogen recovery units | Not used because of the low H2 concentration in the feed | H2 purity: >95% H2 pressure: 15-30 bar Recovery of a mixed stream containing >99+% of C2+ components
Ethylene off-gas | 80-90%vol H2 CO, CO2, CH4 balance Pressure: 15-30 bar | H2 purity: 95-97% H2 recovery: 80-90% Final destination: make-up hydrogen compressor | H2 purity: 99.5% H2 recovery: 80-90% Final destination: primary source of make up hydrogen for hydrocracker | H2 purity: 95% H2 pressure: 15-30 bar Final destination: make-up hydrogen compressor

## Slide 44
Separation | Process | Traditional technology | Membrane Material | Status of membrane technology application
H2/N2 | Ammonia purge gas | PSA | Polysulfone | Plant installed (Prism by Permea)
 |  |  | Pd-based | Lab scale
H2/CO | Adjustment of H2/CO ratio in syngas plant | PSA | Silicon rubber | Lab scale
 |  |  | Polyimide | Plant installed (Separex)
 |  |  | Pd-based | Lab scale
H2/hydrocarbons | Hydrogen recovery in refineries | PSA | Silicon rubber Polyimide | Plant installed (Sinopec Zhenhai (china) Prism by Permea Du Pont)
 |  |  | Pd-based | Lab scale
H2/light hydrocarbons | Ethylene cracker old trains | Cryogenic distillation | PTMSP; PMP | Pilot plant
 |  |  | Pd-based | Lab scale
O2/N2 | Air separation | Cryogenic distillation | Silicon rubber | Plant installed (Cynara; Separex; GMS; Air Products)
 |  |  | Polysulfone | Plant installed (Permea)
 |  |  | Polyimide | Plant installed (Medal; Dow-Generan; UBE)
 |  |  | Polyphenilene | Plant installed (Aquilo)
 |  |  | Ethyl Cellulose | Plant installed (Air Liquide)
 |  |  | Ion transport (perovskite) | Lab scale
 |  |  | Pd-based | Lab scale
Main industrial applications of GS membrane

## Slide 45
N2/CH4 | Nitrogen removal | Cryogenic distillation | Silicon rubber PMP Parel | Pilot plant
 |  |  | PEBAX | Lab scale
H2O/CH4 | Dehydration | Glycol absorption | Cellulose acetate Polyimide polyaramide | Plant installed [51]
CO2/CH4 | Sweetening of natural gas | Amine absorption | Cellulose acetate | Offshore platforms In Thailand gulf. (Cynara-NATCO); Grace-Separex
 |  |  | Polyaramide | Plant installed (Medal)
 |  |  | Polyimide | Plant installed (Medal)
 |  |  | Perfluoro-polymers | Plant installed (MTR)
CO2/Hydrocarbons | Natural gas liquid removal | Glycol absorption and cooling inn a propane refrigeration plant (-20°C) | Cellulose acetate Polyimide polyaramide | Early commercial stage. A demonstration system installed
CO2/N2 | CO2 capture from flue gas streams | Amine absorption | Polyimide | Pilot plant
 |  |  | FSC; PEEKWC; Zeolite, silica based; carbon | Lab scale
VOCs/gas | Polyolefin plant resin degassing; Ethylene recovery | Adsorption, Refrigeration and turbo-expander plants | Silicone rubber PTMSP | Plant installed (MTR; OPW VaporsaverTM)
Main industrial applications of GS membrane

## Slide 46
  Membrane modules

## Slide 47
Thank you for your attention
 | National Research Council Institute on Membrane Technology