## Slide 1: HVR_CCPD: Hybridization
Pixel R&D Projects Meeting
Milano, 8 June 2015
G. Darbo / INFN – Genova
On behalf of HVR_CCPD Genova:
M. Biasotti, V. Ceriale, G. Darbo, G. Gariano, F. Gatti, C. Gemme, P. Morettini, L. Rossi, A. Rovani, E. Ruscino, M. Sannino.
Indico:
https://agenda.infn.it/conferenceDisplay.py?confId=9770

## Slide 2: CCPD – Capacitively Coupled Pixel Detectors
Thin FE chip
R/O Architecture
Electrical Interconnection
Bump-bond
HV/HR-CMOS
Amp/Disc layer
Drift layer
New generation of Pixel detectors under development for the ATLAS Pixel detector at the HL-LHC
  Passive hybrid detectors use “resistive” coupling between sensor and R/O chip
  HV-CMOS detector use a High Voltage chip technology to make sensor and amplifier which is then coupled to the “usual” front-end chip…
  through a dielectric…
Why capacitive?
  Passive sensors need diode biasing from amplifier other than for collecting charge: AC coupling is (almost) not an option.
  Capacitive coupling it might be cheaper: glue and alignment looks easier.
Thin FE chip
Dielectric (glue)
HV/HR-CMOS
Amp/Disc layer
Drift layer
© T. Hemperek, Bonn, DE

## Slide 3: (Some) Requirements
Capacitance uniformity
  Between pixels, from an assembly to another: ~10 %  thickness uniformity
  Most critical for analog coupling (no discriminator in the HV/HR-CMOS)
  RD-53 chips will have 50µm pitch, but also versions for very small pixels: 25µm pitches are considered
  X-Y alignment: better than few µm (cross talk / signal loss)
Glue requirements
  Low viscosity: 0.1 ÷ 0.5 Pas
  Radiation hard: epoxy
  Not degassing
  Low temperature curing, investigating UV/Temp curing glues
  Minimum thickness of glue to give for full adhesion (usual specs are 1-2 mil, but we want less!)
For chip-to-wafer and wafer to wafer TVS are needed on one or both facing chips
  For the moment we are looking at chip-to-chip processes

## Slide 4: Controlled Glue Thickness
Procedure for Controlled Glue Thickness
  Deposit uniform layer of SU8 photoresist on R/O chip wafer (or single chip) by spinning – tune for 5 µm layer by controlling RPM speed
  Pattern pillars using lithographic process .
R/O CHIP
R/O CHIP
Spin SU-8 photoresist
Pattern pillars by mask
Glue deposition
R/O CHIP
DETECTOR CHIP
Align & pressure
Deposition of SU8 photoresist by spinning
Profile of pillars on top of a FE-I4 chip
Pillars
FE-I4 topography
© V. Ceriale, A. Rovani, Genova, IT

## Slide 5
sd
Scan 1
Scan 2
Scan 3
Scan 4
Scan 5
 | Side A [µm] | Side B [µm]
Scan 1 | 254.40 | 257.04
Scan 2 | 257.31 | 257.91
Scan 3 | 256.77 | 257.83
Scan 4 | 256.55 | 257.55
Scan 5 | 255.97 | 257.23
Side A
Side B
© A. Rovani & V. Ceriale - Genova
FE-I4 chip
SU8 pillar

## Slide 6: Basic CCPD Process under Study
Pillars can be produced by standard lithographic processes:
  SU8 photoresist deposition (3 – 5 µm thickness) by spinning on 8 – 12-inch wafers (for testing we could use 6-inch wafers)
  Pillars are made by mask as for bump-bonding openings in the photoresist
  Chips need alignment after a glue is deposited (flip-chip machine)
  SU8 deposition by spinning

## Slide 7: Plan for Hybridization - Glues
Look for UV/Temp curing glues
  Reason: tacking of glued chips and the final cure in the oven – this reduces the flip-chip machine time from several hours to few minutes!
  Fineplace modified by Alessando R. by adding UV LEDs. – tested on glasses with bump pads and available glue samples (wirebond potting glue) – looks promising!
  Valentina C. has searched for glue candidates – Individuated suitable candidate we are going to order.

## Slide 8: Plan for Hybridization – Dummy wafers
Test pillar and glue process on dummy wafers/chips
  Design a 6-inch wafer with FE-I4 size dummies
    Place 48 capacitors of 1 mm2 each on every dummy chip.
    Capacitance gives information of glue thickness uniformity
PROBING PADS
FLIP
Equivalent circuit
after flip Ctot = ½ C

## Slide 9: Dummy Assembly
Credits: Alessandro Rovani – INFN / Genova

## Slide 10
Overlaid – Bottom metal + SU8 pillard + Top metal
Credits: Alessandro Rovani – INFN / Genova

## Slide 11: Mask Layout (draft)
pillars
metal
Ref.: Alessandro R.

## Slide 12: 3D Simulation - HyperLynx® 3D EM
Stack-up:
5µm dielectric thickness
Credits: Ettore Ruscino – INFN / Genova

## Slide 13: Dielectric thickness (µm)  Capacitance (pF)
Dielectric | 2.5um | 3um | 3.75um | 5um | 7.5um | 15um
C(1,2) | 6,7485 | 5,6125 | 4,4937 | 3,3829 | 2,2878 | 1,1613
C(3,4) | 6,7267 | 5,5912 | 4,4731 | 3,363 | 2,268 | 1,1436
C(5,6) | 6,8096 | 5,6761 | 4,5565 | 3,4424 | 2,3444 | 1,2124
C(7,8) | 6,7485 | 5,6125 | 4,4937 | 3,3829 | 2,2878 | 1,1613
C(9,10) | 6,7267 | 5,5912 | 4,4731 | 3,363 | 2,268 | 1,1436
C(11,12) | 6,8096 | 5,6761 | 4,5565 | 3,4424 | 2,3444 | 1,2124
1/X
C3,4
C5,6
C9,10
C11,12
C1,2
C7,8
Dielectric thickness (um)
Capacitance (pF)
10 MHz
Chart: 
| 2.5 | 3.0 | 3.75 | 5.0 | 7.5 | 15.0
C(1,2) | 6.7485 | 5.6125 | 4.4937 | 3.3829 | 2.2878 | 1.1613
C(3,4) | 6.7267 | 5.5912 | 4.4731 | 3.363 | 2.268 | 1.1436
C(5,6) | 6.8096 | 5.6761 | 4.5565 | 3.4424 | 2.3444 | 1.2124
C(7,8) | 6.7485 | 5.6125 | 4.4937 | 3.3829 | 2.2878 | 1.1613
C(9,10) | 6.7267 | 5.5912 | 4.4731 | 3.363 | 2.268 | 1.1436
C(11,12) | 6.8096 | 5.6761 | 4.5565 | 3.4424 | 2.3444 | 1.2124
Credits: Ettore Ruscino – INFN / Genova

## Slide 14: Dummy Wafers & Process Plan…
Dummy wafer layout completed
  6-inch wafer will be produced by FBK – standard thickness, one metal layer on top of passivation (oxide)
Spinning of SU8 – two options:
    Selex – they have experience with SU8 and they can do – we do not have a quote of the cost.
    PTA - http://www.pta-grenoble.com/ - near Grenoble – Clean room and equipment available at hour cost to users (after training).
Flip chip at Genova or at other sites (Barcelona and Geneva)
  Modified the flip-chip machine for UV curing
After qualification, process a full FE-I4 wafer.
We are also looking at full simulation of HV/HR-CMOS – FE chip coupling for optimal signal transfer
  Configuration data from R/O chip to HV/HR-CMOS can be transmitted capacitively… only power/ground need DC connection (laser soldering to flex hybrid as in ALICE proposal?)

## Slide 15: AIDA-2020 – WP6
Task 6.4 Hybridisation
  Perform basic R&D on capacitive interconnection
  Setup production facilities for full-prototype assemblies (chips on test boards)
  Deliver full assemblies to all participating projects
  Investigate options for future industrialisation of the interconnection process
Task 6.4 Beneficiaries and (INFN) interested groups:
  INFN-GE, IFAE, UNILIV  HVR_CCPD will be carried on in collaboration with AIDA-2020
  Additional INFN groups involved: Milano.
Activities on HV/HR-CMOS hybridization funded by 3 year INFN project:
  AIDA 2020: 1/5/2015 – 30/4/2019
  HVR_CCPD: 2015 – 2017
  Matching funds to AIDA-2020 WP6 Task 4 comes from INFN – HVR_CCPD will cover it partially.
More INFO on AIDA-2020:
  WEB Site: http://aida2020.web.cern.ch
  AIDA-2020 kick-off meeting (3-5/6/2015): https://indico.cern.ch/event/382133/

## Slide 16: Conclusions
Hybridization activities started with funds from CSN1 in 2014 and followed by CSN5 (HVR_CCPD)
  Most of the work done at home using ATLAS and LTD (Low Temperature Detector) laboratories at INFN – Genova
Start to involve Industries for more systematic studies on dummies:
  FBK and Selex (contracts in preparations)
The AIDA-2020 approval shall provide an international collaboration framework:
  Collaboration with the other beneficiaries: Liverpool and Barcelona

## Slide 17: Backup slides

## Slide 18: UV/Thermal Curing Glue 1/2
Valentina contacted Master Bond. They propose two epoxy glues.
  UV15DC80LV -> looks interesting, do we have questions to Master Bond?
  UV15-7DC -> viscosity too high!
  The price to purchase the products in the ½ pint size is $ 800/each
Similar to EpoTEK 301-2 and Araldite 2020.
1000 cps = 1 Pas

## Slide 19: PTA Quote
Regarding the use of MA8:
- Mask dimension 7x7” for 6” wafers (available)
- Mask dimension 9x9” for 8” wafers (available)
- Photoresist available : SU8-2005 (negative, 5 microns thick); SU8-2025 (negative, 25 microns thick) ; AZ4562 (positive, 5 to 10 microns thick)
Regarding the PTA access:
Project submission in line
Process flow definition
If work done by the team of the project
Safety training for cleanroom access (thanks to a badge)
Equipment training
Use the equipment to do the work
Billing based on the using machine time (210 euros/hours)
If work done by the PTA technical team
Work definition by both technical team and project team
Work done by the technical team
Billing based on the attendance time (120euros/hours) and the using machine time (210 euros/hours)

## Slide 20: Plateforme Technologique Amont

## Slide 21: Summary of Mask/Wafers
This activity will be supported by AIDA-2020 (1/5/2015 – 30/4/2019)
  2 x 2 years “assegno di ricerca”
And funded by INFN (2015 – 2017)
  RD_FASE2 (BB)
  HVR_CCPD (HV-CMOS)
Description | Use | Mask / Wafer | Qty
Resistive chain | BB | Mask | 2 (metal, bump opening)
Dummy chip with chains | BB | Wafer @ FBK | 8
Bump deposition | BB | Mask | 1
12” wafers for deposition | BB | wafers | 9 (few used by Selex)
12” wafer bumps | BB | Mask | 1
Dummy chip for glue | HV | Mask | 1 (metal)
Dummy chip for glue | HV | Mask | 1
Dummy chip for glue | HV | Wafer @ FBK | 6

## Slide 22
Units in pF
0.43
0.25
3.61
0.24
0.39
0.32
0.39
0.24
3.61
0.25
0.43
3.47
3.61
3.47
3.61
3.49
3.49
2µm metal thickness
(@ 10MHZ)
Credits: Ettore Ruscino – INFN / Genova