## Slide 1
Looking with Terahertz Eyes
Mauro Missori, Istituto dei Sistemi Complessi – CNR
and
C. Conti, R. Fastampa, Università di Roma "Sapienza"
A. Mosca Conte, O. Pulci, Università di Roma Tor Vergata
M. Peccianti, University of Sussex (UK)
RAIN15 -- RAdiazione per l'INnovazione 2015
Frascati, 12-13 October 2015

## Slide 2
This is the so-called ‘terahertz gap’. It has historically been defined by the relative lack of convenient and inexpensive sources.
Application in science and industry, offering complementary or even
alternative methods of material characterization.
Terahertz (THz) radiation = electro-magnetic waves in a frequency range 0.1 - 10 THz
Electronics
Photonics
0.001
0.01
0.1
1
10
100
1000
10000
Microwave
mm wave
Sub mm wave
Infrared
Visible
Ultraviolet
X-ray
Terahertz Technology:
optoelectronic devices
?
Frequency [THz]
Wavelength 3 – 0.03 mm
Wavenumber: 3.3 – 333 cm-1
Energy: 0.41 – 41meV
Temperature: 1 – 100K

## Slide 3
Broadband THz radiation can be efficiently generated and detected using femtosecond lasers and photoconductive antennas based on semiconductor materials.
THz-Generation and Detection

## Slide 4
THz Time-Domain Spectroscopy
Phase sensitive
coherent detection scheme
THz waveform
Fourier Transform
50
60
70
80
90
100
-0.2
0
0.2
0.4
0.6
0.8
1
1.2
Time [ps]
Amplitude [n.u.]
0
0.5
1
1.5
2
2.5
3
3.5
-60
-50
-40
-30
-20
-10
0
Frequency [THz]
Power Spectral Density [dB]
Optical Delay (rad)
0
-


## Slide 5
Medical diagnostics
Morphological and compositional diagnoses,(e.g. Tumors)
New therapies? (High-Energy THz)
in-Vivo imaging (Dental Imaging)
Paleontology
Fossil Imaging
Process control
Drug analysis
Cellular chemistry
Cellular Microscopy
Security
(Horizon 2020)
Morphological identification of Illicit items (e.g. weapons).
Life Science
Materials,Sensing
and Environment
Forensic medicine
Morphological and compositional identification of illicit substances (drugs, explosives, bio-harzard)
Material structural analysis
Food analysis
Degradation analysis
Cultural heritage conservation
Material science
Ultrafast dynamics (High-Energy THz)
Interaction with charges and magnetic dipoles
Quantum computing
THz Emerging Markets

## Slide 6
B. B. Hu and M. C. Nuss, "Imaging with terahertz waves," Opt. Lett. 20, 1716-1718 (1995)
Freshly cut Leaf
After 48 hours
Water concentration
THz waves penetrate a wide variety of non-conducting materials such as polymers, paper, textiles, ceramics, composite materials, chemical powders…

## Slide 7
Clery, Science 297, 763 (2002)
TeraView Ltd (UK)
…and are being reflected by metals
2 million people will fly today only in US

## Slide 8
Coherent Imaging
V. P. Wallace et al.,
J. Opt. Sec. Am. A 25, 3120 (2008)
Image at different delays (a): t = 10.0 ps, surface of SD card, (b) t = 11.5 ps, bonding plastic, (c) t = 15.0 ps, control chip, (d) t = 16.7ps, main memory chip
(a)
(a)
(b)
(c)
(d)
Raster-Scan (the image is reconstructed by moving the sample). Pixel size=300m

## Slide 9
Mapping the Formation of Paper Products
THz images and photographs of raw cardboard with irregular and smooth formation.
Paper thickness 200 µm, sample size 45 mm x 70 mm.
Distribution of the grammage for the two cardboard samples compared to a plastic foil with a similar grammage.
Papiertechnische Stiftung (PTS) & Menlo Systems

## Slide 10
Quality Control of Chocolate Products with THz Imaging
Front and back side of chocolate bar after preparation with a glass splinter, a stone, and a metal screw.
THz intensity image of a chocolate bar with different contaminating particles
C. Jördens et al., European Conference on Non-Destructive Testing, 2006

## Slide 11
Optics Communications 285, 1868 (2012)
Spectral Data Base (SDBS) AIST (Japan)
THz enable agile organic compound discrimination through selective absorption and dispersion due to rotational and vibrational transitions

## Slide 12
PROGETTO PREMIALE THEIA
Terahertz imaging advances: looking with teraherts eyes
“The THz core system will be assembled focusing on the establishment of a highly sensitive THz imaging test bed, i.e. a time-domain spectroscopy imaging system, oriented to industry deployment.”
Work-package WP5: Route Toward Super-High Resolution THz Imaging.
Theoretical and experimental investigation of sub-wavelength resolved THz images.
Work-package WP6: Implementation of THz Time-Domain Reflective Spectroscopy.
Theoretical and experimental investigation of material spectroscopic fingerprints from the data retrieved by reflective TDS.
Work-package WP7: THz spectroscopy for non-destructive characterization of cultural heritage artefacts.
Deploy the technology developed in the framework of this project in a real application scenario.
Methods and applications
Other institutions involved

## Slide 13
Early monitoring of the mechanical degradation of ancient paper

## Slide 14
100 mm
M. Missori, et al., Phys. Rev. Lett. 97, 238001 (2006).
Paper: morphology and molecular structure
cellulose fibre
macrofibrils
microfibrils
chains of
cellulose
molecules
Notes: Isolated cellulose possesses a stable thermodynamical configuration, which allows an excellent durability over time.
14

## Slide 15
M. Bicchieri, et al., J. of Raman Spectr. 37, 1186 (2006).
T. Lojewski, et al., Carbohydrate Polymers 82, 370 (2010).
Variations of mechanical and morphological properties
C
O
H
hydrolysis
UV-Vis active oxidized groups (chromophores)
C
O
H
oxidation
C
O
H
thermal energy
humidity
micro-organisms
radiative energy
Degradation at the molecular scale

## Slide 16
Materials
Modern paper samples made of pristine cotton cellulose were artificially aged at 90°C up to 48 days in different environmental settings
Ancient samples produced in 15th century in Italy and France exhibiting different state of conservation and damages

## Slide 17
THz Time-Domain Spectroscopy: paper sheets
Delay (refractive index)
Sample
Reference

## Slide 18
THz Time-Domain Spectroscopy: results
1.9THz
2.4THz
Set up a method to evaluate the degree of crystallinity of ancient paper from THz spectra.
Main spectral features at 1.47 THz, 1.90 THz, 2.13 THz, 2.4 THz and 3.1THz.

## Slide 19
Clare J. Strachan et al., Using terahertz pulsed spectroscopy to study crystallinity of pharmaceutical materials, Chemical Physics Letters 390, 20–24 (2004)
IM=indomethacin
(anti-inflammatory drug)
amorphous
crystalline
Effect of sample crystallinity on THz spectra

## Slide 20
THz data were compared with X-ray diffraction spectra used to calculate crystallinity indexes of samples
THz peak absorption intensity vs
XRD deconvolution crystallinity index
M. Missori et al., Conference on Lasers and Electro-Optics/Europe (CLEO 2015)

## Slide 21
Thanks for
your attention
And a special thank to other scientists involved: Jacek Bagniuk, Matteo Clerici, Joanna Łojewska, Roberto Morandotti, Lorenzo Teodonio, Claudia Violante