## Slide 1
DiaC2Lab
Diamond and Carbon Compounds Laboratory
CVD Diamond for
Ionising Radiation Detection and Concentrated Solar Radiation Conversion
Daniele M. Trucchi
    A. Bellucci – Optical Characterization
    P. Calvani – Diamond Surface Processing & Characterization
    M. Girolami – Photo-electrical Characterization
    V. Valentini – Chemical Characterization
    +
    S. Orlando – Fs-laser Surface Texturing
    A. Santagata + his group
    +
    R. Flammini – Surface Analysis + low dimensional materials
Institute for Structure of Matter (ISM) of the Italian National Research Council (CNR)
Montelibretti Section
Institute for Structure of Matter (ISM) Tito Scalo Section
Institute for Structure of Matter (ISM) TorVergata Section

## Slide 2
Outline
Detection & Monitoring of Radiation:
Diamond Dosimeters for X-Ray and Radiation Therapy
Diamond Detectors for Fast Neutrons
Exploitation of Solar Radiation & Use of Advanced Radiation for Technology:
High-Temperature Solar Cells
    Advanced Surface Texturing
    Turning Diamond into Graphite!

## Slide 3
CVD Diamond
DLC, 1-3 nm
DLC, 1-3 nm
Au, 100 nm
Au, 100 nm
Me, 100 nm
Me, 100 nm
CVD Diamond Dosimeters – Fabrication of Photoconductor Structure
D.M. Trucchi, P. Allegrini, P. Calvani, A. Galbiati, K. Oliver, G. Conte, IEEE Electron Device Letters 33 (2012) 615-617
Dosimeter
Radiation damage resistant
Tissue-equivalent
Primingless
Linear with radiation dose-rate at high bias
Fast with high bias voltages
Highly sensitive

## Slide 4
Fast response under low bias voltage and even under photovoltaic regime (@ 0V)!!!
Schottky Photodiode
Photoconductor
CVD Diamond
DLC, 1-3 nm
Au, 100 nm
Me, 100 nm
WC by PLD, 200 nm
Annealing @ 450 °C
A. Bellucci, S. Orlando, D. Caputo, E. Cappelli, and D.M. Trucchi, IEEE Electron Device Letters 35 (2013) 695-697
CVD Diamond Dosimeters – Schottky Photodiode
WC Schottky/Diamond/Ohmic Structure
Linearity to dose-rate at low voltages and high frequency
Linearity to dose-rate at high frequency needs a continuous increase of bias voltage

## Slide 5
CVD Diamond detector is a compact and versatile solution for fast neutrons, alpha and beta particles spectroscopy and time-of-flight.
Diamond radiation hardness, high radiation sensitivity, low dark current and high thermal conductivity allow room temperature spectroscopy as well as time of flight accurate measurements.
Charge collection efficiency close to 100%
Minimized space charge effects owing to a proprietary diamond/metal junction technology
M. Rebai et al., Journal of Instrumentation 10 (2015) C03016.
M. Girolamiet al., Phys. Status Solidi A (2015) in press, DOI 10.1002/pssa.201532191.
Fast Neutron Spectrometry
Single-pixel diamond spectrometer is operating at ISIS
Diamond Spectrometer Array (12 pixels) will operate at JET
The development of the diamond technology was performed by the DiaC2 Lab of CNR-ISM (Rome),
in collaboration with CNR-IFP (Milan)

## Slide 6
Photon-Enhanced Thermionic Emission (PETE) Devices

A (%)
100
0
IR selective absorber
Function: exploiting IR for heating the cathode
CATHODE
ANODE
CONCENTRATED SOLAR RADIATION

Transparent window
Vacuum enclosure
(pressure as low as possible)
Optically transparent substrate for mechanically supporting the cathode (quartz, sapphire, etc.)
Back surface contact
Absorber: thin-film semiconductor with bandgap of 1.8 eV and a thickness of hundreds of nm
Ideally, a number n semiconductor layers with scaling bandgap
Optimized d to allow photoelectrons to be injected in the following layer
Emitting layer, able to drastically reduce the work function and allow electron escape
ZLOAD
Photo-generation increases electron population at conduction band above the equilibrium level, and the emission energy barrier is reduced:
more electrons are emitted from the cathode at lower cathode temperatures compared to conventional thermionic emitters
Thermalization processes within the cathode increase its temperature, further increasing the emission current density (thermionic emission)
PETE devices utilize both photonic and thermal processes for energy conversion, and are not subject to either the Shockley-Queisser limit or the thermal limit (Carnot)**
**G. Segev, Y. Rosenwaks, A. Kribus, Solar Energy Materials & Solar Cells 140 (2015) 464
PETE* devices can be defined as high-temperature cells for solar concentrating systems, since they avoid the limitations of junction cells and even benefit from high operating temperatures
*J. Schwede,et al., Nature Materials 9 (2010) 762
Secondary conversion system

## Slide 7
CATHODE
III-V Semiconductors
Advantage: no p-n junction is needed
Capability to operate at high temperature
Exploitation of additional thermionic emission
Advanced IV Semiconductors (CVD Diamond)
Bandgap Engineering
Advantages:
Low “native” work function caused by NEA conditions (surface hydrogen termination)
Wide range of operating temperature (<780 °C)
High thermal stability
High robustness
Advantages:
Proper bandgap for absorption and photocarrier generation (about 1.8 eV)
Disadvantages:
High work function -> Necessity of coatings for “work-function-engineering”
Instability at high-temperature
Disadvantages:
Wide bandgap (5.47 eV @ RT)
Defect Engineering
High electron diffusion lengths
Photo-Thermionic Cathode
May 2013 - Apr 2016
Total Project Cost: 4.2 M€
Total EU Funding: 3.0 M€
www.prometheus-energy.eu

## Slide 8
Diamond Photo-Thermionic Defect-Engineered Cathode
d < Ld (diffusion length)
Diamond plate
P-type layer
Graphitic distributed electric contact
n-doped diamond thin layer (100-500 nm)
Surface Texturing
Technological steps:
Implantation of B ions on front surface for a buried p-type layer a) acting as a back electric contact; b) increasing the photogeneration contribution; c) separating e-h for reducing recombination
Fs laser-induced distributed contacts for reducing device series resistance
Fs laser front surface nanoscale texturing for increasing optical absorption and photogeneration
CVD deposition of n-doped thin diamond layer (100-500 nm)
Emitting surface hydrogenation for NEA
Deposition of electric contacts
Electric
contacts
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
H
A. Bellucci, P. Calvani, M. Girolami, and D.M. Trucchi, 2015 IEEE 15th International Conference on Environment and Electrical Engineering Proc., (2015) 1616

## Slide 9
The laser system employed is based on a Spectra Physics Tsunami S - fs oscillator (pulse duration about 100 fs, repetition rate 80 MHz, wavelength 800 nm, peak power > 0.7 W) pumped by a Spectra-Physics Millennia Pro 5sJS (CW, wavelength 532 nm, power 5W). The output of the oscillator is the seed for the Spectra-Physics Spitfire Pro 100 F 1K XP 4W amplifier (pulse duration < 120 fs, repetition rate up to 1000 Hz, wavelength 800 nm, pulse energy up to 4 mJ/pulse) pumped by a Spectra-Physics Empower 30 Q-switched DPSS (Diode Pumped Solid State) Nd:YLF (repetition rate 1000 Hz, wavelength 527 nm, pulse energy up to 20 mJ/pulse, pulse duration 100 ns).
Femtosecond Laser installed in the CNR-ISM of Tito Scalo (PZ)
Vacuum or Reactive gas atmosphere
Femtosecond Laser
Surface Texturing – Ultrashort Laser Pulses
Femtosecond laser pulses are able to texture the surface of materials and dielectrics with periodic nanoscale structures without use of photolithographic steps

## Slide 10
Sample | Number of fs-pulses | Dose, D
OG-1 | - | -
OG-2 | 7×105 | 2.5 kJ/cm2
OG-3 | 1.4×106 | 5.0 kJ/cm2
OG-4 | 3.5×106 | 12.5 kJ/cm2
Diamond target is moved by an automated X-Y translational stage perpendicular to the laser axis with selectable speed under vacuum (P < 10-7 mbar)
It is possible to vary the number of laser pulses impingining on the sample and so the radiation dose per surface unit D
Energy of Single Pulse
Number of Pulses
Sample Area
D =
D is varied from 2.5 to 12.5 kJ/cm2
Samples used are freestanding CVD polycrystalline Optical Grade (OG) diamond plates purchased from Element Six Ltd: 8 mm Ø × 0.5 mm thickness, K>1900 W/mK, Ra < 30 nm, ρbulk > 1012 Ω∙cm
Surface Texturing – Process Parameters
Laser parameters:
 = 800 nm
Pulse duration = 100 fs
Repetition rate = 1000 Hz
Pulse energy = 3.6 mJ
Spot size = 100 um (diameter)
DOSE

## Slide 11
DOSE
OG-1 (untreated)
OG-2 (treated@2.5kJ/cm2)
OG-3 (treated @ 5kJ/cm2)
OG-4 (treated @ 12.5kJ/cm2)
Low doses (2.5 kJ/ cm2 ): the structures are not well defined
Medium doses (5 kJ/ cm2 ): defined linear structures with periodicity of 170 nm and length of several m
High doses (12.5 kJ/ cm2 ): degraded structures (post-ablation)
Surface Texturing - BLACK DIAMOND - Microstructure

## Slide 12
Surface Texturing - BLACK DIAMOND
Surface structures characterized by:
Periodicity =  / 2n = 170 nm
Depth of 400 nm
Length of several m
Raman spectroscopy, after debris removal produced by the treatment, points out:
No presence of graphitic domains
A negligible variation of the diamond peak, consistent with structural properties comparable to the untreated sample
It means that bulk physical properties do not change
P. Calvani, A. Bellucci, M. Girolami, S. Orlando, V. Valentini, A. Lettino, and D.M. Trucchi, Applied Physics A 117 (2014) 25-29
The ripples formation mechanism is debated in literature and typically attributed to the interaction of the laser pulse with the laser-induced plasma* that gives rise a periodicity close to
λr = λ/2n
λ is the wavelength of the incident laser radiation = 800 nm
n is the refractive index of diamond, n  2.41 at 800 nm.
The resulting λr = 167 nm is confirmed by SEM and AFM
Q. Wu, et al., Appl. Phys. Lett. 82, 1703 (2003);
P. P. Rajeev, et al., J. Phys. B: At. Mol. Opt. Phys. 40, S273 (2007);
B. Stuart, et al., Phys. Rev. Lett. 74, 2248 (1995);
T.J.-Y. Derrien, et al., J. Appl. Phys. 114, 083104 (2013).

## Slide 13
BLACK DIAMOND – Optical Characterization
Absorptance, reflectance, and transmittance spectra in the 200-2000 nm range highlighted:
A significant increase in absorbance for the treated samples
Absorbance is an increasing function of treatment dose D
D
Solar absorptance , defined as the normalized integral product between absorbance A and solar irradiance spectrum Wsolar
The solar absorptance values are similar at a same treatment doses independently from the values of the untreated samples
An efficient optical absorption is ONLY a NECESSARY but NOT SUFFICIENT condition for an efficient solar energy converter
ABSORBED PHOTONS have to generate CHARGE CARRIERS
P. Calvani, A. Bellucci, M. Girolami, S. Orlando, V. Valentini, R. Polini, and D.M. Trucchi , Physica Status Solidi A (2015) in press, DOI 10.1002/pssa.201532189
Thermal Grade samples (TM)
Optical Grade samples (OG)

## Slide 14
BLACK DIAMOND – Photo-Electrical Characterization
Spectral photoconductivity measurements have been performed to quantify the photogeneration capability of useful charge carriers
The external QE of the most performing sample is maximum at bandgap energy. QE ranges from 2% to 6% from about 3 eV (420 nm) to 5.1 eV ( 250 nm)
This is an excellent result, but needs to be further improved for competitive performance with solar radiation
D
A. Bellucci, P. Calvani, M. Girolami, S. Orlando, V. Valentini, R. Polini, and D.M. Trucchi , in preparation

## Slide 15
In order to disentangle the effect of:
absorption centers and
electronically defect states
natively present in the crystal from the ones induced by the periodic surface texturing, we define
Optical
D
Photoelectric
D
BLACK DIAMOND – Origin of the effect
We suppose that the subwavelength surface texturing acts
Optically as a diffraction grating smoothing the refractive index of the material
Electronically by introducing an intermediate band favoring the photogeneration

## Slide 17
Graphitic Columns for 3D Diamond Structures
Femtosecond laser is able to transform diamond into graphite according to 3D arbitrary paths and minimizing thermal effects (i.e. sharp transitions between the two carbon phases)
High electric conductivity graphitic columns with diameters down to 1 m along all the thickness can be fabricated within the diamond plate acting as distributed electrodes for thermal electrons
45 m
45 m
 = 10 m
Green
IR
power
speed
Collaboration with IIT Milan & CNR-IFN
Laser wavelength
From design (target: series resistance <<1  with 10k columns)…
…to fabrication (presently under characterization)

## Slide 18
Thank you for the Attention!
The activity was funded by the European Community within the framework of the ProME3ThE2US2 project – GA 308975
…AND THANKS TO
May 2013 - Apr 2016
www.prometheus-energy.eu
TorVergata University
Dep.t of Chemical Technologies
Riccardo POLINI – SEM characterization
Institute for Photonics & Nanotechnologies (IFN-CNR) Andrea NOTARGIACOMO – Conductive AFM
Marialilia PEA - Conductive AFM
Center for Nanotechnology of the Italian Technology Institute (IIT)
Luigino CRIANTE – Microcolumns fabrication
Sara LO TURCO - Microcolumns fabrication
TECHNION Israeli Institute of Technology Shaul MICHAELSON – Ion implantation
Alon HOFFMAN - Ion implantation

## Slide 19
Hot electrons
Thermal electrons
H
H
H
H
H
H
H
H
H
H
H
H
H
h
Band Diagram