## Slide 1: Bakelite production
Panel Production
Resistivity measurement
Panel cut -> shape of prototype chambers
Tentative time schedule
Salvatore
(on behalf of bakelite working group)

## Slide 2: Panel production
50 panels (3.2x1.6m each) produced in Puricelli firm on April 23rd for Atlas (31) and CMS (19)
CMS panel thicknesses are :
5 pcs 2mm, 7 pcs 1.6mm, 7 pcs 1.8 mm
Resistivity measured on April 28th (see next slide)
Material transported this week to Riva firm for cut

## Slide 3: Resistivity measurements
In Yellow the CMS panels
Resistivity range 3-6 ohm*cm
(CMS panels 3-4.7)
We asked Puricelli to repeat CMS panel production to achieve 0.9-2 ohm*cm : July
ID # | Thickness (mm) | Resistivity (Ohm*cm) | ID # | Thickness (mm) | Resistivity (Ohm*cm)
1 | 1,5 | 3,19 | 26 | 1,2 | 4,78
2 | 1,5 | 4,33 | 27 | 1,2 | 4,15
3 | 1 | 6,10 | 28 | 1,2 | 4,88
4 | 1,8 | 4,04 | 29 | 1,2 | 5,47
5 | 1,8 | 4,04 | 30 | 1,2 | 5,13
6 | 1,8 | 2,63 | 31 | 1 | 6,10
7 | 1,8 | 1,89 | 32 | 1 | 5,14
8 | 1,8 | 1,87 | 33 | 1 | 3,66
9 | 1,8 | 2,56 | 34 | 1 | 4,20
10 | 1,8 | 4,20 | 35 | 1 | 5,52
11 | 1,5 | 4,73 | 36 | 1 | 5,68
12 | 1,5 | 4,68 | 37 | 1 | 5,74
13 | 1,5 | 3,24 | 38 | 1 | 4,66
14 | 1,5 | 3,61 | 39 | 1 | 4,26
15 | 1,5 | 3,65 | 40 | 1 | 4,52
16 | 1,2 | 5,58 | 41 | 1 | 5,42
17 | 1,2 | 5,08 | 42 | 1 | 5,32
18 | 1,2 | 5,13 | 43 | 1 | 5,68
19 | 1,2 | 5,13 | 44 | 1 | 4,86
20 | 1,2 | 5,53 | 45 | 1 | 5,32
21 | 1,2 | 5,65 | 46 | 2 | 3,25
22 | 1,2 | 5,78 | 47 | 2 | 3,93
23 | 1,2 | 5,18 | 48 | 2 | 4,27
24 | 1,2 | 5,58 | 49 | 2 | 4,15
25 | 1,2 | 5,92 | 50 | 2 | 4,04

## Slide 4: Tentative schedule
Cut in Riva by last week
Brushing in GT by July 10th
Shipment of HPL pieces to Kodel by July 15th
Rectangular Gap production in GT by end of July (Best case of GT chambers produced by end of August)
Shipment of HPL pieces to Kodel by July 15th (Trapezoidal Gap production in Kodel September
Both rectangular and trapezoidal chambers with new bakelite ready for GIF++ test in October