## Slide 1: Stainless Steel SEY: A controversial story.
M. Angelucci1, L.A. Gonzalez1, Rosanna Larciprete1,2 and R. Cimino1
1)
2)

## Slide 2
LHC BS
in 2012:
Electron conditioning of technical 316LN stainless steel samples from RHIC and effect on the secondary electron yield with: M. Blaskiewicz and W. Fischer
There was some inconsistency and something “mysterious” in the data:
Why Scrubbing was much slower that for Cu? (the chemistry should be the same)
Why such difference in the two St. St. samples?
Why between 10-2 and 1 C/mm2 dmax seems stable (@ 1.3) and only after a huge dose it decreases again?
Intriguing in itself, no more of interest for RICH, but maybe still important for SPS.

## Slide 3
LHC BS
The Chemical origin of scrubbing was identified in 2012 for Cu:
R. Cimino et al. PRL 109 064801 (2012) & R. Larciprete PR ST (2013)
sp2
sp3
sp3
sp2
sp3
C-H
C-O
O-C=O
sp2
XPS
SEY

## Slide 4
LHC BS
C-O
C
O
Cu
H
dissociation
C film
growth
O2
reaction
CO2
CO
CO
Cu-O dissociation
O2
C-H dissociation
H2
C  sp3sp2 conversion
the contribution of all electron-induced surface reaction reduces max from 2.2 to 1.1 in Cu. It should work for St. St.
sp3
sp2
C
C
oxide reduction
The Chemical origin of scrubbing was identified in 2012 for Cu:
R. Cimino et al. PRL 109 064801 (2012) & R. Larciprete PR ST (2013)

## Slide 5
LHC BS
We repeated carefully the experiment:
Cu
St. St.
Same as before: much slower than on Cu and higher SEY value

## Slide 6
LHC BS
We repeated carefully the experiment:
Cu
St. St.
Same as before: much slower than on Cu and higher SEY value
What about the chemistry? The XPS was surprising.
After Ar
Sputtering
After
10-1 C/mm2
After
1 C/mm2
HOPG Graphite reference

## Slide 7
LHC BS
We repeated carefully the experiment:
Same as before: much slower than on Cu and higher SEY value
What about the chemistry? The XPS was surprising.
After Ar
Sputtering
After
10-1 C/mm2
After
1 C/mm2
HOPG Graphite reference
The As received St. St. shows some C
in the Bulk + The typical C in sp3 form.
The Semi scrubbed St. St. shows some C in the bulk + most C already in sp2 form.
The fully scrubbed St. St. shows some C in the bulk+ most C already in sp2 form. Identical to the Semi scrubbed
The As received St. St. shows that C is in the Bulk.
The HOPG Graphite shows the C in sp2 form as a reference.

## Slide 8
If chemistry is identical for the semi scubbed (after 10-1 C/mm2)
and the fully scubbed (after 1 C/mm2)
WHY dmax = 1.1 is not reached in both cases?
By looking at the relative intensities we see that, while the C 1s shape for intermediate and fully scrubbed is identical, the Intensity is not!
After 1 C/mm2 XPS unambiguously shows that C on the St. St. surface is more than doubled than after 10-1 C/mm2 (being in all cases in Sp2 form).
Where does this C comes from?

## Slide 9
SEY measured on the Cu-LHC BS cleaned by Ar sputtering (grey circles) and after scrubbing with 500 eV e- (Dose= 3.6 10-2 C/mm2) (red diamonds)
C 1s, core level spectra measured on the Ar sputtered (grey lines) and on the scrubbed surface (red lines).
The origin of C during scrubbing
R. Larciprete PR ST (2013)
The growing of a C layer during e- bombardment was already observed to occur when irradiating an atomically clean Cu surface, [R. Larciprete PR ST (2013)].
During long doses, not only we bombard the surface with electrons, but we expose the same surface to residual Vacuum and to the C0, C02, etc. produced by the hot filament of the gun itself.
Those molecules adsorb on the surface, where the electrons brakes them to form the sp2 C layer.

## Slide 10
+
Molecular Dose (1 ML  10-3 / 10-1 el. Dose)
Time (s) + (1 s  ~ 10-6 el. Dose)
Electron
Warning: Careful choice of the Abscissa!
Depends on:
e- Flux
Spot size
Etc.
Depends on:
base pressure (10-9 - 10-11 mBar)
Partial pressure of C containing molecules
e- Flux
Gun type and cleanliness
Surface Temperature
Etc.

## Slide 11
LHC BS
Why a C thickness increases change the SEY?
(in simple terms)
ST. St.
C
ST. St.
C
three-step process:
 production of SEs at a depth z
 transport of the SE toward the surface
emission of SE across the surface barrier
SEY electrons are produced within a semi-sphere of about 20 – 40 nm radius
secondary electron emission
dmax=1.3
dmax=1.14
dmax=1.55
dmax=1.05
SEY
ST. St.
C
SEY is intrinsically a Surface Parameter

## Slide 12
St. St. Scrubs as Cu: the chemistry is identical!
The native C content on the “as Received” St. St. surface seems less than the one on the “as Received” Cu.
Thickness matters: To reach the thickness where SEY is mainly dominated by the a-C overlayer, we need to add C-based molecules during Scrubbing.
Does this evidence play a role also in Cu?
Could this observation justify a potential difference in dmax (in both Cu and St. St.) from measurements done in the Lab. (under e- irradiation) and to what happen in the accelerator?
What if... Contaminant Layer thickness could be responsible of the different sectors behaviour in LHC?
Can we learn something (for mitigation mechanisms) from this?
Conclusion