## Slide 1
Photo Reflectivity and Photo Electron Yield
of technical surfaces
A.Liedl1, E. La Francesca1,2, M. Angelucci1, and R. Cimino1
1INFN – Laboratori Nazionali di Frascati
2Università “Sapienza “ di Roma
In collaboration with F. Schäfers and F. Siewert
Helmholtz-Zentrum, Berlin

## Slide 2
Photon Tracing (hence Reflectivity) is essential to understand where these detrimental phenomena occur
It is important to measure such quantities in condition as close as possible to operation
Synchrotron Radiation
Vacuum Chamber Wall
Absorbed Radiation
Heat Load
PhotoYield
Photo Stimulated Desorption
Seeds E-Cloud
Single bunch Instability
Heat Load
Vacuum Instability
Beam Instabilities
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces

## Slide 3
Synchrotron Radiation on High Energy Accelerator Walls
Grazing angles: e.g LHC 0.28° FCC-hh 0.07°
Radiation Energy Spectrum: from eV to several keV
R. Cimino, V. Baglin and F. Schäfers, PRL. 115 (2015) 264804
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces

## Slide 4
For such conditions, there are few experimental setups that could work close to the required geometry
A.A.Sokolov,et al,Proc.of SPIE92060J-1-13(2014)
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
Experimental Parameters
Phot. Energy range 351800 eV
Beam height h=0.3 mm
Incident Beam measurement
GaAsP Photodiodes (4x4mm) (0.1*4mm)
Incidence angle 0.1, 0.25, 0.5, 1 deg
REFLECTOMETER
BESSYII “Optics” beamline

## Slide 5
θ/2θ geometry allows to detect the specular reflected signal.
Two possible way
Fixed θ/2θ
Beam Energy Scan
Fixed Beam Energy
θ/2θ Scan
Contemporary, the current generated on the insulated sample is detected for PY
Fixed energy and incident angle.
The detector moves around the sample mapping the angular distribution of the Reflected and Scattered signal.
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
i
F
r

## Slide 6
Investigated Samples
50 mm
5 mm
LHC Cu
LHC Saw Tooth
LASE Cu
Cu (different Roughness)
Cu+ amorphous Carbon Thin Film
And: NEG, Stainless Steel, ...
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces

## Slide 7
Investigated Samples
50 mm
5 mm
LHC Cu
LHC Saw Tooth
LASE Cu
Cu (different Roughness)
Cu+ amorphous Carbon Thin Film
And: NEG, Stainless Steel, ...
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces

## Slide 8
Specular Reflectivity
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces

## Slide 9
Specular Reflectivity
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces

## Slide 10
Photon Yield
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces

## Slide 11
Photon Yield
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces

## Slide 12
Experimental Observation
Angular Distribution of Reflectivity
Integrating the angular distribution we calculate the Total Reflectivity
Angular Distribution of Reflectivity is measured keeping the incidence angle and the photon Energy fixed and mapping Reflected and Scattered radiation with the detector over the reachable Solid Angle F[0;7.4] r[0;5]
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
Detector
Acceptance angle
F
r

## Slide 13
Experimental Observation
Angular Distribution of Reflectivity
Integrating the angular distribution we calculate the Total Reflectivity
Angular Distribution of Reflectivity is measured keeping the incidence angle and the photon Energy fixed and mapping Reflected and Scattered radiation with the detector over the reachable Solid Angle F[0;7.4] r[0;5]
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
Detector
Acceptance angle
F
r

## Slide 14
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
Sample | hn (eV) | qi (deg) | Specular Reflect. (E) ( 10%) | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Sample | hn (eV) | qi (deg) |  | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Monochromatic values

## Slide 15
Sample | hn (eV) | qi (deg) | Specular Reflect. (E) ( 10%) | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Sample | hn (eV) | qi (deg) |  | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Monochromatic values
Decreasing Reflectivity
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces

## Slide 16
Sample | hn (eV) | qi (deg) | Specular Reflect. (E) ( 10%) | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Sample | hn (eV) | qi (deg) |  | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Monochromatic values
Decreasing Total Reflectivity
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces

## Slide 17
Sample | hn (eV) | qi (deg) | Specular Reflect. (E) ( 10%) | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Sample | hn (eV) | qi (deg) |  | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Monochromatic values
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
82%
65%

## Slide 18
Sample | hn (eV) | qi (deg) | Specular Reflect. (E) ( 10%) | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Sample | hn (eV) | qi (deg) |  | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Monochromatic values
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
TOP

## Slide 19
Sample | hn (eV) | qi (deg) | Specular Reflect. (E) ( 10%) | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Sample | hn (eV) | qi (deg) |  | Total Reflect. (E) (±10%) | PY (E) (±2%)
Cu + Carbon | 1500 | 0.25° | 0.77 | 0.92 | 0.09
 |  | 0.5° | 0.70 | 0.90 | 0.14
Cu Ra=9.6 nm | 1500 | 0.25° | 0.61 | 0.74 | 0.18
 |  | 0.5° | 0.57 | 0.67 | 0.30
LHC-Flat Ra=14.9 nm | 1800 | 0.25° | 0.468 | 0.722 | 0.32
 |  | 0.5° | 0.421 | 0.627 | 0.44
LHC-ST | 1800 | 0.25° | 0.0040 | 0.054 | 0.07
 |  | 0.5° | 0.0017 | 0.006 | 0.06
LASE | 1800 | 0.25° | 0.0015 | 0.007 | 0.08
 |  | 0.5° | 2.50E-05 | 0.0003 | 0.07
Monochromatic values
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
1.125
0,69
1,14
0,07
0,08
PY
(absorbed pht.)

## Slide 20
Investigated Samples
Side A
Side B
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
Sample | RMS Roughness (Ra)
Cu 1A | 9.6 nm
Cu 2A | 27 nm
Cu 1B | 25 nm
Cu 2B | 643 nm
LHC | 14.9 nm
Polished
Lapped
Cu & LHC Cu
VS
Roughness

## Slide 21
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
Specular Reflectivity VS Roughness

## Slide 22
Angular Distribution VS Roughness
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces

## Slide 23
R and PY strongly depend on :
Material, angle of incidence and photon energy
Surface Contaminants at grazing angles
Thin film Coverage
Surface finish
Surface Treatments
There are setup which allow us to study these features,
providing useful data for the simulations
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
Conclusion

## Slide 24
Italy, La Biodola Bay, Isola d'Elba 3-7June ‘18
Liedl A. et al. -Photo reflectivity and PEY of technical surfaces
Thank you for the attention!