## Slide 1
Jonathan D.A. Smith: Tech-X UK Ltd, Daresbury, Warrington, UK
Oleg Malyshev, Reza Valizadeh: ASTeC, STFC Daresbury Lab, UK
W. Allan Gillespie, Amin Abdolvand, Svetlana A. Zotlovskaya
Univ. Dundee, UK
Seth A. Veitzer, David N. Smithe, Peter H. Stoltz
Tech-X Corp. Boulder, CO, USA
Computation of Geometric Secondary Electron Yield Suppression in Metals (LASE) with VSim
ECLOUD, June 2018,
Biodola, Elba, Italy

## Slide 2: Presentation contents:
Tech-X, Tech-X UK and ECLOUD
Motivation: Experiments indicate low impedance, low SEY
Our electrostatic computational model
VSim explaining STFC experimental results
VSim helping us understand the SEY reduction process
Work in progress: Does this work for the latest structures?
What this lets us do (SEY, distribution, spectrum) : prospects for particle accelerators and satellite components.

## Slide 3: Tech-X, Tech-X UK Ltd, …
Tech-X : a computational software consulting company
Based in Boulder CO, employing about 45 staff, most with PhDs
We are research focussed, our software and researchers contributing to the seminal computational Laser Plasma Acceleration Nature paper
Our software is high performance and flexible – lending itself to research

## Slide 4: … and ECLOUD
An important source of our income is government lab research
Seth Veitzer was working on ECLOUD intermittently 2008-2015. Build up simulations (full self-consistent PIC),
Resonant Cavity vs. Travelling wave RF Diagnostics (using Linear Plasma Dielectric Simulations)

## Slide 5: This is a story about what happens when computationalists (us at Tech-X) get together with experimentalists (at STFC) to mutually increase understanding.
Aim: Characterize the mechanism by which SEY is being reduced for novel {micro|nano}-structured materials.
Build macroscopic model
  SEY=f(E(x,y,z,t),α,dir)
  dN/dtheta=f(E(x,y,z,t), α, dir)
  dE/dtheta=f(E(x,y,z,t), α, dir)
  … can add dRs(ω)/dx => impedances come from measurement
Use this model on beam pipes, spacecraft components => determine both multipactor & ecloud susceptibility and impedance/losses.
Use the understanding to design better surfaces to mitigate ECLOUD
These surfaces being (have been?) tested at CERN.

## Slide 6: My STFC colleagues took note of seeral techniques to suppress the SEY by passive means (not our work…)
Surface structures
Adapting surface chemistry:
Coating with a low SEY material with submicron size structure
See for example: I. Montero et.al, Proc. e-Cloud12
Above: KEKB Vacuum Chamber
(from Y Suetsugu)
A Krasnov
L Wang

## Slide 7: At STFC Vacuum Scientists are developing new treatments to reduce SEY (LASE)
They started out a few years ago with laser engineered surface structures.
Notes: The surface treatment (blackening) was carried out on a surface of commercially available copper (Cu), aluminium (Al), and 316L stainless steel (SS) foils with a purity of 99.999% of 1-mm thickness. Prior to laser exposure, the samples were degreased. A Nd:YVO4 laser with maximum average power of 20W at lamda=1064nm (for processing Al and stainless steel foils) and 10W at lamda=532nm (for processing Cu foil) was utilized for irradiation of the samples in an argon atmosphere at room temperature. The diameter of the laser beam focused spot on each target, between the points where the intensity has fallen to 1/e2 of the central value, was measured to be 60micron. The laser beam had a Gaussian intensity proﬁle (Msquared~1.1) and was focused onto the target surfaces using a ﬂat ﬁeld scanning lens system, a specialised lens system in which the focal plane of the deﬂected laser beam is a ﬂat surface. The average laser ﬂuences employed for processing were 6.1, 6.8, and 3.6J/cm2 for copper, aluminium, and stainless steel, respectively. The beam was raster-scanned over the surface of the targets in both the horizontal and vertical directions using a computercontrolled scanner system.27 Figure 1 shows images of Cu samples with and without the laser treatment

## Slide 8: At Daresbury lab, they have a setup to measure SEY (and also impedance and other figures of merit for the surface)
e-gun
IP, Primary electrons
IF, Secondary electrons
Faraday cup
Sample
Sample holder
A
A
VBIAS
IF
IS

## Slide 9: This setup tells us that SEY for these structures is very low
VBIAS=-18V
Original data: Jun 2014, Applied Physics Letters 12/2014; 105 (23): 231605

## Slide 10: SEY improvement applies to SS and Al
NB: Conditioning ~500eV electrons, significant flux

## Slide 11: Tech-X got involved in the simulations: has correct comp. physics capabilities for such calculations
1D/2D/3D ES or EM PIC, eg can apply external bias, dE/dz, Poisson Solve, Yee Solve.
Initial electrons with arbitrary physical and velocity distribution: Choose energy, angle.
Variable weight macroparticles – sim need not slow down towards saturation. Restart.
Furman & Pivi model (or Vaughan, or any other for SEY, dn/dE, dn/dphi, eg for dielectric)
Flat or complex structured geometry, with accurate emission from complex surfaces.
Collisions between particles, fluid, plasmas
Switch on/off space-charge
  Models saturation (Lingwood et al. 2012)
Secondaries:
  Probability/SEY, Energy Spread, Angular Spread
  Parameters may be varied by # previous impacts
  or time, position, any field that may be calculated.
Field scaling particles, Hard & Soft barriers
Separating backscattered, ‘true’ secondaries, rediffused
Monitoring particles belonging to different multipactor orders
Fields defined
and initialized
on a grid
{Ei, Bi}
Particle positions
& velocities
initialized
{xα, vα}
Particles
accelerated
by the fields
{v'α}
Particles
moved based on
new velocity
{x'α}
Charge
“deposited”
on the grid
{ρi}
New fields
computed from
charges
{E’i}
One Time Step
Initialization Steps...

## Slide 12: Tech-X got involved in the simulations: has correct comp. physics capabilities for such calculations
1D/2D/3D ES or EM PIC, eg can apply external bias, dE/dz, Poisson Solve, Yee Solve.
Initial electrons with arbitrary physical and velocity distribution: Choose energy, angle.
Variable weight macroparticles – sim need not slow down towards saturation. Restart.
Furman & Pivi model (or Vaughan, or any other for SEY, dn/dE, dn/dphi, eg for dielectric)
Flat or complex structured geometry, with accurate emission from complex surfaces.
Collisions between particles, fluid, plasmas
Switch on/off space-charge
  Models saturation (Lingwood et al. 2012)
Secondaries:
  Probability/SEY, Energy Spread, Angular Spread
  Parameters may be varied by # previous impacts
  or time, position, any field that may be calculated.
Field scaling particles, Hard & Soft barriers
Separating backscattered, ‘true’ secondaries, rediffused
Monitoring particles belonging to different multipactor orders
Fields defined
and initialized
on a grid
{Ei, Bi}
Particle positions
& velocities
initialized
{xα, vα}
Particles
accelerated
by the fields
{v'α}
Particles
moved based on
new velocity
{x'α}
Currents
“deposited”
on the grid
{Ji}
New fields
computed from
old fields
{E’ i ,B’i }
One Time Step
Initialization Steps...

## Slide 13: Tech-X got involved in the simulations: has correct comp. physics capabilities for such calculations
1D/2D/3D ES or EM PIC, eg can apply external bias, dE/dz, Poisson Solve, Yee Solve.
Initial electrons with arbitrary physical and velocity distribution: Choose energy, angle.
Variable weight macroparticles – sim need not slow down towards saturation. Restart.
Furman & Pivi model (or Vaughan, or any other for SEY, dn/dE, dn/dphi, eg for dielectric)
Flat or complex structured geometry, with accurate emission from complex surfaces.
Collisions between particles, fluid, plasmas
Switch on/off space-charge
  Models saturation (Lingwood et al. 2012)
Secondaries:
  Probability/SEY, Energy Spread, Angular Spread
  Parameters may be varied by # previous impacts
  or time, position, any field, file that may be calculated.
Field scaling particles, Hard & Soft barriers
Separating backscattered, ‘true’ secondaries, rediffused
Monitoring particles belonging to different multipactor orders

## Slide 14: Tech-X got involved in the simulations: has correct comp. physics capabilities for such calculations
1D/2D/3D ES or EM PIC, eg can apply external bias, dE/dz, Poisson Solve, Yee Solve.
Initial electrons with arbitrary physical and velocity distribution: Choose energy, angle.
Variable weight macroparticles – sim need not slow down towards saturation. Restart.
Furman & Pivi model (or Vaughan, or any other for SEY, dn/dE, dn/dphi, eg for dielectric)
Flat or complex structured geometry, with accurate emission from complex surfaces.
Collisions between particles, fluid, plasmas
Switch on/off space-charge
  Models saturation (Lingwood et al. 2012)
Secondaries:
  Probability/SEY, Energy Spread, Angular Spread
  Parameters may be varied by # previous impacts
  or time, position, any field, file that may be calculated.
Field scaling particles, Hard & Soft barriers
Separating backscattered, ‘true’ secondaries, rediffused
Monitoring particles belonging to different multipactor orders

## Slide 15: Tech-X performed 3D calculations to predict geometric factor (effective SEY)
+ parallel computation + open data format + …
Flat surface was compared to Pyramidal structure with high-to-base ratio a/b= 1 for α0 = 90 degrees and α0 = 45 degrees
Structures had height 10 to 50um.

## Slide 16: Simulation setup in
(A) (green) incident particles (not necessary normal)
(B) (red) outgoing particles
(C) periodic BCs (on or off)
(D) Electrostatic Biassed wall, Furman-Pivi applied here for particles
x (10-6)
(A)
(B)
(C)
(D)
Tested with absorbing and periodic BCs
Notes: A particle source is created at the left wall (lower x), emitting particles quasi-randomly with a uniform time and transverse spatial distribution. We start with no secondary electrons. Dirichlet conditions are applied to the fields (0 V). Matched current density in the 2014 APL papers. “
(B) As in the experiment, only secondary particles that do not go on to have further interactions with the surface matter, so only those leaving the simulation domain on the left hand side are counted in the determination of SEY.
(C) Periodic boundary conditions are applied on both particles and fields in both transverse coordinates, y and z. Particles exiting at +y are wrapped around and come back in at –y, ensuring no loss of electrons from the side of the simulation. Previous tests were performed using absorbing walls and a prescribed field with no substantial difference.
(D) Primary and secondary particles are absorbed and saved on right wall (upper x). The current and spectrum of absorbed particles may be measured here independently for each separate species. Model [6] applied on absorbed particles to determine new particle velocities and probability of generating them. We are able to apply time averaging to the current on this wall. Dirichlet conditions are applied to the fields on the flat surface, or surface of the pyramids.

## Slide 17: We measure various currents in the model to determine effective SEY away from the surface, same as experiment
(0) Primaries
Secs on right
Secs out left & sides
Tertiary+ out left & sides
Noise affects # macroparticles to use
Secondaries on right can be ignored.

## Slide 18: Behaviour of Cu SEY on complex surface close to experiment
Conditioning
(high field processing)
Bias
Incident
electrons
Lower bias
Greater bias
Resolution
Difference between “as received” and model peak SEY
Notes: Conditioning reduces the SEY from what is shown here.
The bias mechanism acts to increase the number of particles getting out to the faraday cup
Unsurprisingly the flat surface doesn’t really require high-res simulation. A more complex geometry is more sensitive to incorrect representation of the structure, and justifies handling this semi-independently from a macroscopic simulation
Since the Cu Furman Pivi model we use peaks at delta>2, it is not surprising this is reflected in our simulation results. Relevant plot from the Furman Pivi paper is shown.
Note, behaviour under these ‘ideal’ experimental conditions may not reflect behaviour in presence of (very) high fields.

## Slide 19: SEY dependence on angle is much as expected
Dependence less pronounced for laser engineered surface structure
Furman-Pivi model gives angular dependence below:
Chart: 
| -1.5707963267948966 | -1.3089969389957472 | -1.0471975511965976 | -0.78539816339744828 | -0.52359877559829882 | -0.26179938779914941 | 0 | 0.26179938779914941 | 0.52359877559829882 | 0.78539816339744828 | 1.0471975511965976 | 1.3089969389957472 | 1.5707963267948966
if all true secondaries then dependence of delta on incoming angle | 1.66 | 1.4362 | 1.2809 | 1.1598 | 1.0717 | 1.0181 | 1 | 1.0181 | 1.0717 | 1.1598 | 1.2809 | 1.4362 | 1.66
if elastic or rediffused | 1.26 | 1.2426 | 1.195 | 1.13 | 1.065 | 1.0174 | 1 | 1.0174 | 1.065 | 1.13 | 1.195 | 1.2426 | 1.26

## Slide 20: Looking at second and third+ generation particles
2nd
3rd
Notes: Grouping third and higher generations.
General slope present as electrons are being accelerated in the bias.
Tertiary and higher order particles are a much lower energy

## Slide 21: Results indicate particles likely to experience multiple impacts & move to low energy, low SEY part of curve
Vertical location above metal backplate correlates with surface area
Tertiary particles appear near 50% near tips, higher frac. near base

## Slide 22: Laser engineered surface: summary
The technique can easily be applied to existing vacuum surfaces where the improvement has to be done in-situ with minimum disturbance to the beam line/DUT.
The blackening process is carried out in air at atmospheric pressure; therefore the actual cost of mitigation is considerably lower, a fraction of the existing mitigation processes.
The process is also readily scalable to large areas.
The surface is highly reproducible and offers a very stable surface chemistry which can be influenced during the process. The surface is robust and is immune to any surface delamination which can be a detrimental problem for thin film coating

## Slide 23: Takeaway
δ < 0.6
No outgassing problems
(Insignificant?) increase in impedance
Easy implementation
Robust
Highly reproducible
Inexpensive
In-situ
Acknowledgements
Sihui Wang, Philippe Goudket, Lewis Gurran (STFC)
Graeme Burt (Lancaster Uni/Cockcroft Inst.)

## Slide 24: More recent work involves creating smaller scale structures on Cu with YAG lasers.
LOW SECONDARY ELECTRON YIELD OF LASER TREATED SURFACES OF COPPER, ALUMINIUM AND STAINLESS STEEL,
Proc IPAC2016, Busan, Korea, TUOCB02

## Slide 25: There is always a trade off with impedance
While SEY<1 for energies of interest, we are checking (simulation / experiment) higher powers.
Resistance is over double what it would be for untreated materials – acceptable?
Material treatment can be engineered to set this trade off between SEY performance and impedance.

## Slide 26: We have started to simulate these structures in
Very preliminary results:
No resolution study
Try modifying gaps between ‘balls’
More layers

## Slide 27: Outlook
… sadly our funding has run out
We are seeking to put together a new proposal
Try already validated structure with macroscopic version of the model in build-up Sim or SatCom environment (filter/diplexer?)
Build the SEY model from this latest structure modelled on the micro-scale, and use in design of some potentially susceptible filters/diplexers at the mm scale
Compare results with treatment of accelerators
Model saturation effects, thermal load, MP tailoff, and compare these with experiment

## Slide 28
Jonathan.Smith@txcorp.co.uk
www.txcorp.com/vsim
(M)ANY QUESTIONS?

## Slide 29: Sample analysis: