## Slide 1: Material science and accelerator R&D: Reflectivity and Photo Yield measurements of vacuum chamber technical surfaces
Eliana La Francesca
Dottorato in fisica degli acceleratori
(XXXI ciclo)
Relatore interno: prof. M. Migliorati
Relatore esterno: dott. R. Cimino

## Slide 2: Outline
Synchrotron radiation detrimental effects
Reflectivity and Photo Yield
Bessy II measurements
Conclusions and Future work
2
Eliana La Francesca
Roma, 16 October 2017

## Slide 3: Synchrotron Radiation detrimental effects
Photon stimulated desorption
Heat load on the accelerator walls
Production of photo emitted electrons (e- cloud effect)
3
Eliana La Francesca
Roma, 16 October 2017
Beam instability

## Slide 4
4
Eliana La Francesca
Roma, 16 October 2017
Synchrotron Radiation interaction with Matter
Reflected + Absorbed + Transmitted
Specular reflected
Scattered

## Slide 5
5
Eliana La Francesca
Roma, 16 October 2017
Synchrotron Radiation interaction with Matter
Reflected + Absorbed + Transmitted
Electron cloud effect
Heat Load
Photo-electrons
generation

## Slide 6
Photo-emitted electrons can be:
produced directly by SR (dipoles): emitted in the orbit plane (not participate to electron cloud build up).
Produced by the reflected or scattered light (dipoles and free field zone): emitted perpendicularly to the orbit plane (generate secondary electrons)
6
Eliana La Francesca
Roma, 16 October 2017
SR and electron cloud generation
Original representation F. Ruggero
Beam instability

## Slide 7
7
Eliana La Francesca
Roma, 16 October 2017
Synchrotron Radiation interaction with Matter
Reflected + Absorbed + Transmitted
Electron cloud effect
Heat Load
Photo-electrons
generation

## Slide 8: FCC Parameters
4
Parameters LHC H-L LHC FCC-hh
http://tlep.web.cern.ch/content/fcc-hh
Version 1.0 (2014-02-11)
Dipoles at
1.9 K
Eliana La Francesca
Roma, 16 October 2017
Total Power to dissipate such HL at cold bore temperature: 3 GW

## Slide 9: Synchrotron Radiation interaction with Matter
Arc SR Heat Load = 28.4 (44.3) W/m/aperture
Reflected + Absorbed + Transmitted
To be increased in cold parts (Superconductive Magnets)
To be increased in high temperature parts (absorbers)
9
R. Cimino, V. Baglin and F. Schäfers, PRL. 115 (2015) 264804
Eliana La Francesca
Roma, 16 October 2017

## Slide 10: Reflectivity
X-Ray Reflectivity depends on a limited number of parameters:
Photon energy and light polarization
Angle of incidence
Surface roughness
Material
10
Eliana La Francesca
Roma, 16 October 2017

## Slide 11: Specular Reflectivity VS Incidence angle
11
http://henke.lbl.gov/optical_constants/
Cu
Eliana La Francesca
Roma, 16 October 2017

## Slide 12: Reflectivity
X-Ray Reflectivity depends on a limited number of parameters:
Photon energy and light polarization
Angle of incidence
Surface roughness
Material
Eliana La Francesca
Roma, 16 October 2017
12

## Slide 13: Specular Reflectivity VS Roughness
13
REFLEC simulations
Eliana La Francesca
Roma, 16 October 2017
FCC-hh SR incidence angle: 0.035 deg
(0.62 mrad)

## Slide 14: Reflectivity
X-Ray Reflectivity depends on a limited number of parameters:
Photon energy and light polarization
Angle of incidence
Surface roughness
Material
14
Eliana La Francesca
Roma, 16 October 2017

## Slide 15: Specular Reflectivity VS Material
15
REFLEC simulations
Eliana La Francesca
Roma, 16 October 2017
FCC-hh SR incidence angle: 0.035 deg
(0.62 mrad)

## Slide 16: Specular Reflectivity: the case of Carbon
(C) 3.5 nm (X-ray range)
20 nm of C can reflect all photons
Attenuation depth ():
P(x)=exp(-x/)
For x= the intensity of X-rays
falls to 1/e of its value at
the surface.
15
R. Cimino, V. Baglin and F. Schäfers, PRL. 115 (2015) 264804
Eliana La Francesca
REFLEC simulations
Roma, 16 October 2017
FCC-hh SR incidence angle: 0.035 deg
(0.62 mrad)

## Slide 17: BESSY-II Optic Beamline and Reflectometer
A.A.Sokolov,et al,Proc.of SPIE92060J-1-13(2014)
Eliana La Francesca
Roma, 16 October 2017
17

## Slide 18: BESSY-II Optic Beamline and Reflectometer
Incidence angle θ: -90° – 90°
Detector in-plane 2θ: -180° – 180°
Detector off-plane χ : -4° – 4°
Sample – detector: 310 mm
Six axes sample positioning
Sample current measurement
GaAsP-Photodiodes
Detector slits, pinholes
A.A.Sokolov,et al,Proc.of SPIE92060J-1-13(2014)
18
Eliana La Francesca
Roma, 16 October 2017

## Slide 19: Bessy II Measurements
Photon Energy range 351800 eV
Beam height h=0.3 mm
Incident Beam measurement
GaAsP Photodiodes (4x4mm2) (1.2*4mm2)
Incidence angle 0.25, 0.5, 1 deg
Reflectivity measurement
Photo Yield:
PY= Ne/N
Specular Reflectivity
Specular
Total
Detector
Eliana La Francesca
Mirror
Scattered Light
19
Roma, 16 October 2017

## Slide 20
Copper samples
Eliana La Francesca
Roma, 16 October 2017
18
AFM (20x20µm2)
78.4 nm
Sample | RMS Roughness (Ra)
Cu 1A | 9.6 nm
Cu 1B | 25 nm
Cu 2A | 27 nm
Cu 2B | 643 nm
Cu 1A
Cu 2A
Cu 1A
Polished
Side A – means polished
Side B – means lapped

## Slide 21
Copper sample Cu1A and REFLEC simulations
Eliana La Francesca
Roma, 16 October 2017
At grazing incidence angle
contaminants are influencing Cu Reflectivity
21

## Slide 22
C K edge
O K edge
Cu L2,3 edge
REFLEC
BESSY II
Copper sample Cu1A and REFLEC simulations
REFLEC
At grazing incidence angle
contaminants are influencing Cu Reflectivity
Eliana La Francesca
Roma, 16 October 2017
22

## Slide 23: Specular Reflectivity VS Photon Energy
Eliana La Francesca
Cu 1A
C K edge
O K edge
Cu L2,3 edge
20
Carbon coating reduces
reflectivity at low energy
At high energy reflectivity
is significantly enhanced
Roma, 16 October 2017
Cu 1A + CC
23

## Slide 24: Photo Yield VS Photon Energy
Eliana La Francesca
C K edge
O K edge
Cu L2,3 edge
20
Carbon coating reduces
Photo Yield at high energy
Peaks correspond to absorption edge
Roma, 16 October 2017
Cu 1A
Cu 1A + CC
24

## Slide 25: Reflectivity VS Photon Energy
Eliana La Francesca
Roma, 16 October 2017
Low energy photons can be reflected even at high incidence angles
Cu 1A
25

## Slide 26: Total Reflectivity VS Specular Reflectivity
Reflectivity
5 10 15
twotheta (deg)
100
10-1
10-2
10-3
10-4
10-5
10-6
= 5 deg
small angle
scatter
wide angle
scatter
Ra=0.5 nm
hn=1500 eV
Eliana La Francesca
Sample | Specular Reflectivity | Total Reflectivity
Cu 1A | 0.61 | 0.73
Cu 1A + CC | 0.78 | 0.90
specular reflection
Ra= 10 nm
Spec. Reflectivity
Roma, 16 October 2017
Cu 1A
26

## Slide 27: Total Reflectivity VS Specular Reflectivity
27
Reflectivity
5 10 15
twotheta (deg)
100
10-1
10-2
10-3
10-4
10-5
10-6
= 5 deg
small angle
scatter
wide angle
scatter
Ra=0.5 nm
Eliana La Francesca
Sample | Specular Reflectivity | Total Reflectivity
Cu 2A | 0.32 | 0.69
Cu 2A + CC | 0.45 | 0.76
specular reflection
Roma, 16 October 2017
hn=1500 eV
Ra= 27 nm
Cu 2A

## Slide 28
Cu data (full line)
Cu + CC data (dashed line)
hn=1500 eV
hn=1500eV
Angular distribution of Reflectivity (in plane)
Eliana La Francesca
Roma, 16 October 2017
Cu 2A
Cu 1A
28

## Slide 29
qi=0.25 deg
hn=1500 eV
Angular distribution of Reflectivity (off plane)
Eliana La Francesca
Roma, 16 October 2017
Cu 2A
Cu 1A

## Slide 30
Photo Yield VS Incidence angle
Eliana La Francesca
Preliminary Results:
little dependence on roughness
Carbon coating seems to reduce PY
Sample | Cu 1A (Ra=9.6 nm) Max value | Cu 2A (Ra=27 nm) Max value
Cu | 0.47 | 0.46
Cu + CC | 0.23 | 0.15
Tech. Surf
hn= 1800 eV
PY= Ne/N
Roma, 16 October 2017
30

## Slide 31: Conclusions and Future work
At grazing incidence angle contaminants deeply influence Reflectivity.
For technical surfaces scattered light cannot be neglected.
Photo Yield does not seem to significantly depend on roughness.
Carbon coating seems to increase Total Reflectivity and reduce absorption and related Heat Load.
In the next year we plan to continue the measurements and analysis on different technical materials.
31
Eliana La Francesca
Roma, 16 October 2017

## Slide 32: Thank you for your attention.
Eliana La Francesca
Roma, 16 October 2017