## Slide 2
COLDEX:
a tool to study cold surfaces in accelerators
V. Baglin
CERN TE-VSC, Geneva
https://agenda.infn.it/conferenceDisplay.py?ovw=True&confId=13351

## Slide 3
Outline
Experimental
Cu surface
a-Carbon coated surface
Laser treated surface
Summary

## Slide 4
1. Experimental

## Slide 5
LHC Cryogenic Vacuum System
Cold bore (CB) at 1.9 K which ensures leak tightness
Beam screen (BS) at 5-20 K which intercepts thermal loads and acts as a screen
Courtesy N. Kos CERN AT/VAC

## Slide 6
LHC vs SPS Beam parameters
Parameters
LHC
SPS
Beam energy (GeV)
7 000
26
450
Bunch length (ns)
1
2.8
1.7
Revolution period (s)
89
23
Batch spacing (ns)
-
225
Beam current (mA)
560
55 / 110 / 165 / 220
Number of batches
-
1 / 2 / 3 / 4
Number of bunches
2808
72 / 144 / 216 / 288
Filling factor (%)
79
9 / 16 / 24 / 31
Bunch current (protons/bunch)
1.1 1011
Bunch spacing (ns)
25
SPS is the injector of the LHC
A cycle is ~ 42 s during which the beam energy is ramped from 26 GeV to 450 GeV
1 to 4 batches of 72 bunches can be injected into LHC
   SPS can be used as a test bed to simulate the LHC

## Slide 7
COLDEX: A Bench to Study Electron Cloud
The COLDEX set up is installed in a bypass of SPS BA4 since 2002 to study electron cloud effects
It mimics a LHC type cryogenic beam vacuum system (no magnetic field)

## Slide 8
Experimental set up
COLDEX cryostat:
  A 2 m long LHC type cryogenic beam vacuum system
  A beam screen temperature from 10 to ~ 100 K and a cold bore temperature from 3 to 4.5 K
  Circular beam screen (ID 67 mm), with 1 % slots transparency (2x7.5 mm)
Measurement of pressure, heat load and electron activity without and with gas condensates
RT calorimeter
(WAMPAC)
Electrodes
RT Chimney
Solenoids

## Slide 9
Instrumentation
A chimney, located in the middle of COLDEX, collected the gas from the BS held at cryogenic temperature
Electrodes are inserted into the chimney and behind the BS slots
Solenoids are wrapped at the COLDEX extremities
Chimney
Chimney
electrode
Chimney
port
BS electrode
Solenoids
WAMPAC position

## Slide 10
Instrumentation
Total and partial pressures can be measured in the centre and at the extremities
Heat load onto the BS can be derived from temperature sensors and He flow meters
Warm calorimeters (WAMPAC) are installed at each extremities
Cold warm transitions (CWT) are installed at each extremities
Gas injection system
CWT
Gas injection system
WAMPAC

## Slide 11
2. Cu surface

## Slide 12
LHC Beam Screens Functionalities
Intercept the heat load induced by the circulating beam
Operate between 5 and 20 K
Pumping holes to control the gas density
Cu surface with sawtooth structure to reduce PEY and forward scattering
Courtesy N. Kos CERN TE/VSC
An innovative and complex system, produced at several 10 km scale !
Functional design map of beam screen
P. Lebrun et al. Proc. of ICEC 24, Fukuoka, Japan, May 2012.

## Slide 13
2002:
  OFE Cu, 2.2 m long, elliptical shape, H=84 mm, V = 66 mm
  1 % holes (7 mm diameter)
2003:
  OFE Cu, 2.2 m long, circular, D= 67 mm (cleaned following LHC standard)
  1 % slots (2 x 7.5 mm)
OFE Cu beam screen

## Slide 14
Electron cloud signatures (1)
Electron cloud current is detected at both electrodes
Heat load is measured on the beam screen
Threshold at 7 1010 ppb
V. Baglin et al., CERN LHC PR 721, 2004
B. Spataro et. al, NIM A, 581, (2007)881-889
Estimated δmax from PyCloud simulation by R. Salemme: δmax = 1.4

## Slide 15
Electron cloud signatures (2)
Electron cloud is reduced with 75 ns bunch spacing
Bunch spacing ns | EC activity µA | Heat load W/m
75 | 1.6 | 0.2
25 | 20 | 1.4

## Slide 16
Beam scrubbing
Scrubbing run 2003 : 12 A.h
Normalised to 4 batches with ~ 1.1 1011 protons/bunch, 95 % duty cycle
Heat load (HL) onto the BS is decreasing with electron dose : beam conditioning
Final heat load ~ 1.5 W/m
HL = 1.9 exp(-D/70)
Electron dose ~ 20 mC/mm2
for estimated <85> eV
No heat load is dissipated onto the CB thanks to the electron shields
BS = 13 K
CB = 3 K
V. Baglin et al., CERN LHC PR 721, 2004

## Slide 17
Pressure observations
Strong dynamic outgassing dominated by H2
H2 recycling of physisorbed molecules
Electron flux ~ 6 1016 e-/m/s (if 100 eV e-)
 ~ 5 10-2 H2/ e-
Other molecules, ~ low recycling :
( + ’)/  ~ 2 10-2 to 2 10-1 molecules/ e-
Long term beam circulation (2002)
2 batches with ~ 1.1 1011 protons/bunch, 95 % duty cycle
BS ~ 8 K, CB ~ 4.2 K
Equilibrium, H2 pumped by slots
V. Baglin et al., Vacuum 73 (2004) 201-206

## Slide 18
Comparison with RT data
V. Baglin et al., CERN LHC PR 721, 2004
COLDEX
BS at 13 K, CB at 3 K
WAMPAC 3 at RT
Heat load measured at room temperature (with WAMPAC3) and at cryogenic temperature (with COLDEX) are the same
Estimated δmax = 1.3 from simulation (by F. Zimmermann)
  SEY curves at RT and cryogenic temperature are the same
   Beam scrubbing reduces SEY
F. Zimmermann, April 2004.

## Slide 19
Impact of Thin Gas Condensates: BS ~ 5 K, CB ~ 3K
1015 H2/cm2
  Large pressure increase up to 6 10-8 Torr
  ’ /  ~ 3 H2/e-
  HL < 0.1 W/m
  Fast flushing of gas < 0.01 A.h
5 1015 CO/cm2
  Pressure increase up to 10-8 Torr
  ’ /  ~ 0.4 CO/e-
  HL < 0.1 W/m
  Slow flushing of gas > 0.5 A.h
V. Baglin, B. Jenninger, Proc. of EPAC’04, Luzern, Switzerland

## Slide 20
Electron Cloud induced CO2 Cracking
15 1015 CO2/cm2:
  Pressure increase up to 10-8 Torr
  Cracking of CO2 into CO and O2 : PCO2 / PCO ~ 7
  ’ /  ~ 0.01 CO2/e-
  HL due to physisorbed gas < 0.1 W/m
  Slow flushing of gas > 0.5 A.h
V. Baglin, B. Jenninger, Proc. of EPAC’04, Luzern, Switzerland

## Slide 21
Impact of Thick Gas Condensates
60 1015 CO/cm2
Large heat load up to 6 W/m
Over a long period (slow flushing) larger than 1.5 A.h
Physisorbed gas can be redistributed e.g. after a magnet quench.
This might have consequences on the pressure level and also heat load onto the cryogenic system.
BS heaters are installed to flush the gas towards the CB.
V. Baglin,
Proc. of LHC Project Workshop 2004, Chamonix, France
V. Baglin, B. Jenninger,
Proc. of EPAC’04, Luzern, Switzerland

## Slide 22
H2O condensation
Observation of beam conditioning accompanied with heat load increase !!
~ 6 W/m heat load onto the cryogenic system when the SPS machine is filled by only 24 % with LHC nominal beams (2 x 72b) !
Disappeared after beam screen warm up to 240 K
Origin of the heat load is attributed to H2O condensation onto the beam screen
V. Baglin et al., Vacuum 73 (2004) 201-206
N. Hilleret et. al. Chamonix 2000
δmax = 1.9
at 30 monolayers
 The beam screen surface shall remain bare of physisorbed / condensed molecules

## Slide 23
3. a-C coated surface

## Slide 24
HL-LHC Project
 | LHC Design |  |  | HL-LHC
 | Nominal |  | Ultimate | Nominal
Energy [TeV] | 7 |  |  | 
Luminosity [x1034 cm-2.s-1] | 1.0 | 2.3 |  | 5*
Current [mA] | 584 | 860 |  | 1090
Proton per bunch [x1011] | 1.15 | 1.7 |  | 2.2
Number of bunches | 2808 |  |  | 2736
Bunch spacing [ns] | 25 |  |  | 
Minimum * [m] | 0.55 |  |  | 0.15
Noramlized emittance [μm] | 3.75 |  |  | 2.5
  The HL-LHC Project is a program which consists of multiplying by ~ 5 the LHC luminosity with an objective of 3 000 fb-1 accumulated in the mid 2030ies.
  For this purpose, the optics, the matching section and the inner triplet around ATLAS and CMS are completely rebuilt and shall be ready for operation by the ~ 2026.
ECLOUD'18, La Biodola Bay, Isola d'Elba, Italy 3 - 7 June, 2018

## Slide 25
Shielded Beam Screen
  Around the experiments, the final focussing quadrupoles need to be shielded against the collision debris produced at the interaction point.
Tungsten alloy (Inermet) to intercept the debris produced at the IP
100-200 nm thick a-C coated onto 80 μm copper co-laminated beam screen
Operating temperature : 40 – 60 K (base line under review) with the cold bore at 1.9 K
Length ~ 10 m, weight ~ 500 kg , transparency for pumping ~ 2 %
Courtesy C. Garion TE-VSC
ECLOUD'18, La Biodola Bay, Isola d'Elba, Italy 3 - 7 June, 2018

## Slide 26
a-C Coating for Electron Cloud Mitigation
  a-C coating is proposed to mitigate electron multipacting to reduce the heat load on the beam screen and the background to the experiments.
  It has a maximum SEY of 1 +/- 0.1 ==> no or little multipacting is expected
  The coating is currently under evaluation at cryogenic temperature in the laboratory and with LHC type protons beams in COLDEX.
  Performances at cryogenic temperature of a-C shall be compatible with HL-LHC parameters, in particular with the BS operating temperature of the triplets (40-60 K)
The a-C coating is a key technology for the HL-LHC project
P. Costa Pinto et al., Vacuum 98 (2013) 29-36
ECLOUD'18, La Biodola Bay, Isola d'Elba, Italy 3 - 7 June, 2018

## Slide 27
a-C coated COLDEX beam screen
~2.2 m, ID 67 beam screen
Cu OFE, 1% slots
Internally coated with amorphous carbon
Thickness ~500 nm
Studies in 2015-2016

## Slide 28
H2 adsorption isotherm
The cryosorption capacity for H2 is ≥ 2∙1017 H2/cm2 below 10 K
It is intermediate between metallic surfaces and common cryosorbers
  a-C coating is porous:
     With the presence of C, the porosity contributes to the low SEYmax !
R. Salemme et al., Proc. of IPAC2016, Busan, Korea

## Slide 29
Thermal desorption studies with CB>150K
H2 is desorbed in the range 40-60 K: the actual HL-LHC baseline operating range!
N2 and CO are desorbed above 80 K
Operating temperature must be carefully studied
The activation energy (temperature) for desorption (release) is a function of the surface coverage
R. Salemme et al.,
Proc. of IPAC2016, Busan, Korea

## Slide 30
Thermal desorption spectroscopy
Study as a function of surface coverage for usual gases
Peak in | H2 | CH4 | CO | CO2
40-60 K | Any coverage | For coverage > 1017 CH4/cm2 | For coverage > 2 1016 CO/cm2 | For coverage > 1018 CO2/cm2
60-80 K | A few monolayers ? |  |  | 
  The larger the coverage, the lower the desorption temperature.
  Binding energies are in the range 100-500 meV and decrease with surface coverage
  Is the 60-80 K window appropriate for HL?
A-L. Lamure et al., Presented at 64th AVS, Tampa, FL, USA, Oct, 2017

## Slide 31
Observation of beam-gas ionisation
COLDEX’s electrode is sensitive enough to measure beam gas ionisation!
Sensitivity ~ 0.1 nA i.e. ~4∙106 e-/(mm2 s)
Electron/ion
current
a-C, pressure bump
P at extremities
Beam circulating
intensity
Data courtesy R. Salemme

## Slide 32
Observation with LHC type beams
Long term irradiation with 4x72 bunches, 25 ns, up to 1.5∙1011 ppb:
  BS at 10 K, CB from 4.5 to 3 K
  No pressure rise larger than a few 10-10 mbar
  No significant heat load (≤0.2 W/m compared to 1.4 W/m for scrubbed Cu)
  No significant current on pick-up (<5 nA compared to >1000 nA for copper)
Effect of operating temperature and gas adsorption:
  No dynamic pressure larger than 10-9 mbar due to ESD is observed for:
    bare surface at 10, 50 or 80 K
    surface coverages of:
      ~3 1016 H2/cm2 , ~2 1016 CO/cm2, ~3 1016 CO2/cm2
  Measured dynamic heat load are within:
    0.2 +/- 0.1 W/m for all studied cases
  No multipacting electron activity is measured above 0.1 nA

## Slide 33
a-C coating performance at cryogenic temperature
2015 detection limit
2016 detection limit
SEY ≤ 1.1
Current measurements are more sensitive than heat load measurements
No multipacting electron activity is measured above 0.1 nA
The secondary electron yield can be estimated from simulations:
δmax < 1.1
Data courtesy R. Salemme

## Slide 34
4. Laser treated surface

## Slide 35
Laser treated COLDEX beam screen
Studies started in 2017: preliminary results!
~2.2 m, ID 67 beam screen made of 9 segments
1% perforated with slots (7.5x2)
Laser treated segments treated in collaboration with STFC – University of Dundee
Laser treatment parameters:
  Under N2,
  532 nm (2.3 eV), repetition rate = 200 kHz
  Pulse length < 15 ps
  Focal spot diameter = 12 µm
LESS treatment is of type “C2”
  A single groove with “cauliflower” like shape on the top of the ridge
  Grooves are perpendicular to the beam
~ 23 μm
~ 3 μm
Depth ~ 10 μm
  Intensity = 0.4 TW/cm2 (1030 ph/s/cm2)
  Rotating speed = 10 mm/s
  Advancing speed = 1-2 µm/s

## Slide 36
Laser treated COLDEX beam screen
Electron shield
BS electrode
Slots
RF fingers

## Slide 37
Laser treated WAMPAC 5.3
a 216 mm long WArm MultiPActing Calorimeter (WAMPAC 5.3) made of laser treated copper was also built and installed in the COLDEX experiment
A dummy segment was used to measure SEY in the laboratory
  SEYmax = 0.9 at room temperature
s = 1.88
E0 = 150 eV
Measurement by E. Garcia, curve fitting by R. Salemme

## Slide 38
Pressure signal
At 10 K
  ΔP < 10-10 mbar
At 50 K
  ΔP ~ a few 10-9 mbar
  H2 is the main gas (right, white curve)
  Solenoids do not reduce the pressure rise
     desorption is happening inside COLDEX
mbar

## Slide 39
Electron activity
When scanning the applied voltage from 0 to 80 V in step of 20 V, electron current up to ~ 0.1 μA was measured at the beam screen electrode
Applying a solenoid field at the COLDEX extremity did not reduced significantly the measured current with the electrode voltage set at 500 V
Solenoids ON
Solenoids OFF
  Collected electrons are produced inside the beam screen
NB: The chimney electrode did not measured any current above 5 nA

## Slide 40
Heat load
On the beam screen held at cryogenic temperature:
  observed heat load ≤ 0.5 W/m
At room temperature, heat load are observed on the Cu and LESS WAMPACs:
  WAMPACs are in-situ calibrated by Joule effect (sensitivity ~ 70 mW/m)
  Cu: 0.9 W/m (in agreement with previous observations and δmax~1.3)
  Laser treated surface: 0.2 W/m
  all sources included (electrons, ions, impedance, losses)
Cu WAMPAC
LESS WAMPAC
ΔT = 1.3 K
ΔT = 0.3 K
Beam off
Beam off

## Slide 41
5. Conclusions

## Slide 42
Summary
Electron cloud studies with surface held at cryogenic temperature are of primary importance for superconducting storage rings
OFE Cu surface:
  in the range 10-20 K behave like RT surface
  Electron cloud stimulate gas desorption, (fast or slow) recycling and cracking of molecules
  reaches SEYmax ~ 1.3-1.4 after ~ 20 A.h beam scrubbing
  are prone to large heat load / pressure rise when thick layers of gas are condensed on the surface
a-C coated surface (~500 nm):
  are porous and might cryo-trap molecules
  are not prone to multipacting in the range 10-80 K even when several monolayers of gas are condensed
      SEY max < 1.1
Preliminary results on laser treated surface (grooves 10 µm, particles 3 µm) indicates:
  pressure rise, electron activity at 50 K
  heat load (~ 0.2 W/m) at room temperature

## Slide 43
O. Gröbner, C. Grünhagel, B. Jenninger, I. Collins, R. Salemme for their expertise and their commitment to the success of the COLDEX experiment
STFC, University of Dundee, TE-VSC and EN-MME colleagues for the production of COLDEX beam screens
TE-CRG and BE-OP for providing a high quality of support with excellent cryogenic and beam performances during the studies
AB&TE departments, the HL-LHC project and the FCC study office for their support
Acknowledgments

## Slide 44
References
Performance of a cryogenic vacuum system (COLDEX) with an LHC type beam. V. Baglin, I.R. Collins, B. Jenninger. Vacuum 73 (2004) 201-2016.
Pressure and heat load in a LHC type cryogenic vacuum system subjected to electron cloud. V. Baglin, B. Jenninger. Proc. of ECLOUD’04, Napa, Ca, USA, April 2004.
Gas condensate onto a LHC type cryogenic vacuum system subjected to electron cloud. V. Baglin, B. Jenninger. Proc. of EPAC’04, Lucerne, Switzerland, July 2004.
Impedances of the cold bore experiment, COLDEX, installed in the SPS machine. B. Spataro et al. Nucl. Instr. And Meth. A 564 (2006) 38-43.
Coupling impedance studies and power loss measurement of the COLDEX upgraded vacuum chamber. B. Spataro et al. Nucl. Instr. And Meth. A 581 (2007) 885-889.
Recommissioning of the COLDEX experiment at CERN. R. Salemme et al. Proc. of IPAC2015, Richmond, VA, USA, May 2015.
Amorphous carbon coatings at cryogenic temperatures with LHC type beams: first results with the COLDEX experiment. R. Salemme et al. Proc. of IPAC2015, Richmond, VA, USA, May 2015.
Vacuum performance of amorphous carbon coating at cryogenic temperature with presence of proton beams. R. Salemme et al. Proc. of IPAC2016, Busan, Korea, May 2016.
First beam test of laser engineered surface structures (LESS) at cryogenic temperature in CERN SPS accelerator. R. Salemme et al. Proc. of IPAC2017, Copenhagen, Denmark, May 2017.

## Slide 45
Thank you for your attention !!!

## Slide 46
Back up slides

## Slide 47
PyCloud simulation
COLDEX ID 67, no magnetic field, SPS, 4 batches, 25 ns bunch spacing
R. Salemme

## Slide 48
ECloud simulation
COLDEX & WAMPAC3 ID 67, no magnetic field, SPS, 4 batches, 25 bunch spacing, 1.1 1011 ppb
F. Zimmerman

## Slide 49
A Natural Warm Up of a St. Steel Cold Bore
ECLOUD'18, La Biodola Bay, Isola d'Elba, Italy 3 - 7 June, 2018

## Slide 50
Laser treated surface natural warm up
Beam screen desorbed first (CB at 2.8 K)
H2 desorption peak is observed between 20-30 K
N2 and (or) CO is desorbed between 30-35 K
H2
CO/N2
14

## Slide 51
SEY of condensed gas at cryogenic temperature
As received surface
For large surface coverage (> 10-20), the SEY is defined by the condensed layer.
A. Kuzucan et al. J. Vac. Sci. A. 30, 051401, (2012)
Chart: CO2
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 15 | 20 | 25 | 30 | 35 | 40
Aluminium | 3.06 | 2.38 | 2.18 | 1.98 | 1.85 | 1.78 | 1.74 | 1.71 | 1.7 | 1.71 | 1.72 | 1.83 | 1.91 | 1.95 | 1.96 | 1.94 | 1.94
Copper | 2 | 1.71 | 1.65 | 1.6 | 1.63 | 1.72 | 1.79 | 1.9 | 1.94 | 2
e.p.Copper | 1.67 | 1.63 | 1.71 | 1.73 | 1.77 | 1.79 | 1.81 | 1.83 | 1.83 | 1.9 | 1.97 | 1.99 | 2.04
Chart: CO
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 15 | 20
Aluminium | 3.06 | 1.68 | 1.35 | 1.29 | 1.25 | 1.2 | 1.2 | 1.21 | 1.21 | 1.23 | 1.24 | 1.28 | 1.3
Copper | 2 | 1.77 | 1.68 | 1.6 | 1.44 | 1.37 | 1.28 | 1.23 | 1.2 | 1.19 | 1.18 | 1.19 | 1.24 | 1.24 | 1.22 | 1.25 | 1.28
e.p.Copper | 1.67 | 1.46 | 1.34 | 1.28 | 1.26 | 1.26 | 1.26 | 1.26 | 1.27 | 1.27 | 1.27 | 1.31 | 1.32
Chart: CH4
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45
Aluminium | 3.06 | 2.36 | 2.23 | 2.12 | 2.01 | 1.93 | 1.84 | 1.76 | 1.7 | 1.67 | 1.64 | 1.56 | 1.48 | 1.47 | 1.48 | 1.47 | 1.45 | 1.46
Copper | 2 | 1.78 | 1.71 | 1.7 | 1.69 | 1.69 | 1.68 | 1.61 | 1.55 | 1.47 | 1.5
e.p.Copper | 1.67 | 1.62 | 1.64 | 1.67 | 1.71 | 1.72 | 1.69 | 1.67 | 1.63 | 1.63 | 1.62 | 1.6
Chart: N2
| 0 | 1 | 2 | 3 | 5 | 6 | 8 | 9 | 10 | 15 | 20 | 25
Aluminium | 3.06 | 2.29 | 1.56 | 1.42 | 1.42 | 1.45 | 1.48 | 1.51 | 1.54 | 1.65 | 1.69 | 1.7
Copper | 2.05 | 1.41 | 1.33 | 1.33 | 1.36 | 1.44 | 1.49 | 1.7 | 1.74 | 1.75 | 1.81 | 1.87
e.p.Copper | 1.67 | 1.31 | 1.31 | 1.35 | 1.39 | 1.45 | 1.5 | 1.55 | 1.59 | 1.62 | 1.66 | 1.77 | 1.82 | 1.83